Production of xylooligosaccharides and monosaccharides from poplar by a two-step acetic acid and peroxide/acetic acid pretreatment

Peiyao Wen1, Tian Zhang1, Jinye Wang1, Zhina Lian2, Junhua Zhang1, 2*

Corresponding author. Tel.: +86-13892883052; fax: +86-29-87082216.

E-mail address: junhuazhang@nwafu.edu.cn (J. Zhang)

Peiyao Wen, e-mail address: wenpeiyao@nwafu.edu.cn

Tian Zhang, e-mail address:15002906131@163.com

Jinye Wang, e-mail address: wjy6520@nwafu.edu.cn

Zhina Lian, e-mail address: zhinalian@163.com

Table S1 The AC concentration of AC pretreatment liquor.

| AC concentration before pretreatment ( mg/mL) | Treatment time | AC concentration after pretreatment (mg/mL) |
| --- | --- | --- |
| 0.0 | 10 min | 0.21±0.00 |
| 5.2 | 10 min | 3.49±0.08 |
| 10.5 | 10 min | 7.60±0.11 |
| 0.0 | 30 min | 0.22±0.04 |
| 5.2 | 30 min | 4.68±0.23 |
| 10.5 | 30 min | 8.41±0.21 |
| 0.0 | 50 min | 0.23±0.09 |
| 5.2 | 50 min | 4.70±0.14 |
| 10.5 | 50 min | 8.41±0.16 |

\

Figure S1 XRD analysis of raw and two steps pretreated poplar.

Figure S2 FT-IR spectrum of raw and two steps pretreated poplar.

First step pretreatment

Second step pretreatment

Figure S3 XPS analysis of raw and two steps pretreated poplar.

Figure S4 Hydrophobicity of raw and two steps pretreated poplar.

Raw

The first step pretreatment

0% AC, 30 min

5% AC, 30 min

10% AC, 30 min

The second step pretreatment

40% HPAC, 60 °C

80% HPAC, 60 °C

60% HPAC, 60 °C

Figure S5 SEM analysis of raw and two steps pretreated poplar.

Figure S6 Effect of CTec2 loading on the hydrolysis of poplar (2%) pretreated by AC (5%, 170°C, 30 min) for 48 h.