Sequential catalytic lignin valorization and bio-ethanol production: an integrated biorefinery strategy

Yilu Wu a, Changsheng Su a, Zicheng Liao b, Gege Zhang c, Yongjie Jiang a, Yankun Wang a, Changwei Zhang a, Di Cai a,*, Peiyong Qin b, Tianwei Tan a

a National Energy R&D Center for Biorefinery, Beijing University of Chemical Technology, Beijing 100029, PR China

b College of Life Science and Technology, Beijing University of Chemical Technology, Beijing 100029, PR China

c School of International Education, Beijing University of Chemical Technology, Beijing 100029, PR China

Corresponding author

Email: caidibuct@163.com (D. Cai)

Fig. S1 (A) Scatter plot of δT versus lignin monomers yields with different ratios of 2-PrOH:H2O (v/v) in initial liquor. (B) Scatter plot of δT versus delignification of pulps with different ratios of 2-PrOH:H2O (v/v) in initial liquor. (C) Scatter plot of RED versus lignin monomers yields with different ratios of 2-PrOH/H2O in initial liquor. (D) Scatter plot of RED versus delignification of pulps with different ratios of 2-PrOH/H2O in initial liquor.

Fig. S2 SEM images of RCF pulps using the pulping liquor with different 2-PrOH:H2O ratios. (A)-(F) represented to the raw poplar sawdust, and the pulps after RCF using the liquor that consisted of 1:9, 3:7, 5:5. 7:3 and 9:1 of 2-PrOH:H2O (v/v), respectively.

Fig. S3 Fermentation performances of the parent S. cerevisiae and engineered S. cerevisiae strains for ethanol production using the YPX medium containing 40 g/L of xylose. Time course of (A) OD600, (B) xylose, and (C) ethanol concentration in batch fermentation process. (D) Comparison of ethanol concentration, yield, and OD600max in YPD medium using different strains.

Table S1 Sugar concentrations after enzymatic hydrolysis of RCF pulps by different ratios of 2-PrOH:H2O (v/v).

| 6 wt% solid dosage | Glucose concentration (g/L) | Xylose concentration (g/L) | Total sugar concentration (g/L) |
| --- | --- | --- | --- |
| 1:9 | 28.10±0.12 | 1.64±0.08 | 29.74±0.25 |
| 3:7 | 36.42±0.15 | 3.38±0.21 | 39.80±0.32 |
| 5:5 | 35.42±1.26 | 4.51±0.28 | 39.93±1.67 |
| 7:3 | 29.60±0.34 | 4.38±0.33 | 33.98±0.62 |
| 9:1 | 17.71±0.09 | 3.92±0.10 | 21.63±0.31 |
| 12 wt% solid dosage | Glucose concentration (g/L) | Xylose concentration (g/L) | otal sugar concentration (g/L) |
| 1:9 | 42.17±0.15 | 3.23±0.15 | 45.40±0.76 |
| 3:7 | 55.20±0.38 | 5.70±0.33 | 60.90±0.67 |
| 5:5 | 55.80±1.03 | 7.65±0.75 | 63.45±0.39 |
| 7:3 | 45.60±0.78 | 7.47±0.45 | 53.07±0.46 |
| 9:1 | 30.18±0.62 | 6.00±0.23 | 36.18±0.62 |

Table S2 Yield of RCF oil (wt%) using different ratios of 2-PrOH:H2O (v/v) as initial liquor, in which process 11.70 g dry poplar sawdust was mixture with the initial liquor for before fractionation.

| 2-PrOH:H2O (v/v) | 1:9 | 3:7 | 5:5 | 7:3 | 9:1 |
| --- | --- | --- | --- | --- | --- |
| Mass (g) | 2.003 ± 0.027 | 2.135 ± 0.020 | 2.289 ± 0.013 | 2.416 ± 0.020 | 2.420 ± 0.033 |
| Yield (wt%) | 17.12 ± 0.41 | 18.25 ± 0.33 | 19.56 ± 0.26 | 20.65 ± 0.31 | 20.63 ± 0.44 |

Table S3 Hildebrand solubility parameter (δT) and HSP (δD, δP, δH) for selected solvents (2-PrOH:H2O) and poplar lignin.

|  | δD (MPa½) | δP (MPa½) | δH (MPa½) | δT (MPa½) | RED |
| --- | --- | --- | --- | --- | --- |
| Lignin [1] | 21.9 | 14.1 | 16.9 | 31.0 | / |
| 2-PrOH [2] | 15.8 | 6.1 | 16.4 | 23.6 | 1.07 |
| H2O [3] | 15.5 | 16.0 | 42.3 | 47.8 | 2.10 |
| 1:9 | 15.5 | 15.0 | 39.7 | 45.2 | 1.92 |
| 3:7 | 15.6 | 13.0 | 34.5 | 40.1 | 1.60 |
| 5:5 | 15.7 | 11.1 | 29.4 | 35.0 | 1.32 |
| 7:3 | 15.7 | 9.1 | 24.2 | 30.2 | 1.12 |
| 9:1 | 15.8 | 7.1 | 19.0 | 25.7 | 1.05 |

The δ-values of aqueous solutions of selected solvents (2-PrOH:H2O) are calculated by δM = φ1δ1 + φ2δ2, where φ is the volume fraction of the 2-PrOH (index 1) or H2O (index 2), and δ is the δ-value of 2-PrOH (index 1) or H2O (index 2) [4].

δT2 = δD2+δP2+δH2, δT represented Hildebrand solubility parameter.

RED: Relative energy difference, was used to determine the miscibility of poplar lignin with selected solvents (2-PrOH:H2O). RED = Ra / R0. R0 is the radius of the Hansen sphere obtained by a computerized optimization method as described above. Ra2 = 4(δD1-δD2)2+(δP1-δP2)2+(δH1-δH2)2. The “1” referred to the selected solvents and “2” referred to lignin [2, 3].

Table S4 Molecular weight distribution of the lignin oil fractionated by different proportion of 2-PrOH:H2O (v/v) in the initial liquor.

| 2-PrOH:H2O (v/v) | Mn (Da) | Mw (Da) | PDI |
| --- | --- | --- | --- |
| 1:9 | 620 | 1050 | 1.694 |
| 3:7 | 681 | 1101 | 1.616 |
| 5:5 | 723 | 1282 | 1.773 |
| 7:3 | 724 | 1255 | 1.735 |
| 9:1 | 904 | 1114 | 1.233 |

Table S5 Lignin monomers yield (wt%, lignin monomers yield=lignin monomers mass in the lignin oil / raw poplar sawdust × 100 %) using different proportion of 2-PrOH:H2O (v/v) in initial liquor.

| Types a | Lignin monomers | Lignin monomers yields (wt%) using different proportion of 2-PrOH:H2O (v/v) in initial liquor |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 1:9 | 3:7 | 5:5 | 7:3 | 9:1 |
| S | 4-(3-Hydroxypropyl)-2,6-dimethoxyphenol | 0.83 | 2.01 | 1.84 | 2.00 | 1.00 |
|  | 4-Propyl-2,6-dimethoxyphenol | 0.28 | 0.21 | 0.17 | 0.16 | 0.08 |
|  | 4-Ethyl-2,6-dimethoxyphenol | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
|  | 4-Methyl-2,6-dimethoxyphenol | 0.07 | 0.01 | 0.25 | 0.35 | 0.04 |
|  | 2,6-Dimethoxyphenol | 0.02 | 0.03 | 0.01 | 0.02 | 0.04 |
| G | 4-(3-Hydroxypropyl)-2-methoxyphenol | 0.44 | 0.99 | 0.72 | 0.78 | 0.48 |
|  | 4-Propylguaiacol | 0.07 | 0.05 | 0.07 | 0.08 | 0.02 |
|  | 4-Ethyl-guaiacol | 0.26 | 0.13 | 0.30 | 0.29 | 0.11 |
|  | 4-Methylguaiacol | 0.07 | 0.07 | 0.03 | 0.03 | 0.01 |
| H | 4-(3-Hydroxypropyl)phenol | 0.83 | 0.07 | 0.74 | 0.67 | 0.62 |
|  | 4-Propylphenol | 0.07 | 0.13 | 0.07 | 0.06 | 0.03 |
|  | 4-Ethylphenol | 0.02 | 0.01 | 0.12 | 0.01 | 0.01 |
|  | 4-Methylphenol | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| Others | 4-Propylcyclohexanol | 0.01 | 0.05 | 0.08 | 0.02 | 0.04 |
|  | 4-Ethylcyclohexanol | 0.04 | 0.02 | 0.03 | 0.05 | 0.04 |
|  | 4-Methylcyclohexanol | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
|  | Total | 3.01 | 3.78 | 4.43 | 4.52 | 2.52 |

a S: Syringl units; G: Guaiacyl units; H: p-Hydroxyphenyl units.

Table S6 Types and contents of hydroxyl groups in the RCF oil.

| 2-PrOH:H2O ratios (v/v) | S-OH (mmol/g) | G-OH (mmol/g) | H-OH (mmol/g) | Phenolic-OH (mmol/g) | Aliphatic-OH (mmol/g) | COOH (mmol/g) |
| --- | --- | --- | --- | --- | --- | --- |
| 1:9 | 0.413 | 0.111 | 0.467 | 1.991 | 21.580 | 4.203 |
| 3:7 | 0.070 | 1.104 | 0.007 | 1.181 | 28.601 | 3.871 |
| 5:5 | 0.420 | 1.192 | 0.458 | 2.070 | 29.860 | 4.268 |
| 7:3 | 0.229 | 0.845 | 0.279 | 1.353 | 31.724 | 4.827 |
| 9:1 | 0.081 | 1.018 | 0.222 | 1.321 | 13.752 | 4.806 |

Table S7 Crystallinity (CrI %) of the RCF pulps fractionated by different ratios of 2-PrOH:H2O.

| 2-PrOH:H2O (v/v) | CrI (%) |
| --- | --- |
| 1:9 | 51.42 |
| 3:7 | 51.38 |
| 5:5 | 53.60 |
| 7:3 | 66.50 |
| 9:1 | 63.72 |

Table S8 Ethanol fermentation performances by parent S. cerevisiae and the engineered S. cerevisiae using YPX as substrate (40 g/L xylose).

| Strain | M3013 | YL13 | YL23 | YL23-1 |
| --- | --- | --- | --- | --- |
| Residual xylose (g/L) | 38.25±0.18 | 8.77±1.01 | 5.91±1.74 | 0±0.00 |
| OD600max | 3.20±0.32 | 9.70±0.38 | 10.54±0.10 | 11.64±0.70 |
| Ethanol concentration (g/L) | 0±0.00 | 10.63±0.33 | 11.24±0.18 | 14.77±0.60 |
| Ethanol yield (g/g) | 0±0.00 | 0.277±0.009 | 0.292±0.005 | 0.371±0.003 |

Table S9 Ethanol fermentation performances by S. cerevisiae YL23-1 using enzymatic hydrolysates of the RCF pulps.

| 2-PrOH:H2O (v/v) | 1:9 | 3:7 | 5:5 | 7:3 | 9:1 |
| --- | --- | --- | --- | --- | --- |
| Ethanol concentration (g/L) | 18.19±1.02 | 24.63±1.05 | 25.49±1.02 | 21.61±0.62 | 14.38±0.90 |
| Ethanol yield (g/g) | 0.422±0.023 | 0.426±0.018 | 0.423±0.017 | 0.429±0.010 | 0.418±0.026 |

Table S10 Ethanol fermentation performances by S. cerevisiae YL23-1 using synthetic medium, enzymatic hydrolysates of the 5:5 of 2-PrOH:H2O (v/v) ratio group with and without nutrients (YP) addition.

| Medium | Synthetic medium | Enzymatic hydrolysate with nutrients addition | Enzymatic hydrolysate without nutrients addition |
| --- | --- | --- | --- |
| Ethanol concentration (g/L) | 26.38±0.48 | 26.12±0.88 | 25.49±1.02 |
| Ethanol yield (g/g) | 0.434±0.08 | 0.431±0.015 | 0.423±0.017 |

Table S11 Saccharomyces cerevisiae, plasmid, gRNA and primers used in this study.

| Strain | Relevant Genotype and Manipulation |  | Source |
| --- | --- | --- | --- |
| M3013 | Parent strain used for bioethanol fermentation. |  | Laboratory preservation |
| YL13 | M3013 derivative, XI-3:: PTEF2-XYL1, PTEF1-mXYL1, PPGK1p-XYL2, PHXT7p-XKS1, PHO13::gRNA, GRE3::gRNA, XII-2:: PTDH1p-RPE1, PPGK1p-TAL1, PTEF1p-RKI1, PTDH3p-TKL1 |  |  |
| YL23 | YL13 derivative, XI-5:: PPGK1-XUT4, PPGK1-XUT6 |  | This work |
| YL23-1 | YL23 derivative, single-colony isolate from adaptive laboratory evolution by xylose |  | This work |
| Plasmid | Relevant properties or genotype |  | Source |
| pRS03 | pSPGM1 carrying XUT4 and XUT6 |  | This work |
| pLacZ-XII-5 | ori, AmpR, 2μ, G418, pTEF1-iCas9-tADH1, pSNR52-(XII-5 gRNA)-gRNA scaffold-tSNR52 20bp Target Sequence: CTATAACCGGTTTGAATTTA, TTGTCACAGTGTCACATCAG |  | This work |
| Primer |  | Nucleotide sequence (5’ >3’) |  |
| P-XUT4-F |  | CGCGGATCCGCGTTCCATCtCATTCAACTTGTACTTAAAGAT |  |
| P-XUT4-R |  | TCCCCGCGGGGAATGTCTTCGTTATTGACTAACGAATACTT |  |
| XUT4-YAN-F |  | TGTGACAACAACAGCCTGTTCTCA |  |
| XUT4-YAN-R |  | TTGCTTTTATCTGGATCTGTGCTCA |  |
| P-XUT6-F |  | TCCCACTAGTGGGAATGTCCAGTGTTGAAAAAAGTGCT |  |
| P-XUT6-R |  | CGGGAGCTCCCGTTAGCTGATGTTTTCGACATGCTCT |  |
| XUT6-YAN-F |  | GTGCGGGCCTCTTCGCTA |  |
| XUT6-YAN-R |  | CCTGGTTAGGTGGATCCTGGT |  |
| Donor-XUT4-F |  | GATGAGTCACTGACAGCCACCGCAGAGGTTCTGACTCCTACTGAGCTCTATACGACTCACTATAGGGCGAATTGGGTACC |  |
| Donor-XUT6-R |  | CTGTCACTGAACTAAAACAATAAGGCTAGTTCGAATGATGAACTTGCTTGATCAAGCTTATCGATACCGTCGACCTCGAG |  |
| Goden-XII-5-F |  | AAAGGTCTCTGATCTTGTCACAGTGTCACATCAGGTTTTAGAGCTAGAAATAGCAAGTTAAAATAAGGC |  |
| Goden-XII-5-R |  | AAAGGTCTCTAAACTAAATTCAAACCGGTTATAGGATCATTTATCTTTCACTGCGGAGAAGT |  |
| Cas9-I-F |  | CGATTTTTGTGATGCTCGTCAGGG |  |
| Cas9-I-R |  | AAAAAGAAGAGAAAGGTCTGACTCGAG |  |

References

[1] K. Huang, M. Mohan, A. George, B.A. Simmons, Y. Xu, J.M. Gladden, Integration of acetic acid catalysis with one-pot protic ionic liquid configuration to achieve high-efficient biorefinery of poplar biomass, Green Chemistry. 2021; 23(16): 6036-6049. https://doi.org/10.1039/d1gc01727f.

[2] S.R. Haiyue Ni, G. Fang, Y. Ma, Determination of Alkali Lignin Solubility Parameters by Inverse Gas Chromatography and Hansen Solubility Parameters, BioResources. 2016; 11(2): 4353-4368.

[3] R. Rinken, D. Posthuma, R. Rinaldi, Lignin Stabilization and Carbohydrate Nature in H‐transfer Reductive Catalytic Fractionation: The Role of Solvent Fractionation of Lignin Oil in Structural Profiling**, ChemSusChem. 2022; 16(3). https://doi.org/10.1002/cssc.202201875.

[4] F. Cheng, T. Ouyang, J. Sun, T. Jiang, J. Luo, Using Solubility Parameter Analysis to Understand Delignification of Poplar and Rice Straw with Catalyzed Organosolv Fractionation Processes, BioResources. 2019; 14(1): 486-499.