# Supplementary Material

Synergistic Cell-Free Enzyme Cocktails for Enhanced Fiber Matrix Development: Improving Dewatering, Strength, and Decarbonization in the Paper Industry

Nelson Barrios1, María Gonzalez1, Richard Venditti1, Lokendra Pal1*

1Department of Forest Biomaterials, North Carolina State University, Raleigh, North Carolina, 27695.

*Corresponding author contact email: lpal@ncsu.edu

# Table S1: Fiber properties of bleached hardwood kraft pulp.

| Pre-treatment | Sample ID | Fiber length, Lw (mm) | Fines, Lw (%) | Tensile index (Nm/g) | Mean fiber width (µm) | Mean Curl Index (Lw) | Mean Kink Index (1/mm) | Freeness, CSF (ml) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| None | BHW | 0.99 ± 0.01 | 3.30 ± 0.23 | 24.15 ± 1.86 | 19.0 ± 0.1 | 0.078 ± 0.002 | 2.02 ± 0.02 | 577 ± 6 |

# Figure S1: Simplified flowsheet of the cell-free enzyme fiber modification methodology. Adapted from [1].

# Figure S2: Sensitivity analysis of primary variable cost contributors in the enhanced dewatering scenario.

# Table S2: Uncertainty of GWP reduction accounting for the experimental variability in solids after pressing.

| Parameter | Min:48% | Nominal:50% | Max:52% |
| --- | --- | --- | --- |
| GWP | 871 | 844 | 823 |
| Total GWP reduction | -10% | -12% | -15% |

Mean=12%+10%+12%3=12.3%

Half-range=∆(max-min)2= 15-103=2.5%

Uncertainty: (12.3% ± 2.5%)

# Table S3: Sensitivity analysis of cost savings variability based on fluctuations in natural gas prices, enzyme usage, and starch costs in the enhanced dewatering scenario.

| Parameter | -25% | 0 | 25% |
| --- | --- | --- | --- |
| Natural gas | -7.27 | -11.28 | -15.30 |
| Enzyme | -11.74 | -11.28 | -11.74 |
| Starch cost | -12.48 | -11.28 | -10.09 |

# Table S4: Effect of cell-free enzyme pretreatment on water retention value (WRV), hard-to-remove water (HW), freezing bound water (FBW), and non-freezing bound water (NFBW) content of the fibers.

| Enzyme dose (%) | Cationic starch dose (%) | Refining (PFI revs) | Water retention value (gwater/gdry fibers) |  | Hard-to-remove water (gwater/gdry fibers) |  | Freezing bound water (gwater/gdry fibers) |  | Non-freezing bound water (gwater/gdry fibers) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Avg. | Std. | Avg. | Std. | Avg. | Std. | Avg. | Std. |
| 0 | 0 | 0 | 1.98 | 0.08 | 1.48 | 0.10 | 0.33 | 0.05 | 0.31 | 0.07 |
| 0 | 0 | 1000 | 2.42 | 0.06 | 2.02 | 0.06 | 0.63 | 0.09 | 0.30 | 0.06 |
| 0.5 | 0 | 1000 | 2.21 | 0.09 | 1.91 | 0.16 | 0.58 | 0.11 | 0.29 | 0.04 |
| 0 | 0.5 | 1000 | 2.21 | 0.18 | 1.71 | 0.18 | 0.41 | 0.08 | 0.31 | 0.04 |
| 0.5 | 0.5 | 1000 | 1.89 | 0.09 | 1.49 | 0.09 | 0.38 | 0.04 | 0.30 | 0.06 |

# Table S5: Energy Variation for enhanced dewatering scenario of virgin integrated bleached hardwood fiber production.

| LP steam demand | GJ/h | Baseline (39%) | Enhanced dewatering (50%) |
| --- | --- | --- | --- |
| Bleaching plant | GJ/h | 203.931 | 203.931 |
| Seal pit PM | GJ/h | 33.310 | 33.310 |
| Evaporators | GJ/h | 192.478 | 192.478 |
| Concentrator | GJ/h | 101.624 | 101.624 |
| Mud washer | GJ/h | 1.959 | 1.959 |
| Slaker | GJ/h | 0.587 | 0.587 |
| ClO2 production | GJ/h | 1.505 | 1.505 |
| Digester | GJ/h | 19.711 | 19.711 |
| Air heater | GJ/h | 0.001 | 0.949 |
| Tota LP | GJ/h | 555.109 | 556.057 |
| MP steam demand |  |  |  |
| Dryer PM | GJ/h | 363.763 | 228.001 |
| Digester | GJ/h | 159.583 | 159.583 |
| CLO2 production | GJ/h | 0.348 | 0.348 |
| Air heater | GJ/h | 31.205 | 29.080 |
| Total MP | GJ/h | 554.898 | 417.012 |
| Steam for electricity | GJ/h | 194.400 | 194.400 |
| Steam loss | GJ/h | 166.501 | 145.960 |
| Condensate returned | GJ/h | 223.789 | 257.448 |
| Steam production |  |  |  |
| RB | GJ/h | 1075.127 | 1076.988 |
| BB | GJ/h | 123.145 | 123.145 |
| NG | GJ/h | 496.425 | 360.664 |
| Total steam produced | GJ/h | 1694.697 | 1560.797 |

# Table S6: Life Cycle Inventory for the baseline of virgin integrated bleached hardwood fiber production with 39% solids after press.

| LCI hardwood (baseline 39%) |  |  |
| --- | --- | --- |
| Input |  |  |
| Logs (50% moisture) | m3/ADt | 59.432 |
| Bleaching chemicals |  |  |
| Oxygen | kg/ ADt | 1.987 |
| H2O2 | kg/ ADt | 1.987 |
| H2SO4 | kg/ ADt | 3.647 |
| ClO2 (internal) | kg/ ADt | 24.651 |
| MgSO4 | kg/ ADt | 8.253 |
| NaOH | kg/ ADt | 9.818 |
| Chlorine Dioxide Production |  |  |
| Methanol | kg/ ADt | 8.692 |
| H2SO4 | kg/ ADt | 20.173 |
| Sodium chlorate | kg/ ADt | 88.752 |
| Make up chemicals |  |  |
| NaOH makeup | kg/ ADt | 23.433 |
| Na2SO4 makeup | kg/ADt | 14.369 |
| CaO (98%) | kg/ ADt | 18.073 |
| Fossil fuels |  |  |
| NG for limekiln | m3/ ADt | 37.088 |
| NG for Boiler | m3/ ADt | 230.108 |
| Water demand | m3/ ADt | 101.839 |
| Electricity from grid | kWh/ ADt | 71.776 |
| Output |  |  |
| Product | ADt / ADt | 1.000 |
| Waste |  |  |
| Dregs | kg/ ADt | 14.026 |
| grits | kg/ADt | 6.011 |
| sludge | kg/ ADt | 54.227 |
| Wastewater | kg/ ADt | 28.628 |
| Emissions |  |  |
| Biogenic RB | kg/ ADt | 2428.795 |
| Biogenic BB | kg/ADt | 230.165 |
| Biogenic Limekiln | kg/ ADt | 142.167 |
| Fossil Limekiln | kg/ ADt | 67.504 |
| Fossil NG boiler | kg/ ADt | 416.931 |
| H2S | kg/ADt | 0.169 |

# Table S7: Life Cycle Inventory for the enhanced dewatering scenario of virgin integrated bleached hardwood fiber production with 50% solids after press.

| LCI hardwood 50% |  |  |
| --- | --- | --- |
| Input |  |  |
| Logs (50% moisture) | m3/ADt | 59.432 |
| Bleaching chemicals |  |  |
| Oxygen | kg/ ADt | 1.987 |
| H2O2 | kg/ ADt | 1.987 |
| H2SO4 | kg/ ADt | 3.647 |
| ClO2 (internal) | kg/ ADt | 24.651 |
| MgSO4 | kg/ ADt | 8.253 |
| NaOH | kg/ ADt | 9.818 |
| Chlorine Dioxide Production |  | 20.173 |
| Methanol | kg/ ADt | 8.692 |
| H2SO4 | kg/ ADt | 20.173 |
| Sodium chlorate | kg/ ADt | 88.752 |
| Make up chemicals |  |  |
| NaOH makeup | kg/ ADt | 23.433 |
| Na2SO4 makeup | kg/ ADt | 14.369 |
| CaO (98%) | kg/ ADt | 18.073 |
| Papermaking chemicals |  |  |
| Starch | kg/ ADt | 4.77 |
| Enzymes | kg/ ADt | 4.77 |
| Fossil fuels |  |  |
| NG for limekiln | m3/ ADt | 37.088 |
| NG for Boiler | m3/ ADt | 159.031 |
| Water demand | m3/ ADt | 93.929 |
| Electricity from grid | kWh/ ADt | 207.903 |
| Output |  |  |
| Product | ADt/ADt | 1.000 |
| Waste |  |  |
| Dregs | kg/ ADt | 14.026 |
| Grits | kg/ADt | 6.011 |
| Sludge | kg/ ADt | 54.227 |
| Waste water | kg/ ADt | 29.164 |
| Emissions |  |  |
| Biogenic RC boiler | kg/ ADt | 2,301 |
| Biogenic BM boiler | kg/ADt | 218.058 |
| Biogenic Limekiln | kg/ ADt | 142.167 |
| Fossil Limekiln | kg/ ADt | 67.504 |
| Fossil NG boiler | kg/ ADt | 294.966 |
| H2S | kg/ADt | 0.160 |

# Table S8: Life cycle assessment of enhanced dewatering scenario for virgin integrated bleached hardwood fiber production.

| GWP (kg CO2-eq/ADt) |  |  |
| --- | --- | --- |
| Distribution | Baseline (39%) | Enhanced dewatering (50%) |
| Direct emissions Boiler | 417 | 305 |
| Direct emissions Limekiln | 68 | 68 |
| Electricity | 34 | 34 |
| Wood production | 93 | 93 |
| Transport | 86 | 86 |
| Chemicals | 86 | 111 |
| Waste | 60 | 60 |
| Fuels | 121 | 88 |
| GWP | 963 | 844 |
| Total GWP reduction | - | -12% |

# Table S9: Direct emissions breakdown of enhanced dewatering scenario for virgin integrated bleached hardwood fiber production.

| kg CO2-eq/ADt |  |  |  |
| --- | --- | --- | --- |
| Distribution | Baseline (39%) | Enhanced dewatering (50%) | Red. % |
| Share dryer | 290.44 | 177.68 | -37% |
| NG boiler | 394.59 | 294.97 | -27% |
| Total (lime kiln + boiler) | 484 | 373 | -23% |

# Table S10: Information available for cost estimation for enhanced dewatering scenario for virgin integrated bleached hardwood fiber production.

| Natural Gas cost1 ($/GJ) | 5.80 |
| --- | --- |
| Starch cost1 ($/kg) | 0.62 |
| Enzymes cost2 ($/Kg protein) | 4.25 |
| Enzyme concentration3 (kg/OD ton fiber) | 5.00 |
| Enzyme protein per fiber3 (kg/ADt) | 0.45 |
| Starch (Kg/OD ton fiber) | 5.00 |
| Pulp production (ODt/h) | 53.80 |
| Pulp production (ADt/h) | 56.50 |
| Pulp production (ADt/day) | 1356 |
| Pulp production (ADt/year) | 484,092 |

1Gas and starch price were obtained though Fisher Solve [2].

2Enzyme cost is based on Larnaudie et al. (2019, 2021) [3,4].

3Protein concentration is calculated based on protein content (90 mg/ml) and enzyme wt% used in this study.

# Breakdown of energy cost savings

Calculation of fuel savings

- Change in Natural Gas Consumption:

∆NGconsumed=(NGenhanced-NGbaseline)

- ∆NGconsumed: natural gas change in consumption

- NG baseline: (natural gas in baseline): 230.108 m³/ADt (from Table S4),

- NG enhanced (natural gas in enhanced dewatering scenario): 159.031 m³/ADt (from Table S4)

∆NGconsumed=∆159.031-230.108m3ADt=-71.077 m3ADt

This represents the reduction in natural gas consumption.

- Unit Conversion of NG Volume to Energy: To convert the volume of natural gas to energy, we use the following values:

- Natural gas high heating value (HHV): 55.58 GJ/mt, [5]

- NGdensity: 0.7 kg/ m3, [6]

The energy savings are calculated as:

NGcomsumed= ∆NGcomsumed x NGdensityx HHV x (1x10-3mtkg)

Substituting the values:

NGcomsumed=-71.077m3ADtx 0.7kgm3x 55.58 GJmtx (1x10-3mtkg)

NGcomsumed=-2.765 GJADt

This represents the energy savings per ADt.

- Cost savings: The cost of natural gas is 5.80 USD/GJ [2]. Therefore, the fuel cost savings are calculated as:

∆cost = NGcost × NGcomsumed

Substituting the values:

∆cost=5.80$GJ x (-2.765)GJADt= -16.05 $ADt

This represents a cost savings of 16.05 USD/ADt due to the reduced natural gas consumption in the enhanced dewatering scenario.

# Calculations of enzyme dose per protein content.

- Enzyme dose concentration: 0.5% wt per OD fiber

0.5%=0.5 kg100kg*100%

- Protein concentration in enzyme dose: 90 mgmL

- Fiber amount: 1 ton = 1000 kg

- Cost of enzyme: 4,24 $Kgprotein

- Production OD basis 53.80 OD/h

- Working day: 357

- Calculation of enzyme dose per ton of fiber

Enzyme dose (kg) = Fiber amount (kg)×Enzyme dose concentration (wt. fraction)

Enzyme dose (kg)=53,800 kg×0.005=269kg

- Conversion of protein concentration

Protein concentration in enzyme dose is:

90 mgmL = 90 gL = 0.09 kgL

Since 1 L of enzyme solution weighs approximately 1 kg (assuming mostly water-based), the protein concentration can also be expressed as:

0.09 kg protein per kg enzyme dose

- Calculation of protein used per ton of fiber

Protein (kg) = Enzyme dose (kg) × Protein concentration ( kgkg )

Protein (kg OD ton fiber ) = 269 kg × 0.0953.80 ODt = 0.45 kg

- Calculation of enzyme cost per OD fiber annually

Annual cost ($) = Annual protein usage (kg) x annual production x Cost per kg of protein ($Kgprotein)

0.45 kgOD fiber *53.80 OD t 56.49 ADt*4.25 $Kgprotein= 1.82$/ADt

# References

1. Barrios N, Smith MM, Venditti RA, Pal L. Enzyme-assisted dewatering and strength enhancement of cellulosic fibers for sustainable papermaking: A bench and pilot study. J Clean Prod. 2024;434.

2. Fisher International I. FisherSolve Database [Internet]. 2023. Available from: https://www.fisheri.com/fishersolve

3. Larnaudie V, Ferrari MD, Lareo C. Techno-economic analysis of a liquid hot water pretreated switchgrass biorefinery: Effect of solids loading and enzyme dosage on enzymatic hydrolysis. Biomass and Bioenergy. 2019;130.

4. Larnaudie V, Ferrari MD, Lareo C. Life cycle assessment of ethanol produced in a biorefinery from liquid hot water pretreated switchgrass. Renew Energy. 2021;176.

5. Ortega R, Forfora N, Urdaneta I, Azuaje I, Vivas KA, Vera RE, et al. Life cycle assessment of Brazilian bleached eucalyptus kraft pulp: Integrating bleaching processes and biogenic carbon impacts. Clean Environ Syst. 2024;15:100234.

6. Density of Gases Data [Internet]. [cited 2025 Mar 19]. Available from: https://www.engineeringtoolbox.com/gas-density-d_158.html