Additional File 1

## Gel point of SBP CNFs

Table 1: Calculated gel point and aspect ratios of SBP CNFs

| Sample | Øg (% w/w) | Aspect ratio |
| --- | --- | --- |
| SBP CNF | 0.18 ±0.008 | 142.0 ± 6.2 |
| SC-CNF | 0.13 ± 0.007 | 167.5 ± 9.2 |
| PAA CNF | 0.15 ± 0.007 | 153.8 ± 6.6 |
| HP.F CNF | 0.13 ± 0.005 | 163.1 ± 5.7 |

## AFM Characterisation of dilute SBP CNF suspensions

Table 2: Lengths and apparent widths of visible fibrils along with standard deviation as measured directly from AFM images, n = 20

| Sample | Length (nm) | Width (nm) | Height (nm) |
| --- | --- | --- | --- |
| SBPe CNF | 993 ± 260 | 11.8 ± 2.6 | 2.6 ± 0.8 |
| SC-CNF | 753 ± 501 | 24.7 ± 16 | 1.3 ± 1.4 |
| PAA-CNF | 1195 ± 824 | 25.4 ± 7.5 | 1.6 ± 1.6 |
| HP.F | 752± 458 | 10.2 ± 3.8 | 2.5 ± 0.9 |

## Statistics

Figure 1: Student T.Testing (unequal variance, 2 tailed, n = 3) of pulp brightnesses from Table 3

(note: SBP here is “SBPe”)

Figure 2: Student T.Testing (unequal variance, 2 tailed, n = 3) of acetyl bromide lignin assay from Table 4

Figure 3. Student T.Testing (unequal variance, 2 tailed, n = 4) of LM12 binding assay from Figure 2

Figure 4: Student T.Testing (unequal variance, 2 tailed, n = 3) of zeta potential measurements from Table 5

Figure 5: Student T.Testing (unequal variance, 2 tailed, n = 3) of pulp brightnesses from Table 7

Figure 6: Student T.Testing (unequal variance, 2 tailed, n = 4) of LM12 binding assay from Figure 6 C

## Broader AMSA analysis of bleached SBP CNFs

Figure 7: Surface-available polysaccharide composition of SBP CNFs as measured via AMSA. Binding is measured as a % of the max possible amount of binding. Antibodies and their epitopes are listed in Table 0.3

Table 3 : List of antibodies and their epitopes used in the AMSA analysis of SBP CNFs

| ANTIBODY | EPITOPE |
| --- | --- |
| LM18 | Homogalacturonanon |
| LM19 | Homogalacturonanon |
| LM5 | beta-1,4-galactan |
| LM6 | alpha-1,5-arabinan |
| INRA-RU1 | RG-I |
| INRA-RU2 | RG-I |
| BS-400-4 | (1→4)-β-mannan/galacto-(1→4)-β-mannan |
| LM21 | Heteromannan |
| LM22 | glucomannan |
| CCRC-M167 | Xylan-3 |
| CCRC-M170 | Xylan-4. |
| CCRC-M175 | (1,4)-β-D-xylosyl |
| CCRC-M145 | Xylan-3 |
| CCRC-M147 | Xylan-4. |
| LM11 | (1,4)-β-D-xylosyl |
| LM28 | glucuronosyl xylan |
| LM14 | Arabinogalactan |
| Jim8 | Arabinogalactan |
| Jim13 | Arabinogalactan |
| Mac207 | Arabinogalactan w. GlcA |
| LM15 | XXXG - xyloglucan |
| LM25 | XLLG, XXLG, XXXG* - xyloglucan |
| CBM3a | Celllulose |