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	Nanoparticles
	Size [nm] [a]
	PDI[b]
	Zeta-potential [mV][c]
	MTX loading content [wt%][d]
	Au thickness [nm]

	MTX-PLGA NPs
	105
	0.015
	-39.1± 1.34
	3.52 ± 0.13
	-

	MTX-loaded MNPs
	110
	0.021
	-23.5± 1.21
	3.02 ± 0.12
	15


[a,b,c]The size, polydispersiy index (PDI) and zeta-potential of the NPs were measured by dynamic light scattering (Zetasizer Nano ZS, Malvem Instruments Ltd) at a concentration of approximately 1 mg of NPs/1 ml of distilled water. [d]To determine the amount of encapsulated MTX, the dried NPs were redissolved in DMSO to extract MTX from the NPs. MTX in the supernatant was quantified by a UV spectrometer (Optizen 2120 UV, MECASYS Co.).
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