Additional file 1 Characterization of Prepared NPs

| Nanoparticles | Size [nm] [a] | PDI[b] | Zeta-potential [mV][c] | MTX loading content [wt%][d] | Au thickness [nm] |
| --- | --- | --- | --- | --- | --- |
| MTX-PLGA NPs | 105 | 0.015 | -39.1± 1.34 | 3.52 ± 0.13 | - |
| MTX-loaded MNPs | 110 | 0.021 | -23.5± 1.21 | 3.02 ± 0.12 | 15 |

[a,b,c]The size, polydispersiy index (PDI) and zeta-potential of the NPs were measured by dynamic light scattering (Zetasizer Nano ZS, Malvem Instruments Ltd) at a concentration of approximately 1 mg of NPs/1 ml of distilled water. [d]To determine the amount of encapsulated MTX, the dried NPs were redissolved in DMSO to extract MTX from the NPs. MTX in the supernatant was quantified by a UV spectrometer (Optizen 2120 UV, MECASYS Co.).