Supplementary Figure 1

A

B

C

Supplementary Figure 1. Immunohistochemical analyses (1A, 1B) and immunohistological (1C) of porcine lung TissueSpec® ECM hydrogel encapsulating ECs after 48-hour incubation with ICs (ATA-ICs, ACA-ICs and SLE-ICs).

1A: CD31 and Haematoxylin staining

1B: CD34 and Haematoxylin staining

1C: H&E staining

Images are representative of 3 independent experiments (n=3).

Upper: original magnification 20X. Scale bars correspond to 50 µm.

Lower: original magnification 40X. Scale bars correspond to 25 µm.

Supplementary Figure 2

Supplementary Figure 2. H&E staining of sections of TissueSpec® Skin ECM Scaffold after 48-hour stimulation of ECs with IC preparations (ATA-ICs, ACA-ICs and SLE-ICs).

Images are representative of 3 independent experiments (n=3).

Upper: original magnification 20X. Scale bars correspond to 50 µm.

Lower: original magnification 40X. Scale bars correspond to 25 µm.

Supplementary Figure 3

Supplementary Figure 3. GTR staining of sections of TissueSpec® Skin ECM Scaffold after 48-hour stimulation of ECs with IC preparations (ATA-ICs, ACA-ICs and SLE-ICs).

Images are representative of 3 independent experiments (n=3).

Upper: original magnification 20X. Scale bars correspond to 50 µm.

Lower: original magnification 40X. Scale bars correspond to 25 µm.

Supplementary Figure 4

A

B

Supplementary Figures 4. Immunofluorescence analysis of sections of TissueSpec® Skin ECM Scaffold after 48-hour stimulation of ECs with IC preparations (ATA-ICs, ACA-ICs and SLE-ICs).

Panel A: patient #2.

Panel B: patient #3.

Collagen IV (red) and αSMA (green) and DAPI (blue).

Images are representative of 3 independent experiments (n=3).

Images were acquired using confocal ZEISS LSM900.

Original magnification 10X, scale bars correspond to 100 µm.

Original magnification 40X, scale bars correspond to 25 µm.

Supplementary Figure 5

Supplementary Figure 5. Immunofluorescence analysis of sections of TissueSpec® Skin ECM Scaffold after 48-hour stimulation of ECs with IC preparations (ATA-ICs, ACA-ICs and SLE-ICs).

CD34 (green) and DAPI (blue).

Images are representative of 3 independent experiments (n=3).

Images were acquired using confocal confocal ZEISS LSM900.

Original magnification 10X, scale bars correspond to 100 µm.