Table S1. Young’s modulus of the scaffolds with different concentration of hydroxyapatite (HAp)

|  | HAp 25mg | HAp 50mg | HAp 75mg | HAp 100mg |
| --- | --- | --- | --- | --- |
| Stiffness(kPa) | 80.98±17.45 | 127.31±12.55 | 165.32±9.63 | 190.51±3.02 |