

Table S1. Young’s modulus of the scaffolds with different concentration of hydroxyapatite (HAp) 
		        
	HAp 25mg
	HAp 50mg
	HAp 75mg
	HAp 100mg

	Stiffness(kPa)
	80.98±17.45
	127.31±12.55
	165.32±9.63
	190.51±3.02



