Table S2. Histological scores for all groups with different treatments for osteochondral defect in rabbits 12 weeks post-surgery. 
	Histological Parameter
	Scores, Median (IQR)

	
	Blank
	HAC
	HAC+gel
	HAC+gel+M
	HAC+gel+M+E

	Overall defect evaluation
	
	
	
	
	

	1. Percent filling with newly formed tissue
	1 (0-1)
	1 (1-1.5)
	2 (1-2)
	2 (2-2)
	3 (2.5-3)

	2. Percent degradation of the implant
	NA
	1 (1-1.5)
	2 (1-2)
	2 (2-2)
	3 (2.5-3)

	Subchondral bone evaluation
	
	
	
	
	

	3. Percent filling with newly formed tissue
	1 (0-1)
	1 (1-1)
	1 (1-1.5)
	2 (1-2)
	2 (2-2)

	4. Subchondral bone morphology
	0 (0-1)
	1 (0.5-2)
	2 (1.5-2)
	3 (2-3)
	4 (3-4)

	5. Extent of new tissue bonding with adjacent bone
	1 (0.5-1)
	1 (0.5-2)
	1 (1-2)
	2 (1.5-2.5)
	3 (2-3)

	Cartilage evaluation
	
	
	
	
	

	6. Morphology of newly formed surface tissue
	1 (0-1)
	1 (0.5-2)
	2 (1.5-2.5)
	3 (2-3)
	4 (3-4)

	7. Thickness of newly formed cartilage
	0 (0-0.5)
	0 (0-1)
	1 (1-1)
	1 (1-2)
	2 (1.5-2.5)

	8. Joint surface regularity
	0 (0-1)
	1 (0.5-1.5)
	1 (1-1.5)
	2 (1.5-2)
	3 (2.5-3)

	9. Chondrocyte clustering
	0 (0-1)
	1 (0-1)
	1 (1-1.5)
	2 (1.5-2.5)
	2 (2-3)

	10. Chondrocyte and GAG content of neocartilage
	0 (0-0.5)
	0 (0-1)
	1 (1-1)
	2 (1.5-2)
	2 (2-3)

	11. Chondrocyte and GAG content of adjacent cartilage
	1 (0.5-1)
	1 (1-1.5)
	2 (1-2)
	2 (2-2.5)
	3 (2.5-3)


IQR, Inter Quartile Range; HAC, Hydroxyapatite and Collagen I; M, BMSCs; E, Electromagnetic Fields (EMF); GAG, Glycosaminoglycan; 

NA, not available.
