## Supplementary Materials

Human stem cells loaded with visible and near-infrared fluorescent core–shell polymeric nanoparticles and revealing tropism toward inflammatory stimuli: in vitro evaluation

Rana Zaki Abdul Bari 1,#, Iuliia Golovynska 1,#, Sergii Golovynskyi 1, Jiantao Liu 1, Yurii V. Stepanov 2, Siqi Gao 1, Hao Xu 1, Liudmyla I. Stepanova 3, Liudmyla O. Vretik 4, Tymish Y. Ohulchanskyy 1,*, Junle Qu 1,*

1 Center for Biomedical Optics and Photonics, College of Physics and Optoelectronic Engineering, Shenzhen University, Shenzhen, 518060, P.R. China

2 R.E. Kavetsky Institute of Experimental Pathology, Oncology and Radiobiology, NAS of Ukraine, Kyiv, 03022, Ukraine

3 Institute of Biology and Medicine, Taras Shevchenko National University of Kyiv, Kyiv 01601, Ukraine

4 Faculty of Chemistry, Taras Shevchenko National University of Kyiv, Kyiv, 01601, Ukraine

* Corresponding author e-mail: tyo@szu.edu.cn, jlqu@szu.edu.cn

# Equally contributed authors

Methods

Cell viability assay

The colorimetric SuperKine maximum sensitivity cell counting kit-8 (CCK-8) assay was employed to assess the viability of cells according to the manual. Initially, hESCs were transferred into a 96-well plate at a density of 5 × 103 cells per well for 24 h. After 24 h, the medium was removed and the cells were incubated for 24 h at 37°C in a medium containing NIR-NPs, Vis-NPs, NIR dye, or Vis dye. Then, the cells were washed, and 10 µL CCK-8 reagent per 100 µL (Abbkine, China) of a fresh medium was added to each well for 4 h. The absorbance of the formazan product at 450 nm was measured using a microplate reader (Rayato, Japan). The absorbance values were used to evaluate cell viability, with the results being normalized to the untreated control group.

Results

## Figure S1. Release of NIR/Vis dyes and NIR/Vis-NPs from stem cells. Comparative analysis of the release dynamics of (A) NIR dye and NIR-NPs from stem cells and (B) Vis dye and Vis-NPs from stem cells. (C) Representative microscopy images showing the migratory ability of hESCs toward the conditioned medium from normal BV-2 and LPS-treated BV-2.