Figure S1: Example of an ERM identifier as added to the registry Turtle.

erm:ERM00000099 a obo:CHEBI_59999 ;

rdfs:label "RiskGONE Literature NM 1" ;

dct:creator wd:Q61965386 ;

foaf:page

<https://h2020-riskgone.github.io/riskgone-materials/RiskGONE_Literature_NM.html> .

Table S1: Overview of nanoparticles (ENMs) in the NanoSafety RDF and how they are divided into the six groups shown in Figure 3 and 6. Names from the papers are abbreviated using CNTs for carbon nanotubes and NP for nanoparticles.

| carbon nanotubes (23) |  | silica particles (3) |  | other metal oxides II (22/31) |  |
| --- | --- | --- | --- | --- | --- |
| single-walled CNTs | 9 | crystalline silica particles | 1 | dysprosium oxide NP | 1 |
| multi-walled CNTs | 8 | silica oxide NP | 1 | erbium oxide NP | 1 |
| multi-walled CNTs aerosol | 1 | silica quartz particles DQ12 | 1 | europium oxide NP | 1 |
| multi-walled CNTs aminated | 1 |  |  | Fe2O3 NP | 1 |
| multi-walled CNTs carboxylated | 1 | silver containing ENMs (11) |  | Fe3O4 NP | 2 |
| multi-walled CNTs polyethyleneimine | 1 | polyvinylpyrrolidone-coated silver NP | 2 | gadolinium oxide NP | 2 |
| multi-walled CNTs pegylated | 1 | silver NM300K | 2 | gold NP | 1 |
| carbon nanotubes | 1 | silver cube NP | 1 | lanthanum oxide NP | 1 |
|  |  | silver NP | 2 | manganese oxide NP | 1 |
| other carbon based ENMs (7) |  | silver plate NP | 1 | neodymium oxide NP | 1 |
| graphene oxide | 3 | spherelike silver NP | 3 | samarium oxide NP | 1 |
| graphene | 2 |  |  | ytterbium oxide NP | 1 |
| fullerene-C60 | 1 | other metal oxides I (9/31) |  | yttrium oxide NP | 1 |
| printex 90 carbon black NP | 1 | cerium oxide NM212 | 1 | zinc oxide NP | 3 |
|  |  | cerium oxide NP | 4 | zinc oxide NP NM110 | 1 |
| titanium dioxide (9) |  | 27% zirconium oxide-doped cerium oxide NP | 1 | zinc oxide NP NM111 | 1 |
| titanium dioxide NP | 9 | 78% zirconium oxide-doped cerium oxide NP | 1 | cobalt oxide NP | 1 |
|  |  |  |  | copper NP | 2 |

Table S2: Overview of  the methods and instruments used to obtain each physicochemical property.

| Physicochemical property | Method | Instrument | Number of ENM |
| --- | --- | --- | --- |
| primary particle size | TEM | Hitachi H-7500 | 46 |
|  | TEM/EDS | Philips CM20 | 1 |
|  | TEM/AFM | JEOL 100CX | 8 |
|  | Method not specified |  | 3 |
| hydrodynamic diameter (medium water) | DLS | HT-DLS, Dynapro Plate Reader, Wyatt Technology | 36 |
|  | Photomicrograph | CytoViva | 3 |
|  | Method not specified |  | 24 |
| bundle diameter | TEM |  | 8 |
| diameter | TEM |  | 8 |
|  | TEM/EDS | Philips CM20 | 1 |
|  | TEM/AFM | JEOL 100CX | 4 |
|  | UV-Vis |  | 8 |
|  | Method not specified |  | 1 |
| shape | TEM |  | 40 |
|  | TEM, SEM |  | 1 |
|  | Method not specified |  | 44 |
| zeta potential |  | Malvern ZetaSizer Nano-ZS | 39 |
|  | ELS |  | 7 |
|  | Method not specified |  | 12 |
| specific surface area | BET |  | 14 |
|  | Method not specified |  | 2 |