AMB Express

The title:

Construction of cell-plastics as neo-plastics consisted of cell-layer provided green alga Chlamydomonas reinhardtii covered by two-dimensional polymer

The full names of the authors (do not include academic degrees)

Akihito Nakanishi*†1,2, Kohei Iritani* 3, Yuri Sakihama4, Nanami Ozawa2, Ayano Mochizuki2, Marina Watanabe2

(*Co-first author, †corresponding author)

The author's institutional affiliations where the work was conducted

1Graduate School of Bionics, Tokyo University of Technology, Hachioji, Japan

2School of Bioscience and Biotechnology, Tokyo University of Technology, Hachioji, Japan

3Department of Applied Chemistry, School of Engineering, Tokyo University of Technology, Hachioji, Japan

4Tokyo University of Technology, Hachioji, Japan

Address correspondence to:

A. Nakanishi

Graduate School of Bionics, Tokyo University of Technology,

School of Bioscience and Biotechnology, Tokyo University of Technology

1404-1 Katakuramachi

Hachioji, Tokyo, 192-0982, Japan

Phone: +81 42-637-2427

E-mail: nakanishiah@stf.teu.ac.jp

Supplemental data

Fig. S1

SEM images of surfaces of cell-plastics without intercellular filler. Magnifications were ×1,000.

Experimental Details for Synthesis of compounds

1. General

All solvents were distilled before use. All commercially available reagents were used as received. Fig. S2 shows synthetic scheme of monomer 1. Compound 4 was prepared according to previous reports (Hosseini et al. 2016). 1H (400 MHz) and 13C (100 MHz) NMR spectra were measured on a Bruker UltraShield Plus 400 spectrometer. When chloroform-d were used as a solvent, the spectra were referenced to residual solvent proton signals in the 1H-NMR spectra (7.26 ppm) and to the solvent carbon signals in the 13C-NMR spectra (77.0 ppm). Figs. S3 and S4 show 1H and 13C NMR spectra of compound 3 and monomer 1, respectively. Preparative HPLC separation was undertaken with a JAI LC-9204 recycling chromatographs using 600 mm  40 mm JAIGEL-1H-40 and 2H-40 (for JAI LC-9204) GPC columns with CHCl3 as the eluent.

2. Synthesis of monomer 1

Fig. S2 Synthesis of monomer 1.

Syntheses of Compounds

Compound 3

A solution of vanilline (2.50 g, 16.4 mmol) and 2 (1.16 g, 1.82 mmol) in DMF (30 mL) was heated under 100 °C in the presence of K2CO3 (2.24 g, 16.2 mmol) for 24 h. After cooling to room temperature, the mixture was added to water dropwise for reprecipitation. After the filtration, compound 3 (1.86 g, 96%) was given as a light yellow solid.

1H-NMR (400 MHz, CDCl3, 25 °C) 9.83 (s, 6H), 7.38 (d, J = 1.8 Hz, 6H), 7.34 (dd, J = 8.1 Hz and 1.8 Hz, 6H), 7.03 (d, J = 8.2 Hz, 6H), 5.36 (s, 12H), 3.80 (s, 18H); 13C-NMR (100 MHz, CDCl3, 25 °C)  190.7, 153.0, 150.2, 137.7, 131.0, 126.3, 112.9, 109.2, 65.0, 55.7.

Monomer 1

Compound 3 (249 mg, 0.234 mmol), 4 (752 mg, 2.76 mmol) were stirred in cyclohexane (2.5 mL). To the solution, pyridine (0.175 mL, 2.17 mmol) and aniline (0.250 mL, 2.74 mmol) were added. After string at 80 °C for 18 h, the mixture was added to water. The product was extracted by CH2Cl2. The organic phase was washed with water and brine, and dried over Na2SO4. After removal of the solvent under vacuum, the crude mixture was purified by preparative HPLC and reprecipitation (CH2Cl2/hexanes) to give 1 (268 mg, 49%) as an orange solid.

1H-NMR (400 MHz, CDCl3, 25 °C) 7.58 (d, J = 16 Hz, 6H), 7.09–6.80 (m, 18H), 6.29 (d, J = 16 Hz, 6H), 5.30 (brs, 12H), 4.26–4.06 (m, 12H), 3.71 (brs, 18H), 1.91–0.95 (m, 120H), 0.92–0.79 (m, 18H); 13C-NMR (100 MHz, CDCl3, 25 °C)  167.1, 150.1, 144.2, 137.9, 129.1, 122.1, 116.5, 114.6, 113.6, 110.1, 65.3, 64.7, 55.5, 31.9, 29.61, 29.58, 29.5, 29.32, 29.29, 28.7, 26.0, 22.7, 14.1.

3. 1H and 13C Spectra of Compounds

Fig. S3 1H and 13C NMR spectra of 3 in CDCl3 at 25 °C.

Fig. S4 1H and 13C NMR spectra of 1 in CDCl3 at 25 °C.

Reference

Hosseini R, Moosavi F, Rajaian H, Silva T, Magalhães e Sikva D, Soares P, Saso L, Edraki N, Miri R, Borges F, Firuzi O (2016) Discovery of neurotrophic agents based on hydroxycinnamic acid scaffold. Chem Biol Drug Des 88:926-937