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Figure S1 EDS spectrum of InGaN.


[image: 텍스트, 스크린샷, 그래프, 라인이(가) 표시된 사진

AI 생성 콘텐츠는 정확하지 않을 수 있습니다.]
Figure S2 EDS spectrum of PMN-PT.
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[bookmark: _Hlk207112652]Table S1 Summary of resonance frequency shifts under active layer and concentrations.
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Table S2 Summary of resonance frequency shifts with microparticle types.
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[bookmark: _GoBack]Table S3 Summary of resonance frequency shifts with dispersion media.
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Resonance Frequency

Material (MH2)
IPA 38.61

DI water 38.76

Glycerol 38.343
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Active layer Resonance Frequency | 0.5 1 2 4 8
v (MHz) mg/mL | mg/mL | mg/mL | mg/mL | mg/mL
PMN-PT 3968 3962 | 3959 | 39.56 | 3954 | 3937
InGaN 39.06 39.002 | 38.941 | 3876 | 3846 | 3811
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Resonance Frequency

Material (MH2)
TPU 38.76
PE 38.73
Chitin 38.512





