Additional file

Figure S1: Preparation of FIB lamella and lift-out procedure (a) cutting the thin lamella with ion beam (b) perpendicular view of the lamella showing uniform thickness (c) lift out (d) Omniprobe FIB holder (e) thin lamella attached to FIB holder (arrow) and (f) low resolution TEM  image of the lamella

(a)                                             (b)                                           (c)

(d)                                              (e)                                           (f)

# Fig. S2 (green sample)

# (a) SEM  image of the green tesserae showing glass matrix with  200-400 nm precipitates (opacifiers/pigments) (b) EDS  analysis on a matrix area (c)  EDS analysis on precipitate area

(b)                                                                          (c)

Table S1 EDS analysis on the matrix of green sample (Fig. S2 - b) kV:15.00, Tilt: 0.00, Take-off:35.22, Tc:35.0

Detector Type :SUTW-Sapphire, Resolution :130.83, Lsec :121

EDAX ZAF Quantification, Standardless,

Element Normalized

SEC Table : Default

Element, Wt %, At %, K-Ratio, Z, A, F

C K, 15.76, 27.08, 0.0296, 1.0657, 0.1761, 1.0003

O K, 31.28, 40.35, 0.1007, 1.0454, 0.3079, 1.0004

CuL, 3.27, 1.06, 0.0169, 0.8587, 0.6014, 1.0022

NaK, 7.07, 6.35, 0.0359, 0.9753, 0.5187, 1.0025

MgK, 0.66, 0.56, 0.0040, 0.9989, 0.6055, 1.0049

AlK, 1.35, 1.03, 0.0096, 0.9695, 0.7269, 1.0090

SiK, 27.02, 19.85, 0.2192, 0.9965, 0.8138, 1.0006

PbM, 7.09, 0.71, 0.0497, 0.6820, 1.0264, 1.0002

ClK, 0.79, 0.46, 0.0063, 0.9403, 0.8346, 1.0020

K K, 0.56, 0.29, 0.0048, 0.9431, 0.9133, 1.0051

SbL, 0.91, 0.15, 0.0068, 0.7459, 1.0041, 1.0002

CaK, 3.59, 1.85, 0.0325, 0.9636, 0.9371, 1.0005

FeK, 0.65, 0.24, 0.0057, 0.8714, 0.9937, 1.0073

Total, 100.000, 100.000

Table  S2   EDS  analysis on the  precipitate of green sample  (Fig. S2 - c)

Acquisition Time:10:49:47, Date:11-Mar-2016

kV:15.00, Tilt: 0.00, Take-off:35.22, Tc:35.0

Detector Type :SUTW-Sapphire, Resolution :130.83, Lsec :66

EDAX ZAF Quantification, Standardless,

Element Normalized

SEC Table : Default

Element, Wt %, At %, K-Ratio, Z, A, F

C K, 13.36, 28.48, 0.0297, 1.1207, 0.1986, 1.0002

O K, 24.07, 38.51, 0.0787, 1.0990, 0.2974, 1.0003

CuL, 3.14, 1.26, 0.0146, 0.9022, 0.5155, 1.0014

NaK, 6.03, 6.71, 0.0275, 1.0246, 0.4452, 1.0015

MgK, 0.77, 0.81, 0.0043, 1.0490, 0.5392, 1.0028

AlK, 1.19, 1.13, 0.0081, 1.0245, 0.6592, 1.0050

SiK, 17.55, 15.99, 0.1407, 1.0617, 0.7546, 1.0007

PbM, 21.66, 2.68, 0.1616, 0.7218, 1.0333, 1.0002

ClK, 0.73, 0.52, 0.0056, 0.9931, 0.7752, 1.0028

SbL, 7.56, 1.59, 0.0571, 0.7890, 0.9568, 1.0002

CaK, 2.80, 1.79, 0.0255, 1.0186, 0.8952, 1.0005

FeK, 1.16, 0.53, 0.0106, 0.9314, 0.9767, 1.0049

# Fig. S3 ( white sample)

# (a) SEM  image of the green tesserae showing glass matrix with  200-400 nm precipitates (opacifiers/pigments) (b) EDS  analysis on a matrix area (c)  EDS analysis on precipitate area

(b)                                                      (c)

Table  S3  EDS  analysis on the  matrix of white sample  (Fig. S3 - b)

| kV:15.00, Tilt: 0.00, Take-off:35.43, Tc:35.0 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Detector Type :SUTW-Sapphire, Resolution :130.83, Lsec :32 |  |  |  |  |
| EDAX ZAF Quantification, Standardless, |  |  |  |  |
| Element Normalized |  |  |  |  |
| SEC Table : Default |  |  |  |  |
| Element, Wt %, At %, K-Ratio, Z, A, F |  |  |  |  |
| C K, 13.06, 21.41, 0.0232, 1.0506, 0.1693, 1.0004 |  |  |  |  |
| O K, 36.21, 44.56, 0.1234, 1.0306, 0.3305, 1.0004 |  |  |  |  |
| NaK, 7.70, 6.60, 0.0410, 0.9617, 0.5511, 1.0032 |  |  |  |  |
| MgK, 0.71, 0.58, 0.0045, 0.9850, 0.6357, 1.0062 |  |  |  |  |
| AlK, 1.51, 1.10, 0.0110, 0.9542, 0.7555, 1.0115 |  |  |  |  |
| SiK, 31.35, 21.97, 0.2569, 0.9781, 0.8372, 1.0009 |  |  |  |  |
| S K, 0.22, 0.14, 0.0017, 0.9678, 0.8030, 1.0023 |  |  |  |  |
| ClK, 0.59, 0.33, 0.0048, 0.9256, 0.8635, 1.0035 |  |  |  |  |
| K K, 0.64, 0.32, 0.0056, 0.9284, 0.9378, 1.0088 |  |  |  |  |
| SbL, 2.35, 0.38, 0.0177, 0.7338, 1.0277, 1.0002 |  |  |  |  |
| CaK, 4.62, 2.27, 0.0420, 0.9482, 0.9583, 1.0003 |  |  |  |  |
| FeK, 0.62, 0.22, 0.0053, 0.8542, 0.9972, 1.0010 |  |  |  |  |
| CuK, 0.41, 0.13, 0.0034, 0.8188, 1.0017, 1.0000 |  |  |  |  |
| Total, 100.000, 100.000 Table S4 EDS analysis on the precipitate of white sample (Fig. 3S - c) kV:15.00, Tilt: 0.00, Take-off:35.43, Tc:35.0. Detector Type :SUTW-Sapphire, Resolution :130.83, Lsec :34. EDAX ZAF Quantification, Standardless,. Element Normalized. SEC Table : Default. Element, Wt %, At %, K-Ratio, Z, A, F. C K, 11.14, 21.69, 0.0250, 1.0932, 0.2049, 1.0003. O K, 29.37, 42.94, 0.1091, 1.0722, 0.3462, 1.0003. NaK, 6.33, 6.44, 0.0282, 1.0000, 0.4440, 1.0020. MgK, 0.59, 0.57, 0.0033, 1.0240, 0.5436, 1.0039. AlK, 1.40, 1.21, 0.0094, 0.9957, 0.6685, 1.0072. SiK, 21.84, 18.19, 0.1717, 1.0260, 0.7644, 1.0022. S K, 0.19, 0.14, 0.0015, 1.0114, 0.8055, 1.0064. ClK, 0.61, 0.40, 0.0052, 0.9659, 0.8649, 1.0108. K K, 0.68, 0.41, 0.0063, 0.9687, 0.9377, 1.0293. SbL, 20.23, 3.89, 0.1593, 0.7665, 1.0272, 1.0002. CaK, 5.96, 3.48, 0.0565, 0.9900, 0.9578, 1.0003. FeK, 0.75, 0.31, 0.0066, 0.8973, 0.9797, 1.0012. CuK, 0.92, 0.34, 0.0079, 0.8638, 0.9933, 1.0000. Total, 100.000, 100.000. |  |  |  |

Fig.  S4  Green  tesserae highlighting some of the crystals with various sizes   analyzed by means of  EPMA

Fig. S5  White tessereae highlighting some of the crystals with  various sizes  analyzed by means of  EPMA