Supplementary information

for article

Reflectance FT-IR spectroscopy as a viable option for textile fiber identification

Pilleriin Peets, Karl Kaupmees, Signe Vahur, Ivo Leito

University of Tartu, Institute of Chemistry, 14a Ravila str, 50411 Tartu, Estonia

Corresponding author: e-mail: pilleriin.peets@ut.ee

Table of contents

Example spectra of each fiber class recorded with FT-IR microspectrometer in reflectance mode	2

Case-study: Scarf from 20th century	13

Case-study: Very small fiber thread from painting on the textile from end of the 20th century	27

Spectra of each fiber class recorded with FT-IR microspectrometer in reflectance mode

All spectra below are original without any alteration or correction.

Figure S1. r-FT-IR spectrum of wool fiber

Figure S2. r-FT-IR spectrum of silk fiber

Figure S3. r-FT-IR spectrum of cotton fiber

Figure S4. r-FT-IR spectrum of linen fiber

Figure S5. r-FT-IR spectrum of jute fiber

Figure S6. r-FT-IR spectrum of sisal fiber

Figure S7. r-FT-IR spectrum of viscose fiber

Figure S8. r-FT-IR spectrum of cellulose acetate fiber

Figure S9. r-FT-IR spectrum of polyester fiber

Figure S10. r-FT-IR spectrum of polyamide fiber

Figure S11. r-FT-IR spectrum of polyacrylic fiber

Figure S12. r-FT-IR spectrum of polyethylene fiber

Figure S13. r-FT-IR spectrum of polypropylene fiber

Figure S14. r-FT-IR spectrum of polypropylene fiber

Figure S15. r-FT-IR spectrum of polypropylene fiber

Figure S16. r-FT-IR spectrum of polypropylene fiber

Figure S17. r-FT-IR spectrum of fiberglass

Figure S18. r-FT-IR spectrum of elastane fiber (deformed due to small fiber diameter)

Figure S19. r-FT-IR spectrum of Tencel

Figure S20. r-FT-IR spectrum of Tencel

Figure S21. r-FT-IR spectrum of Tencel

Figure S22. r-FT-IR spectrum of Tencel

Case-study: Scarf from 20th century

Figure S23. Photo of the analyzed scarf with the locations of the samples (Photo from the Conservation and Digitization Centre Kanut).

| Sample nr | Microscope picture of the sample | Microscope picture of fibers |
| --- | --- | --- |
| 1 |  |  |
|  | Figure S24. Sample 1 | Figure S25. Sample 1 |
| 2 |  |  |
|  | Figure S26. Sample 2 | Figure S27. Sample 2 |
| 3.1 |  |  |
|  | Figure S28. Sample 3.1 | Figure S29. Sample 3.1 |
| 3.2 |  |  |
|  | Figure S30. Sample 3.2 | Figure S31. Sample 3.2 |
| 4 |  |  |
|  | Figure S32. Sample 4 | Figure S33. Sample 4 |
| 5.1 |  |  |
|  | Figure S34. Sample 5.1 | Figure S35. Sample 5.1 |
| 5.2 |  |  |
|  | Figure S36. Sample 5.2 | Figure S37. Sample 5.2 |

Figure S38. Examples of r-FT-IR spectra of sample 1. Two spectra are presented to show the spectral differences within the sample.

Figure S39. Example of mATR-FT-IR spectrum of sample 1

Figure S40. Examples of r-FT-IR spectra of sample 2. Two spectra are presented to show the spectral differences within the sample.

Figure S41. Examples of mATR-FT-IR spectra of sample 2. Three spectra are presented to show the spectral differences within the sample

Figure S42. Examples of r-FT-IR spectra of sample 3.1. Two spectra are presented to show the spectral differences within the sample

Figure S43. Examples of mATR-FT-IR spectra of sample 3.1.

Figure S44. Example of r-FT-IR spectrum of sample 3.2

Figure S45. Examples of mATR-FT-IR spectra of sample 3.2

Figure S46. Examples of r-FT-IR spectra of sample 4. Two spectra are presented to show the spectral differences within the sample.

Figure S47. Examples of mATR-FT-IR spectra of sample 4. Two spectra are presented to show the spectral differences within the sample.

Figure S48. Example of r-FT-IR spectrum of sample 5.1

Figure S49. Examples of mATR-FT-IR spectra of sample 5.1

Figure S50. Example of r-FT-IR spectrum of sample 5.2

Figure S51. Examples of mATR-FT-IR spectra of sample 5.2

Table 1. Classification results with r-FT-IR. The smaller the PCA score is for DA the more accurate the result. The bigger the accuracy score (max 1.00) is for random forest the more accurate the result

| Sample nr | Measured spectra | Class (Discriminant analysis) | PCA scores | Class (Random forest) | Accuracy scores |
| --- | --- | --- | --- | --- | --- |
| 1 | Spec 1 | jute | 3.27 | wool | 0.24 |
|  | Spec 2 | jute | 3.62 | jute | 0.27 |
|  | Spec 3 | jute | 3.53 | jute | 0.30 |
|  | Spec 4 | jute | 3.63 | jute | 0.29 |
|  | Spec 5 | jute | 3.36 | jute | 0.35 |
|  | Spec 6 | jute | 3.37 | jute | 0.29 |
|  | Spec 7 | jute | 3.34 | jute | 0.30 |
|  | Spec 8 | jute | 3.19 | jute | 0.29 |
|  | Spec 9 | jute | 3.58 | jute | 0.30 |
|  | Spec 10 | jute | 3.55 | jute | 0.28 |
|  | Spec 11 | jute | 3.69 | jute | 0.28 |
|  | Spec 12 | jute | 3.34 | jute | 0.33 |
|  | Spec 13 | jute | 3.37 | jute | 0.33 |
|  | Spec 14 | jute | 4.05 | jute | 0.24 |
|  | Spec 15 | jute | 3.29 | jute | 0.28 |
|  | Spec 16 | jute | 2.13 | jute | 0.31 |
| 2 | Spec 1 | silk | 2.51 | jute | 0.59 |
|  | Spec 2 | silk | 1.61 | jute | 0.31 |
|  | Spec 3 | jute | 2.64 | silk | 0.89 |
|  | Spec 4 | wool | 2.54 | jute | 0.43 |
|  | Spec 5 | jute | 2.17 | jute | 0.35 |
|  | Spec 6 | silk | 2.57 | jute | 0.6 |
|  | Spec 7 | silk | 1.77 | jute | 0.29 |
|  | Spec 8 | jute | 2.65 | silk | 0.68 |
|  | Spec 9 | wool | 2.61 | jute | 0.4 |
|  | Spec 10 | cotton | 0.83 | jute | 0.34 |
| 3.1 | Spec 1 | jute | 1.16 | linen | 0.49 |
|  | Spec 2 | cotton | 1.1 | linen | 0.57 |
|  | Spec 3 | jute | 1.37 | cotton | 0.68 |
|  | Spec 4 | jute | 1.99 | linen | 0.67 |
|  | Spec 5 | jute | 1.77 | jute | 0.46 |
|  | Spec 6 | cotton | 0.77 | linen | 0.42 |
|  | Spec 7 | jute | 1.36 | cotton | 0.65 |
|  | Spec 8 | silk | 2.87 | linen | 0.66 |
| 3.2 | Spec 1 | silk | 1.55 | silk | 0.7 |
|  | Spec 2 | silk | 1.15 | silk | 0.95 |
|  | Spec 3 | silk | 1.58 | silk | 0.99 |
|  | Spec 4 | silk | 1.47 | silk | 0.99 |
|  | Spec 5 | silk | 1.37 | silk | 0.99 |
|  | Spec 6 | silk | 1.33 | silk | 0.93 |
|  | Spec 7 | silk | 0.92 | silk | 0.92 |
|  | Spec 8 | silk | 0.98 | silk | 0.99 |
|  | Spec 9 | silk | 1.67 | silk | 0.99 |
| 4 | Spec 1 | jute | 1.38 | jute | 0.37 |
|  | Spec 2 | jute | 1.42 | jute | 0.41 |
|  | Spec 3 | jute | 1.59 | wool | 0.37 |
|  | Spec 4 | jute | 1.35 | wool | 0.28 |
|  | Spec 5 | jute | 1.62 | wool | 0.41 |
|  | Spec 6 | jute | 1.92 | wool | 0.37 |
|  | Spec 7 | jute | 1.46 | wool | 0.29 |
|  | Spec 8 | jute | 1.78 | viscose | 0.31 |
|  | Spec 9 | jute | 1.92 | viscose | 0.26 |
|  | Spec 10 | jute | 1.35 | jute | 0.44 |
|  | Spec 11 | jute | 1.46 | viscose | 0.27 |
|  | Spec 12 | jute | 1.49 | wool | 0.27 |
| 5.1 | Spec 1 | cotton | 1.13 | cotton | 0.49 |
|  | Spec 2 | viscose | 1.08 | cotton | 0.42 |
|  | Spec 3 | viscose | 0.82 | viscose | 0.49 |
|  | Spec 4 | viscose | 1.29 | viscose | 0.61 |
|  | Spec 5 | viscose | 1.07 | linen | 0.34 |
|  | Spec 6 | viscose | 1.12 | cotton | 0.37 |
|  | Spec 7 | cotton | 0.83 | cotton | 0.55 |
|  | Spec 8 | cotton | 1.29 | cotton | 0.49 |
|  | Spec 9 | jute | 1.1 | cotton | 0.4 |
|  | Spec 10 | jute | 1.24 | cotton | 0.47 |
|  | Spec 11 | jute | 1.01 | cotton | 0.47 |
|  | Spec 12 | cotton | 1.06 | cotton | 0.54 |
|  | Spec 13 | cotton | 1.11 | cotton | 0.44 |
|  | Spec 14 | jute | 0.93 | cotton | 0.49 |
| 5.2 | Spec 1 | silk | 1.03 | silk | 0.97 |
|  | Spec 2 | silk | 1.69 | silk | 0.93 |
|  | Spec 3 | silk | 1.19 | silk | 0.96 |
|  | Spec 4 | silk | 1.03 | silk | 0.98 |
|  | Spec 5 | silk | 1.56 | silk | 0.97 |
|  | Spec 6 | silk | 1.42 | silk | 0.96 |
|  | Spec 7 | silk | 1.44 | silk | 0.96 |
|  | Spec 8 | silk | 1.45 | silk | 0.98 |
|  | Spec 9 | silk | 1.2 | silk | 0.95 |
|  | Spec 10 | silk | 1.29 | silk | 0.94 |

Table 2. Classification results with mATR-FT-IR. The smaller the PCA score is for DA the more accurate the result. The bigger the accuracy score (max 1.00) is for random forest the more accurate the result

| Sample nr | Measured spectra | Class (Discriminant analysis) | PCA scores | Class (Random forest) | Accuracy scores |
| --- | --- | --- | --- | --- | --- |
| 1 | Spec 1 | polyacrylic | 2.14 | silk | 0.29 |
|  | Spec 2 | polyacrylic | 1.88 | silk | 0.33 |
|  | Spec 3 | polyacrylic | 1.59 | silk | 0.49 |
|  | Spec 4 | polyacrylic | 1.87 | sisal | 0.27 |
|  | Spec 5 | polyacrylic | 2.21 | sisal | 0.25 |
|  | Spec 6 | polyacrylic | 2.17 | sisal | 0.28 |
|  | Spec 7 | polyacrylic | 2.17 | sisal | 0.27 |
|  | Spec 8 | polyacrylic | 1.68 | silk | 0.48 |
|  | Spec 9 | polyacrylic | 1.67 | silk | 0.52 |
|  | Spec 10 | polyacrylic | 2.05 | silk | 0.35 |
|  | Spec 12 | polyacrylic | 2.22 | sisal | 0.27 |
|  | Spec 13 | polyacrylic | 1.79 | silk | 0.54 |
|  | Spec 14 | polyacrylic | 1.82 | silk | 0.32 |
| 2 | Spec 1 | jute | 1.81 | sisal | 0.34 |
|  | Spec 2 | polyacrylic | 2.04 | sisal | 0.38 |
|  | Spec 3 | polyacrylic | 1.86 | sisal | 0.35 |
|  | Spec 4 | jute | 2.16 | sisal | 0.34 |
|  | Spec 5 | polyacrylic | 2.34 | viscose | 0.54 |
|  | Spec 6 | jute | 1.69 | sisal | 0.28 |
|  | Spec 7 | polyacrylic | 2.34 | sisal | 0.26 |
|  | Spec 8 | polyacrylic | 2.26 | sisal | 0.29 |
|  | Spec 9 | polyacrylic | 2.25 | sisal | 0.4 |
|  | Spec 10 | polyacrylic | 2.11 | sisal | 0.27 |
|  | Spec 11 | polyacrylic | 1.8 | sisal | 0.38 |
|  | Spec 12 | polyacrylic | 1.95 | sisal | 0.36 |
|  | Spec 13 | jute | 2.16 | viscose | 0.61 |
|  | Spec 14 | jute | 2.14 | viscose | 0.66 |
|  | Spec 15 | polyacrylic | 2.22 | silk | 0.42 |
|  | Spec 16 | polyacrylic | 2.29 | sisal | 0.24 |
|  | Spec 17 | polyacrylic | 2.27 | sisal | 0.33 |
|  | Spec 18 | jute | 1.86 | viscose | 0.54 |
|  | Spec 19 | jute | 1.69 | sisal | 0.36 |
|  | Spec 20 | jute | 1.61 | sisal | 0.39 |
| 3.1 | Spec 1 | jute | 0.99 | linen | 0.365 |
|  | Spec 2 | cotton | 1.01 | cotton | 0.34 |
|  | Spec 3 | jute | 1.45 | jute | 0.45 |
|  | Spec 4 | jute | 0.78 | jute | 0.49 |
|  | Spec 6 | jute | 1.05 | linen | 0.285 |
|  | Spec 7 | jute | 1.7 | jute | 0.29 |
| 3.2 | Spec 1 | silk | 1.14 | silk | 1 |
|  | Spec 2 | silk | 1.5 | silk | 1 |
|  | Spec 3 | silk | 1.66 | silk | 0.86 |
|  | Spec 4 | silk | 1.49 | silk | 0.99 |
|  | Spec 5 | silk | 1.82 | silk | 0.74 |
|  | Spec 6 | silk | 1.42 | silk | 0.99 |
| 4 | Spec 1 | jute | 1.35 | viscose | 0.63 |
|  | Spec 2 | jute | 1.54 | viscose | 0.55 |
|  | Spec 3 | jute | 1.49 | viscose | 0.57 |
|  | Spec 4 | jute | 1.72 | viscose | 0.6 |
|  | Spec 5 | jute | 1.96 | jute | 0.31 |
| 5.1 | Spec 1 | jute | 1.26 | viscose | 0.49 |
|  | Spec 2 | viscose | 1.25 | viscose | 0.92 |
|  | Spec 3 | jute | 1.12 | viscose | 0.78 |
|  | Spec 4 | jute | 1.1 | viscose | 0.63 |
|  | Spec 5 | jute | 0.9 | viscose | 0.64 |
|  | Spec 6 | jute | 1.55 | viscose | 0.51 |
| 5.2 | Spec 1 | silk | 1.08 | silk | 0.99 |
|  | Spec 2 | silk | 1.29 | silk | 0.97 |
|  | Spec 3 | silk | 1.41 | silk | 0.97 |

Case-study: Very small fiber thread from painting on the textile from the end of the 20th century

Figure S52. Photo of analyzed object. The red circle at the bottom of the painting shows where analyzed sample was taken (Photo made by Nele Ambos).

| Figure S53. Picture of the analyzed fiber on ATR diamond crystal. | Figure S54. Microscope picture of the fibers | Figure S55. Microscope picture of the fibers |
| --- | --- | --- |

Figure S56. FT-IR spectra of analyzed paint fiber. Spectra are recorded using FT-IR microspectrometer in ATR mode, ATR-FT-IR spectrometer and FT-IR microspectrometer in reflectance mode.

Table 3. Classification results with mATR-FT-IR. The smaller the PCA score is for DA the more accurate the result. The bigger the accuracy score (max 1.00) is for random forest the more accurate the result

| Measured spectra | Class (Discriminant analysis) | PCA scores | Class (Random forest) | Accuracy scores |
| --- | --- | --- | --- | --- |
| Spec 1 | silk | 2.34 | silk | 0.99 |
| Spec 2 | silk | 2.07 | silk | 0.95 |