Additional file for

Different low-cost materials to prevent the alteration induced by formic acid on unstable glasses

Rodrigo Arévalo1, Jadra Mosa2, Mario Aparicio2, Teresa Palomar2*

1 Dpto. Ciencias. Univ. Autónoma de Madrid. Campus de Cantoblanco. Avda. Tomás y Valiente, 7. 28049 Madrid, Spain

2 Instituto de Cerámica y Vidrio (ICV-CSIC), c/ Kelsen 5, Campus de Cantoblanco, 28049 Madrid, Spain

*Corresponding author, e-mail: t.palomar@csic.es

This document contains:

- Supp. Fig. 1

- Supp. Fig. 2

- Supp. Fig. 3

- Supp. Table 1

Supp. Fig. 1. Distribution inside each desiccator during the a) First test: selection of the best formic sink, b) Second test: Optimization of silica gel.

Supp. Fig. 2. SEM image of (a) the silica gel surface and (b) the deposits formed.

Supp. Fig. 3. SEM image of the steel (a) before the test and (b) after the test.

Supp. Table 1. Assignment of FTIR-ATR bands for silica gel.

| Compound | Wavenumber (cm-1) | Assignation | Reference |
| --- | --- | --- | --- |
| Water | 3300 | ν (OH) stretching | 34,35 |
|  | 2170 | δ (H-O-H) bend + libration | 37 |
|  | 1640 | δ (H-O-H) scissors bending | 35 |
| Formate | 2870 | ν (CH) stretching | 34,36 |
|  | 2713 | δ (CH) bending vibration | 36 |
|  | 1739 | ν (COO-) stretching asymmetric | 44 |
|  | 1580 | ν (COO-) of Na stretching asymmetric | 34,36,39 |
|  | 1370 | ρ (COO-) rocking | 34,39 |
|  | 1350 | ν (COO-) of Na stretching symmetric | 34,36,39 |
|  | 1064 | ρ (COO-) rocking | 34,41 |
|  | 750 | δ (COO-) bending | 35,36,39,41 |
| Carbonate | 1425 | ν (COO-) stretching asymmetric | 35,37,40 |
|  | 1370 | ρ (COO-) rocking | 34,39 |
|  | 1064 | ρ (COO-) rocking | 34,41 |
|  | 880 | ν (COO-) stretching symmetric | 35,37 |
|  | 750 | δ (COO-) bending | 35,36,39,41 |
| Bicarbonate | 1362 | ν (HCO3-) stretching asymmetric | 40 |
|  | 1010 | ν (C-OH) stretching | 37 |
| Silanol | 3300 | ν (OH) stretching | 42,43 |
|  | 962 | ν (Si-OH) stretching | 42,45 |
| Silica gel | 1073 | ν (Si-O-Si) stretching asymmetric | 42,43,45 |
|  | 789 | ν (Si-O-Si) stretching symmetric | 42,43 |
|  | 411 | ρ (Si-O-Si) rocking | 42 |