Additional File 2. Wear values of three types of commonly used attachments (Mean ± SEM)

| Time | Average wear depth (10-2 mm) |  |  |  | Wear volume (mm3) |  |  |  | Wear volume (%) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 3mm rectangular | Optimized rotating | Optimized root control | P value | 3mm rectangular | Optimized rotating | Optimized root control | P value | 3mm rectangular | Optimized rotating | Optimized root control | P value |
| T2 | 1.96 ± 0.36 | 1.69 ± 0.34 | 1.76 ± 0.63 | 0.914 | 0.283 ± 0.024 | 0.304 ± 0.070 | 0.214 ± 0.034 | 0.159 | 4.05 ± 0.36 | 5.79 ± 1.18 | 5.67 ± 0.79 | 0.323 |
| T3 | 2.90 ± 0.60 | 2.38 ± 0.30 | 2.00 ± 0.15 | 0.316 | 0.493 ± 0.031 | 0.466 ± 0.073 | 0.376 ± 0.041 | 0.031* | 6.97 ± 0.44 | 8.84 ± 1.18 | 10.12 ± 0.95 | 0.037* |
| T4 | 3.58 ± 0.89 | 2.87 ± 0.19 | 3.08 ± 0.52 | 0.708 | 0.669 ± 0.036 | 0.651 ± 0.102 | 0.548 ± 0.051 | 0.025* | 9.46 ± 0.49 | 12.13 ± 1.55 | 14.93 ± 1.26 | 0.001** |
| T5 | 4.08 ± 1,05 | 4.35 ± 0.29 | 3.83 ±0.98 | 0.910 | 0.916 ± 0.042 | 0.911 ± 0.107 | 0.723 ± 0.059 | 0.005** | 12.93 ± 0.58 | 17.25 ± 1.73 | 20.01 ± 1.68 | <0.001*** |

SEM: standard error of the mean.

*: P < 0.05; **: P < 0.01; ***: P < 0.01.