Supplementary information

Study on application of green sythesized ZnO and Si nanoparticles in enhancing aquaculture sediment quality

Yaoqiang Zhu1,2#, Weidong Li1,2#, Waqas Ahmed1,2, Mohsin Mahmood1,2, Hayssam M. Ali3, Muhammad Rizwan4, Jochen Bundschuh5, Muhammad Akmal6, Sajid Mehmood1,2*

1College of Ecology, Hainan University, Haikou City, 570100, P.R China

2 Center for Eco-Environment Restoration Engineering of Hainan Province, Hainan University, Haikou, 570228, China.

3Department of Botany and Microbiology, College of Science, King Saud University, 11451-Riyadh, Saudi Arabia

4Agricultural Research Station, Office of VP for Research & Graduate Studies, Qatar University, 2713 - Doha, Qatar

5Faculty of Health, Engineering and Sciences, University of Southern Queensland, Toowoomba, 4350 QLD, Australia

6Institute of Soil and Environmental Sciences, PMAS- Arid Agriculture University Rawalpindi 46300, Pakistan

#These authors contributed equally to this paper

*Corresponding author

Dr. Sajid Mehmood: E-mail: drsajid@hainanu.edu.cn

Section S1. Preparation of plant extract

Briefly, Azola Pinnata and horsetail plants, upon collection, underwent multiple washes with ultra-pure deionized water to eliminate dust particles. Subsequently, the plants were air-dried at room temperature (25 °C) for six days until a stable weight was achieved. The dried plants were finely powdered using a Worbush grinder (Dongguan Huatai Electric Appliances Co. Ltd., China) for a duration of four minutes. Following this, finely powdered plants material was subjected to heating in 100 mL of deionized water for 45 minutes at 55 °C. The heated leaves were then filtered and employed for the green synthesis of zinc oxide nanoparticles (GSZnONPs) and silica nanoparticles (GSSiNPs).

Figure S1. Fish pond sediments sites in San Jiang and Tan Niu in eastern Hainan Province, China.

Figure S2: Elemental mapping of Green synthesised silicon nanoparticles (GSSiNPs) and green synthesised zinc oxide nanoparticles (GSZnONPs).

Table S1. Basic attributes of green sythesised nanoparticles, Azzola pinnata (AP) and horsetail plant (HP).

| Item | Unit | GSZnONPs | GSSiNPS | AZ | HP |
| --- | --- | --- | --- | --- | --- |
| pH | —— | 8.550 | 8.910 | 5.400 | 6.420 |
| EC | mS/cm | 31.000 | 60.000 | 0.212 | 0.432 |
| C | Atomic % | 46.100 | 65.300 | 72.700 | 19.68 |
| N | Atomic % | 0.360 | 0.100 | 2.300 | 1.44 |
| O | Atomic % | 39.660 | 8.000 | 17.800 | 63.57 |
| Si | Atomic % | 0.130 | 26.100 | 0.200 | 15.22 |
| P | Atomic % | 0.670 | 0.500 | 1.000 | 0.09 |
| Cd | mg/kg | nd | nd | nd | nd |
| Cu | mg/kg | nd | nd | nd | nd |
| Hg | mg/kg | nd | nd | nd | nd |
| Zn | mg/kg | 41.210 | nd | nd | nd |
| Cr | mg/kg | nd | nd | nd | nd |
| BET Surface Area | m²/g | 18.9884 | 13.7071 | 0.1348 | 0.0066 |
| t-Plot External Surface Area | m²/g | 16.7158 | 13.7141 | -0.653 | -0.0933 |
| Single point surface area at P/Po | m²/g | 18.7299 | 13.2486 | 0.1287 | 0.0059 |

GSZnONPs (green synthesized zinc oxide nanoparticles); GSSiNPS (green synthesized silicon nanoparticles).

Table S2: The BCR sequential extraction procedure a (Rauret et al., 1999)

| Step No. | Fraction | Reagent | Experimental conditions |
| --- | --- | --- | --- |
| 1 | Acid soluble fraction (F1) | 20 mL of 0.11 mol L−1 acetic acid solution | Room temp.16 h, constant shaking |
| 2 | Reducible fraction (F2) | 20 mL of 0.5 mol L−1 hydroxyl amine hydrochloride solution at pH 1.5 (with nitric acid) | Room temp.16 h, constant shaking |
| 3 | Oxidizable fraction (F3) | 5 mL of 30%, w/v, H2O2 5 mL of 30%, w/v, H2O2 15 mL of 1mol L−1 ammonium acetate at pH 2 | Room temp. 1 h, occasional agitation + 85 ◦C, 1h 85 ◦C, 1 h, Reduce the volume to a few mL Room temperature, 16 h, constant shaking |
| 4 | Residual Fraction (F4) | Soil residues were digested with HCl: HNO3:HClO4 acids | Wet oxidation digestion (25 ml) |

a For 0.5-g sample. [1]

Table S3. Basic attributes of sediments from San Jiang (SJ) and Tan Niu (TN) before and after addition of green synthesized (GS) zinc oxide (ZnO) and silicon (Si) nanoparticles.

| Item |  | Unit | SJ | GSZnONPs | GSSiNPs | TN | GSZnONPs | GSSiNPs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H |  | % | 0.837 | 0.910 | 0.806 | 0.672 | 0.865 | 0.795 |
| pH |  | —— | 8.610 | 9.360 | 8.660 | 6.590 | 7.160 | 6.790 |
| OC |  | g/kg | 21.000 | 22.843 | 20.832 | 11.800 | 15.187 | 13.962 |
| TN |  | g/kg | 2.110 | 2.295 | 2.073 | 1.590 | 2.046 | 1.881 |
| Na |  | g/kg | 5.900 | 6.245 | 5.382 | 1.300 | 1.542 | 1.457 |
| Ca |  | g/kg | 11.400 | 12.150 | 11.650 | 1.600 | 1.937 | 1.818 |
| Mg |  | g/kg | 4.100 | 4.325 | 4.235 | 2.100 | 2.465 | 2.337 |
| A.Phosp |  | mg/kg | 48.800 | 50.941 | 49.411 | 200.000 | 227.497 | 217.935 |
| a.Sulpher |  | mg/kg | 180.000 | 191.487 | 184.308 | 149.000 | 179.386 | 168.625 |
| EC |  | mS/m | 121.000 | 126.792 | 125.826 | 13.390 | 15.760 | 15.921 |
| Exch. Potasium |  | mg/kg | 1.540 | 1.685 | 1.557 | 0.280 | 0.330 | 0.331 |
| Particle composition | 2.0~1.0mm | g/kg | 1.100 |  |  | 1.700 |  |  |
|  | 1.0~0.5mm | g/kg | 1.400 |  |  | 2.200 |  |  |
|  | 0.5~0.25mm | g/kg | 2.600 |  |  | 8.300 |  |  |
|  | 0.05~0.02mm | g/kg | 116.700 |  |  | 90.900 |  |  |
|  | 0.02~0.002mm | g/kg | 321.900 |  |  | 288.800 |  |  |
|  | <0.002mm | g/kg | 89.300 |  |  | 236.300 |  |  |
|  | 0.25~0.05mm | g/kg | 467.000 |  |  | 371.800 |  |  |
|  | 2.0~0.05mm | g/kg | 472.100 |  |  | 384.000 |  |  |
|  | 0.05~0.002mm | g/kg | 438.600 |  |  | 379.700 |  |  |
| Texture |  |  | Loam |  |  | Loam |  |  |
| Carbon |  | % | 2.340 | 2.545 | 2.362 | 1.320 | 1.699 | 1.562 |
| Cu |  | mg/kg | 9.000 | 7.382 | 8.282 | 18.000 | 14.027 | 15.243 |
| Zn |  | mg/kg | 40.000 | 29.703 | 36.490 | 28.000 | 21.257 | 23.302 |
| Cr |  | mg/kg | 53.000 | 37.384 | 48.349 | 38.000 | 28.849 | 31.624 |

Reference:

1.	Rauret, G. et al. (1999) Improvement of the BCR three step sequential extraction procedure prior to the certification of new sediment and soil reference materials. J. Environ. Monit. 1, 57–61