Electronic Supporting Information

Boosting Capacitive Performance of Manganese Oxide Nanorods by Decorating with Three-Dimensional Crushed Graphene

Akter Hossain Reaz1, Shimul Saha2, Chanchal Kumar Roy1, Md Abdul Wahab3, Geoffrey Will4, Mohammed A Amin5, Yusuke Yamauchi3,6, Shude Liu6*, Yusuf Valentino Kaneti3*, Md Shahriar Hossain7, and Shakhawat H. Firoz1*

1Department of Chemistry, Bangladesh University of Engineering and Technology, Dhaka 1000, Bangladesh.

2Department of Chemistry, Jashore University of Science and Technology, Jashore 7408, Bangladesh.

3Australian Institute for Bioengineering and Nanotechnology (AIBN), The University of Queensland, Brisbane, QLD 4072, Australia.

4School of Mechanical, Medical and Process Engineering, Faculty of Engineering, Queensland University of Technology, Brisbane City, 4000, QLD, Australia.

5 Department of Chemistry, College of Science, Taif University, P.O. Box 11099, Taif 21944, Saudi Arabia.

6JST-ERATO Yamauchi Materials Space-Tectonics Project and International Center for Materials Nanoarchitectonics (WPI-MANA), National Institute for Materials Science, Tsukuba, Ibaraki 305-0044, Japan.

7School of Mechanical and Mining Engineering, Faculty of Engineering, Architecture, and Information Technology (EAIT), The University of Queensland, Brisbane, QLD 4072, Australia.

Corresponding authors: lsdyy@yonsei.ac.kr (Shude Liu); v.kaneti@uq.edu.au (Yusuf Valentino Kaneti) shfiroz@chem.buet.ac.bd (Shakhawat H. Firoz)

Figure S1. TEM images of (a) MnOx/S-rGO and (b) MnOx/C-rGO and HRTEM images of (c) MnOx/S-rGO and (d) MnOx/C-rGO.

Figure S2. High-resolution O1s XPS spectra of (a) MnOx/S-rGO and (b) MnOx/C-rGO.

Figure S3. High resolution C 1s XPS spectra of (a) MnOx/S-rGO and (b) MnOx/C-rGO.

Figure S4. High resolution Mn 2p XPS spectra of (a) MnOx/S-rGO and (b) MnOx/C-rGO.

Figure S5. (a) CV curves at different scan rates and (b) GCD curves at different current densities of MnOx in 0.5 M Na2SO4 electrolyte in the potential range of −0.1 to 0.8 V.

Figure S6. Electrochemical study in 0.5 M Na2SO4 electrolyte with a three-electrode system: (a) CV curves at different scan rates and (b) GCD curves at different current densities of MnOx/S-rGO in the potential range of −0.1 to 0.8 V.

.

Figure S7. (a) CV curves at different scan rates and (b) GCD at different current densities of MnOx/C-rGO in 0.5 M Na2SO4 electrolyte in the potential range of −0.1 to 0.8 V.

Figure S8. Electrochemical study in 1 M Na2SO4 electrolyte with a two-electrode system. CV curves of the symmetric devices prepared with (a) MnOx/S-rGO and (b) MnOx/C-rGO at different scan rates. GCD curves of the symmetric devices prepared with (c) MnOx/S-rGO and (d) MnOx/C-rGO at different current densities in the voltage range of 0 to 1.5 V.

Cp

Figure S9. Equivalent fitting circuit

Table. S1 The obtained values of RS, Rct, Cdl, Zw, Cp, from EIS fitting.

| Symmetric supercapacitor device | Rs (Ohm) | Rct (Ohm) | Cdl (µF) | ZW | Cp (F) |
| --- | --- | --- | --- | --- | --- |
| MnOx/S-rGO-based device | 5.531 | 10.454 | 7.21 | 0.01605 | 0.03546 |
| MnOx/C-rGO-based device | 3.742 | 8.734 | 4.67 | 0.02194 | 0.03798 |