Supporting Information

Designing injectable dermal matrix hydrogel combined with silver nanoparticles for methicillin-resistant Staphylococcus aureus infected wounds healing

Sunfang Chen1#, Jun Yao1#, Shicheng Huo2#, Chennan Xu1, Ruting Yang1, Danhua Tao3, Bin Fang1, Gaoxiang Ma1, Zaihua Zhu4*, Ye Zhang1*, JingJing Guo5*

1 Department of Orthopedic Surgery, Spine Center, the Central Hospital Affiliated to Shaoxing University, Shaoxing, 321030, China

2 Department of Orthopedic Surgery, Spine Center, Changzheng Hospital, Navy Medical University, Shanghai, 200003, China

3 Department of Pathology, the Central Hospital Affiliated to Shaoxing University, Shaoxing, 321030, China

4 Division of Rheumatology and Immunology, Huashan Hospital, Fudan University, Shanghai, 200040, China.

5 Department of Pharmacy, the Central Hospital Affiliated to Shaoxing University, Shaoxing, 321030, China

#These authors contribute equally.

* Indicates the corresponding author

* Corresponding author: Zaihua Zhu, Ye Zhang, JingJing Guo

E-mail address: 9094116@qq.com(Z,Zh), 809144858@qq.com(Y,Zh), guojingjing-www@163.com(J,G)

- Supplementary Experimental Section

  - Hydrogel degradation in vitro

To assess the degradation of ADMH and Ag@ADMH at pH 5 and 7.4[1], 500μg of each hydrogel were allocated into separate centrifuge tubes. Periodic inspections were conducted to monitor for any fluid secretion or complete disintegration of the hydrogels. Post-degradation, the hydrogel components were extracted, and the residual weight was quantified to evaluate the extent of degradation.

  - AgNPs releasing performance of Ag@ADMH

To investigate the effect of pH on the release kinetics of silver nanoparticles (AgNPs) from Ag@ADMH, a 500 μg sample was distributed in centrifuge tubes, each containing 1 mL of PBS solution. The samples were then incubated at two different pH levels: 5 and 7.4, simulating the pH conditions of infection and normal physiological states [1], respectively, and maintained at 37°C to mimic body temperature. The release of silver nanoparticles into the PBS solution was monitored at various time intervals to evaluate how changes in pH influence the diffusion rate and release mechanisms of AgNPs from the hydrogel matrix. This approach provides a comprehensive understanding of the pH-dependent release kinetics of AgNPs, which is critical for optimizing therapeutic efficacy and safety in clinical applications.

- Supplementary Figure

S1: Degradation of ADMH and Ag@ADMH hydrogel（p > 0.05)；S2: Cumulative release of GA@AgNPs from Ag@ADMH（p < 0.0001).

References

1.	Fang, B., et al., Extracellular matrix scaffold crosslinked with vancomycin for multifunctional antibacterial bone infection therapy. Biomaterials, 2021. 268: p. 120603.