Additional information:

Amplification-Free Colorimetric Detection of Exosomal miRNA Using a CRISPR/Cas13a-Activated HRP/Au/MoS₂ Nanobiohybrid Catalyst

Myeong-Jun Lee1,‡, Minkyu Shin 2,‡, Joungpyo Lim1, Ha Rim Ahn3, Dain Jung1,

Shan Liu4, Chenzhong Li5, Jin-Ha Choi6,*, and Jeong-Woo Choi1,*

1Department of Chemical & Biomolecular Engineering, Sogang University, 35, Baekbeom-ro, Mapo-gu, Seoul, 04107, Republic of Korea

2Department of Chemical Engineering, Research Center of Chemical Technology, Hankyong National University, Gyeonggi–do, 17579, Republic of Korea

3Department of Surgery, Jeonbuk National University Medical School, Jeonju-si 54907, Republic of Korea

4Sichuan Provincial Key Laboratory for Human Disease Gene Study, Department of Medical Genetics, Sichuan Academy of Medical Sciences & Sichuan Provincial, People’s Hospital, University of Electronic Science and Technology of China, Chengdu, 610072, China

5Biomedical Engineering, School of Medicine, The Chinese University of Hong Kong, Shenzhen, 518172, China

6School of Chemical Engineering, Jeonbuk National University, 567, Baekje-daero, Deokjin-gu, Jeonju-si, Jeollabuk-do, 54896, Republic of Korea

‡These authors contributed equally to this work

*Corresponding authors: Jeong-Woo Choi (jwchoi@sogang.ac.kr) and Jin-Ha Choi (jhchoi@jbnu.ac.kr)

Fig. S1. TEM images of (A) MoS2 NP, (B) Au/MoS2 NP, and (C) EDS analysis of Au/MoS2 NP.

Fig. S2. XRD analysis of (A) MoS2 NP and (B) Au/MoS2 NP.

Fig. S3. Optimization of TMB reaction time for the MNB-ssRNA-HRP/Au/MoS₂ system integrated with CRISPR/Cas13a. Prolonged reaction beyond 30 min resulted in an increase in the background signal (I₀), leading to a decrease in the signal-to-background ratio (If/I₀). Experiments were performed at a miR-155 concentration of 10 pM (n = 3).

Fig. S4. Optimization of CRISPR/Cas13a trans-cleavage activity in the MNB-ssRNA-HRP/Au/MoS₂ system. Colorimetric responses were measured under different temperature conditions to evaluate the effect on Cas13a trans-cleavage activity. Experiments were performed at a miR-155 concentration of 10 pM (n = 3).

Fig. S5. Optimization of CRISPR/Cas13a trans-cleavage activity in the MNB-ssRNA-HRP/Au/MoS₂ system. Colorimetric responses were measured at different reaction times to evaluate their effect on Cas13a trans-cleavage activity. Experiments were performed at a miR-155 concentration of 1 pM (n = 3).

Fig. S6. Storage stability of the assembled MNB–ssRNA–HRP/Au/MoS₂ sensing complex at 4 °C. The colorimetric signal in the supernatant was monitored during storage for up to 13 days after magnetic separation. Only background-level signals were observed throughout the storage period, indicating negligible spontaneous release of HRP/Au/MoS₂. After 13 days, the stored complex was challenged with 100 pM miR-155 in the CRISPR/Cas13a assay, resulting in a strong colorimetric response and confirming retention of target-responsive sensing activity. (Base line = If/I0 on Day 0)

Fig. S7. Proof-of-concept extension of the HRP/Au/MoS2-based colorimetric sensing platform to DNA detection using CRISPR/Cas12a. (A) Schematic illustration of the Cas12a-based sensing system, in which target DNA activates CRISPR/Cas12a and induces collateral cleavage of the ssDNA linker, resulting in the release of HRP/Au/MoS₂ for colorimetric signal generation. (B) Colorimetric responses obtained with PBS, non-target miR-155, and target DNA at a nucleic acid concentration of 100 nM. Data are presented as the mean ± SD from three independent experiments (n = 3).

Fig. S8. Evaluation of matrix-derived peroxidase-like background and confirmation of CRISPR/Cas13a-dependent colorimetric signal generation in biological samples. (A) TMB/H₂O₂ colorimetric responses obtained from plasma, isolated exosomes, lysed exosomes, and lysed exosomes analyzed using the complete CRISPR/Cas13a-based sensing platform. Plasma exhibited intrinsic peroxidase-like activity, whereas this background signal was markedly reduced after exosome isolation and remained negligible after exosome lysis. A significant colorimetric response was observed only when the lysed exosome sample was analyzed using the complete sensing platform. (B) Corresponding analysis using cell culture medium, which showed negligible intrinsic peroxidase-like activity before and after exosome isolation and lysis, while a significant signal was generated after analysis with the complete CRISPR/Cas13a-based sensing platform. Data are presented as the mean ± standard deviation (SD) from three independent experiments (n = 3). Statistical significance was determined using one-way ANOVA followed by Tukey’s multiple-comparison test (**P < 0.01, ***P < 0.001; N.S., not significant).

Fig. S9. Correlation between RT-qPCR measurements and colorimetric signals for Exo-miR-155 detection in clinical samples (n = 12). Pearson correlation analysis showed a strong positive correlation between the two methods (r = 0.961, p < 0.001).

Table S1. Nucleic acid sequences used in this study

| Name | Sequence (5’ to 3’) |
| --- | --- |
| CRISPR/Cas13a system |  |
| crRNA | GAUUUAGACUACCCCAAAAACGAAGGGGACUAAAACAACCCC UAUCACGAUUAGCAUUAA |
| Target miRNA (miR-155) | UUAAUGCUAAUCGUGAUAGGGGUU |
| Mis-match | UUAAUGCUAAUCCUGAUAGGGGUU |
| ssRNA | [Thiol]-AAUGGCAAAUGGCA-[Biotin] |
| RT-qPCR primers |  |
| RT-primer | GCGAGCACAGAATTAATACGACTCACTATAGGTTTTTTTTTTTTT |
| Forward | CGTTAATGCTAATCGTGATAGGGGT |
| Reverse | GCGAGCACAGAATTAATACGAC |

Table S2. Kinetic parameters of HRP/Au/MoS2 and HRP. Km is the Michaelis constant, Vmax is the maximal reaction velocity.

| Catalyst | Km (mM) |  | Vmax (10−8 M s-1) |  | Reference |
| --- | --- | --- | --- | --- | --- |
|  | TMB | H2O2 | TMB | H2O2 |  |
| HRP | 0.619 | 2.91 | 0.915 | 0.190 | (Guo et al., 2018) |
| HRP/Au/MoS2 | 0.880 | 4.81 | 13.5 | 20.3 | This work |

Table S3. Intra-assay and inter-assay precision of the CRISPR/Cas13a-based colorimetric sensing platform at representative miR-155 concentrations.

|  |  | Intra-assay |  |  |  |  | Inter-assay |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spike sample |  | Conc. | Mean | SD | CV (%) |  | Conc. | Mean | SD | CV (%) |
| 100 fM | 1 | 81.37 | 91.91 fM | 12.42 | 13.51 | Batch1 | 89.63 | 110.68 | 24.06 | 21.74 |
|  | 2 | 105.6 |  |  |  | Batch2 | 136.9 |  |  |  |
|  | 3 | 88.75 |  |  |  | Batch3 | 105.5 |  |  |  |
| 10 pM | 1 | 14.78 | 12.92 pM | 2.236 | 17.31 | Batch1 | 13.24 | 10.58 | 2.593 | 24.5 |
|  | 2 | 13.55 |  |  |  | Batch2 | 8.06 |  |  |  |
|  | 3 | 10.44 |  |  |  | Batch3 | 10.45 |  |  |  |

Table S4. Nucleic acid sequences used for the proof-of-concept CRISPR/Cas12a-based DNA detection assay. The BRCA1-derived ssDNA sequence was used as the model target, and the ssDNA linker was modified with a thiol group at the 5′ end and biotin at the 3′ end for nanoparticle conjugation and magnetic-bead assembly.

| Name | Sequence (5’ to 3’) |
| --- | --- |
| CRISPR/Cas12a system |  |
| crRNA | UAA UUU CUA CUC UUG UAG AUG AUU UUC UUC CUU UUG UUC A |
| Target ssDNA (BRCA1) | TTA TGA ACA AAA GGA AGA AAA TCA |
| Linker ssDNA | Thiol-AAA AAA AAA ATA GCT TAT CAG AAA AAA AAA-Biotin |

Table S5. The pathological information of plasma sample.

| Sample | Age | Sex | Cancer | TNM stage | HER-2 |
| --- | --- | --- | --- | --- | --- |
| P1 | 60 | Female | Breast cancer | T1bN0 | NEG |
| P2 | 48 | Female | Breast cancer | T1cN0 | NEG |
| P3 | 53 | Female | Breast cancer | T1cN0 | NEG |
| P4 | 77 | Female | Breast cancer | T1cN0 | NEG |
| P5 | 52 | Female | Breast cancer | T2N1a | NEG |
| P6 | 51 | Female | Breast cancer | T2N2a | NEG |
| N1 | 37 | Female | Healthy donor |  |  |
| N2 | 58 | Female | Healthy donor |  |  |
| N3 | 49 | Female | Healthy donor |  |  |
| N4 | 38 | Female | Healthy donor |  |  |
| N5 | 36 | Female | Healthy donor |  |  |
| N6 | 45 | Female | Healthy donor |  |  |

[Reference]

Guo, J. J.; Wang, Y.; Zhao, M. 3D flower-like ferrous(II) phosphate nanostructures as peroxidase mimetics for sensitive colorimetric detection of hydrogen peroxide and glucose at nanomolar level. Talanta 182, 230-240 (2018). https://doi.org/10.1016/j.talanta.2018.01.080