Additional information for

Cross-linked enzyme-polymer conjugates with excellent stability and detergent-enhanced activity for efficient organophosphate degradation

Huan Cheng,a Yu-Lian Zhao,a Xiao-Jing Luo,a Dian-Sheng Xu,a Xun Cao,b Jian-He Xu,a Qing Dai,c Xiao-Yan Zhang,*a Jun Ge*b and Yun-Peng Bai*a

a.State Key Laboratory of Bioreactor Engineering, East China University of Science and Technology, Shanghai, 200237.

b.Department of Chemical Engineering, Tsinghua University, Beijing, 100084.

c.Division of Nanophotonics, CAS Center for Excellence in Nanoscience, National Center for Nanoscience and Technology, Beijing, 100190.

Emails:

cheng_huan@wuxiapptec.com (H. Cheng), yulianzhao1@163.com (Y.-L. Zhao), lxjecust@126.com (X.-J. Luo), xuds@ecust.edu.cn (D.-S. Xu), cx0118@hotmail.com (X. Cao), jianhexu@ecust.edu.cn (J.-H. Xu), daiq@nanoctr.cn (Q. Dai)

*Corresponding authors:

xyzhang@ecust.edu.cn (X.-Y. Zhang),

junge@mail.tsinghua.edu.cn (J. Ge)

ybai@ecust.edu.cn (Y.-P. Bai)

Experimental

- Preparation of CLEPCs by adding Pluronic F127 in different order

PL-AS-GL. Lyophilized enzyme powders were dissolved in Tris-HCl buffer (pH 7.0) to a final concentration of 20 mg/mL, to which Pluronic F127 was slowly added to a final concentration of 80 mg/mL. The solution was then stirred at 4 ºC for 30 min. Subsequently, ammonium sulfate was slowly added into the solution to a final concentration of 0.5 g/mL to precipitate enzymes, and the suspension was continuously stirred at 4 ºC for 30 min. Glutaraldehyde was added to a final concentration of 40 mM to cross-link the aggregates and the suspension was stirred at 4 ºC for 3 h. Then, the suspension was centrifuged at 12,000 rpm for 3 min, and the precipitate was washed three times and re-suspended in 0.5 mL Tris-HCl buffer (pH 7.0).

AS-GL-PL. Lyophilized enzyme powders were dissolved in Tris-HCl buffer (pH 7.0) to a final concentration of 20 mg/mL, to which ammonium sulfate was slowly added to a final concentration of 0.5 g/mL to precipitate enzymes. The suspension was then stirred at 4 ºC for 30 min. Subsequently, glutaraldehyde was added to a final concentration of 40 mM to cross-link the aggregates and the suspension was stirred at 4 ºC for 3 h. Then, Pluronic F127 was added to a final concentration of 80 mg/mL and the suspension was continuously stirred at 4 ºC for 30 min. Then, the suspension was centrifuged at 12,000 rpm for 3 min, and the precipitate was washed three times and re-suspended in 0.5 mL Tris-HCl buffer (pH 7.0).

2. Transmission electron microscopy (TEM) assay

Samples were prepared by dispersing the CLEPC in deionized water and then a well-dispersed droplet of the sample was placed on a copper grid. Samples were then dried and analysed on a H-7650B transmission electron microscope (Tokyo, Japan).

Figure S1. The hydrophobic surface of PoOPHM9 dimer is illustrated by Phenylalanine (blue) and other hydrophobic residues (green).

Figure S2. PoOPHM9 CLEA was incubated in the absence or presence of 0.1% (w/w) COD, APG or SDS, and its residual activity at different time points was measured.

Figure S3. (a) Pluronic F127 of different concentrations were associated with the free enzyme PoOPHM9. The prepared catalyst PoOPHM9-PF127 were incubated at room temperature and their residual activities relative to that of the free enzyme were measured at different time points. (b) PoOPHM9-PF127 was incubated with 0.1% (w/w) different detergents and its residual activity at different time points was measured and compared to that of the free enzyme.

References

- X. J. Luo, J. Zhao, C. X. Li, Y. P. Bai, M. T. Reetz, H. L. Yu and J. H. Xu, Biotechnol. Bioeng., 2016, 113, 2350-2357.