Additional file 1

Table S1. The poly dispersity index (PDI) and Zeta average size (Zavg) for rGO/AgNC in different solvents

| Solvent | PDI (d.nm) | Zavg (nm) |
| --- | --- | --- |
| Water | 0.421 | 324 |
| Methanol | 0.8 | 850 |
| Ethanol | 0.7 | 471 |
| DMF | 0.5 | 397 |
| n-butyl alcohol | 0.5 | 336 |
| Acetone | 0.8 | 1643 |
| Toluene | 0.9 | 1177 |
| Hexane | 0.6 | 632 |