Additional file for

Large-scale expansion of human umbilical cord derived-mesenchymal stem cells using PLGA@PLL nanofiber scaffold

Yujie Liu1, 2, Obed Boadi Amissah1, 3, Xiaoying Huangfang4, Ling Wang5, Habimana Jean de Dieu1, 3, Linshuang Lv1, 3, Xuanyan Ding1, 3, Junyi Li1, 3, Ming Chen5, Jinmin Zhu6, Omar Mukama1, Yirong Sun1, Zhiyuan Li1, 3, 5-8, * and Rongqi Huang1, 7, *

Fig. S1 Porosity of PLGA@PLL scaffold. Distributions of the size of 100 pores in SEM images of the 3D scaffold.

Fig. S2 Degradation profile of the PLGA@PLL scaffold. The changes in dry weight of (A) PLGA and (B) PLGA@PLL scaffolds incubated in the culture medium over a period of 4 weeks. The dry weights of the scaffolds were presented as the mean ± SEM (n=5). (C) The changes in pH value of the culture medium incubated with PLGA@PLL scaffolds over a period of 4 weeks were measured and presented as the mean ± SEM (n=5). ns indicated not significant (p > 0.05, one-way ANOVA tests).

Fig. S3 hUC-MSCs isolated from the human umbilical cord were cultured on a 10 cm dish and observed under a microscope.

Fig. S4 Pictures of newly-prepared PLGA scaffolds (A) before and (B) after PLL modification were captured using a Nikon camera.

Fig. S5 SEM images of hUC-MSCs seeded on the (A) PLGA scaffold and (B) PLGA@PLL scaffold.

Table S1. Primers used in this study

| Primer | Sequence (5' to 3') |
| --- | --- |
| Ki67 Ki67-F Ki67-R | GAAAGAGTGGCAACCTGCCTTC GCACCAAGTTTTACTACATCTGCC |
| PCNA PCNA-F PCNA-R | CAAGTAATGTCGATAAAGAGGAGG GTGTCACCGTTGAAGAGAGTGG |
| ICAM-1 ICAM-1-F ICAM-1-R | AGCGGCTGACGTGTGCAGTAAT TCTGAGACCTCTGGCTTCGTCA |
| VCAM-1 VCAM-1-F VCAM-1-R | GATTCTGTGCCCACAGTAAGGC TGGTCACAGAGCCACCTTCTTG |
| P21 P21-F P21-R | AGGTGGACCTGGAGACTCTCAG TCCTCTTGGAGAAGATCAGCCG |
| P16 P16-F P16-R | CTCGTGCTGATGCTACTGAGGA GGTCGGCGCAGTTGGGCTCC |