Table 1: Results of log k vs log k analysis for selected HIC resins. Hydrophobicity is the slope of the line resulting from log k vs log k plot when plotted against TOYOPEARL Phenyl.
	Resin
	Hydrophobicity 
	R2
	ζ-potential pH 5 (mV)
	ζ-potential pH 6 (mV)
	ζ-potential pH 7 (mV)

	TOYOPEARL Phenyl
	1
	1
	-0.12
	-1.02
	-3.80

	TOYOPEARL Butyl
	0.89
	0.92
	-2.66
	-5.75
	-7.01

	POROS Benzyl
	0.78
	0.92
	-12.98
	-12.99
	-14.51

	CaptoPhenyl Impres
	0.69
	0.96
	-14.31
	-14.88
	-15.25

	CaptoButyl
	0.47
	0.92
	-6.75
	-5.78
	-7.27

	CaptoButyl Impres
	0.48
	0.91
	-3.50
	-5.51
	-7.88

	TOYOPEARL PPG
	0.45
	0.87
	-1.53
	-3.99
	-7.21

	Butyl S FF
	0.38
	0.82
	-0.78
	-1.58
	-1.04

	Phenyl FF (LS)
	0.32
	0.89
	-1.43
	-1.49
	-3.06

	POROS Ethyl
	0.27
	0.91
	-13.34
	-16.61
	-22.38

	CaptoOctyl
	0.20
	0.84
	-6.72
	-6.83
	-7.85

	Phenyl FF (HS)
	N/A
	N/A
	-9.72
	-8.56
	-8.54

	POROS Benzyl Ultra
	N/A
	N/A
	1.66
	-1.03
	-3.87

	
	
	
	
	
	


a Polystyrene Divinyl Benzene
b Polypropylene Glycol

