Complementary material

Crystallographic charts for XRD

PDF#87-1165: QM=Calculated; d=Calculated; I=(Unknown)

Hematite

Fe2O3

Radiation=CuKa1	Lambda=1.5406	Filter=

Calibration=	2T=24.149-88.557	I/Ic(RIR)=3.26

Ref: Level-1 PDF

Hexagonal,  R-3c(167)	Z=6	mp=

CELL: 5.0353 x 5.0353 x 13.7495 <90.0 x 90.0 x 120.0>	P.S=

Density(c)=5.269	Density(m)=	Mwt=	Vol=301.9

Ref: Ibid.

Strong Lines: 2.70/X  2.52/7  1.69/4  1.84/3  3.68/3  1.49/3  1.45/3  2.21/2

2-Theta    d(Å)   I(f)  ( h k l)    Theta  1/(2d)   2pi/d  n^2

24.149  3.6824   31.4  ( 0 1 2)   12.074  0.1358  1.7063

33.158  2.6995  100.0  ( 1 0 4)   16.579  0.1852  2.3275

35.631  2.5176   71.3  ( 1 1 0)   17.815  0.1986  2.4957

39.283  2.2916    1.9  ( 0 0 6)   19.642  0.2182  2.7419

40.862  2.2066   19.2  ( 1 1 3)   20.431  0.2266  2.8474

43.508  2.0783    1.8  ( 2 0 2)   21.754  0.2406  3.0232

49.462  1.8412   34.2  ( 0 2 4)   24.731  0.2716  3.4126

54.069  1.6947   41.1  ( 1 1 6)   27.034  0.2950  3.7076

56.159  1.6365    0.5  ( 2 1 1)   28.079  0.3055  3.8395

57.448  1.6028    2.5  ( 1 2 2)   28.724  0.3120  3.9202

57.597  1.5990    8.6  ( 0 1 8)   28.799  0.3127  3.9295

62.436  1.4862   26.4  ( 2 1 4)   31.218  0.3364  4.2277

64.000  1.4536   25.7  ( 3 0 0)   32.000  0.3440  4.3226

66.031  1.4137    0.2  ( 1 2 5)   33.015  0.3537  4.4445

69.595  1.3498    2.5  ( 2 0 8)   34.798  0.3704  4.6550

71.947  1.3113    8.8  ( 1 0 10)  35.974  0.3813  4.7915

72.281  1.3061    2.1  ( 1 1 9)   36.141  0.3828  4.8108

75.191  1.2626    0.3  ( 2 1 7)   37.596  0.3960  4.9765

75.455  1.2588    5.5  ( 2 2 0)   37.727  0.3972  4.9913

77.738  1.2275    1.9  ( 0 3 6)   38.869  0.4073  5.1189

78.776  1.2139    0.9  ( 2 2 3)   39.388  0.4119  5.1762

79.486  1.2048    0.1  ( 1 3 1)   39.743  0.4150  5.2152

80.582  1.1911    1.6  ( 3 1 2)   40.291  0.4198  5.2749

80.709  1.1896    3.5  ( 1 2 8)   40.355  0.4203  5.2818

82.953  1.1630    4.3  ( 0 2 10)  41.477  0.4299  5.4025

84.485  1.1458    0.2  ( 0 0 12)  42.242  0.4364  5.4837

84.934  1.1409    6.5  ( 1 3 4)   42.467  0.4383  5.5073

88.557  1.1033    5.9  ( 2 2 6)   44.279  0.4532  5.6948

PDF#50-2241: QM=Uncommon(?); d=Diffractometer; I=(Unknown)

Cellulose

(C6H10O5)n

Radiation=CuKa1	Lambda=1.5406	Filter=

Calibration=	2T=14.988-22.781	I/Ic(RIR)=

Ref: Level-1 PDF               Z=	mp=           P.S=

Density(c)=	Density(m)=	Mwt=	Vol=

Ref: Ibid.

Strong Lines: 3.90/X  5.37/3  5.91/3

2-Theta    d(Å)   I(f)  ( h k l)   Theta  1/(2d)   2pi/d  n^2

14.988  5.9061   33.0             7.494  0.0847  1.0638

16.487  5.3724   33.0             8.243  0.0931  1.1695

22.781  3.9002  100.0            11.391  0.1282  1.6110

Statistics of kinetic experiments

SN-PMC

| Effect | Degr. Of Freedom | Time SS | Time MS | Time F | Time p | Qt (mg/SN-PMC) SS | Qt (mg/SN-PMC) MS | Qt (mg/SN-PMC) F | Qt (mg/SN-PMC) p |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Intercept | 1 | 837901.8 | 837901.8 | 15.91751 | 0.001542 | 2.378064 | 2.378064 | 38.98010 | 0.000030 |
| Error | 13 | 684323.2 | 52640.2 |  |  | 0.793093 | 0.061007 |  |  |
| Total | 13 | 684323.2 |  |  |  | 0.793093 |  |  |  |

| Effect | Degr. Of Freedom | Time SS | Time MS | Time F | Time p | Qt (mg/PMC) SS | Qt (mg/PMC) MS | Qt (mg/PMC) F | Qt (mg/PMC) p |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Intercept | 1 | 837901.8 | 837901.8 | 15.91751 | 0.001542 | 1.701586 | 1.701586 | 53.84128 | 0.000006 |
| Error | 13 | 684323.2 | 52640.2 |  |  | 0.410849 | 0.031604 |  |  |
| Total | 13 | 684323.2 |  |  |  | 0.410849 |  |  |  |

Observed and predicted values ​​in variable 1 (time) and variable 2 (qt).

PMC

Observed and predicted values ​​in variable 1 (time) and variable 2 (qt).

Isotherm Models

Isotherm models at 25°C and pH 5 in PMC and SN-PMC.

Isotherm models at 25°C and pH 4 in PMC and SN-PMC.

Isotherm models at 25°C and pH 3 in PMC and SN-PMC.

Isotherm models at 30°C and pH 5 in PMC and SN-PMC.

Isotherm models at 30°C and pH 4 in PMC and SN-PMC.

Isotherm models at 30°C and pH 3 in PMC and SN-PMC

Isotherm models at 40°C and pH 5 in PMC and SN-PMC.

Isotherm models at 40°C and pH 4 in PMC and SN-PMC.

Isotherm models at 40°C and pH 3 in PMC and SN-PMC.

Variance Analysis

Variance Analysis

Pareto diagram a) PMC and b) SN-PMC

Variance Analysis of the adjusted models with respect to PMC adsorbent.

| Fountain | GL | SC Adjust. | MC Adjust. | F value | P Value |
| --- | --- | --- | --- | --- | --- |
| Model | 17 | 5979.83 | 351.75 | 26988.23 | 0.000 |
| Lineal | 5 | 5845.20 | 1169.04 | 89694.09 | 0.000 |
| Temperature (°C) | 2 | 79.38 | 39.69 | 3045.09 | 0.000 |
| pH | 2 | 19.61 | 9.81 | 752.35 | 0.000 |
| Concentration (mg/L) | 1 | 5746.21 | 5746.21 | 440875.58 | 0.000 |
| 2-term interactions | 8 | 116.18 | 14.52 | 1114.22 | 0.000 |
| Temperature (°C)*pH | 4 | 18.47 | 4.62 | 354.31 | 0.000 |
| Temperature (°C)*Concentration (mg/L) | 2 | 78.91 | 39.46 | 3027.34 | 0.000 |
| pH*Concentration (mg/L) | 2 | 18.79 | 9.40 | 720.91 | 0.000 |
| 3-term interactions | 4 | 18.45 | 4.61 | 353.95 | 0.000 |
| Temperature (°C)*pH*Concentration (mg/L) | 4 | 18.45 | 4.61 | 353.95 | 0.000 |
| Error | 18 | 0.23 | 0.01 |  |  |
| Total | 35 | 5980.07 |  |  |  |

| S | R-squared | R squared (adjusted) | R squared (pred) |
| --- | --- | --- | --- |
| 0.1142 | 100.00% | 99.99% | 99.98% |
| S | R-squared | R squared (adjusted) | R squared (pred) |
| 0.1142 | 100.00% | 99.99% | 99.98% |

Variance Analysis of the adjusted models with respect to PMC adsorbent.

Table.  Variance Analysis of the adjusted models with respect to SN-PMC.

| Fountain | GL | SC Adjust. | MC Adjust. | F Value | P Value |
| --- | --- | --- | --- | --- | --- |
| Model | 17 | 7158.21 | 421.07 | 4920.81 | 0.000 |
| Linear | 5 | 7119.76 | 1423.95 | 16640.90 | 0.000 |
| Temperature (°C) | 2 | 6.56 | 3.28 | 38.31 | 0.000 |
| pH | 2 | 7.29 | 3.65 | 42.61 | 0.000 |
| Concentration (mg/L) | 1 | 7105.91 | 7105.91 | 83042.62 | 0.000 |
| 2-term interactions | 8 | 26.08 | 3.26 | 38.10 | 0.000 |
| Temperature (°C)*pH | 4 | 12.86 | 3.21 | 37.57 | 0.000 |
| Temperature (°C)*Concentration (mg/L) | 2 | 6.47 | 3.24 | 37.82 | 0.000 |
| pH*Concentration (mg/L) | 2 | 6.75 | 3.37 | 39.44 | 0.000 |
| 3-term interactions | 4 | 12.37 | 3.09 | 36.15 | 0.000 |
| Temperature (°C)*pH*Concentration (mg/L) | 4 | 12.37 | 3.09 | 36.15 | 0.000 |
| Error | 18 | 1.54 | 0.09 |  |  |
| Total | 35 | 7159.75 |  |  |  |

Table. Variance Analysis of the adjusted models with respect to SN-PMC adsorbent.

| S | R-squared | R squared (adjusted) | R squared (pred) |
| --- | --- | --- | --- |
| 0.2925 | 99.98% | 99.96% | 99.91% |

Pareto diagram a) PMC and b) SN-PMC.

| Factor | Niveles | Valores |
| --- | --- | --- |
| Temperature (°C) | 3 | 25, 30, 40 |
| pH | 3 | 3, 4, 5 |
| Concentration (mg/L) | 2 | 5, 550 |

Table. Factor information in PMC.

Table. Factor information in SN-PMC.

| Factor | Niveles | Valores |
| --- | --- | --- |
| Temperature (°C) | 3 | 25, 30, 40 |
| pH | 3 | 3, 4, 5 |
| Concentration (mg/L) | 2 | 5, 550 |

Effects and interactions of analysis of variance

Interaction of factors (pH, Temperature, Concentration) in PMC.

Interaction of factors (pH, Temperature, Concentration) in SM-PMC.

Interaction of the effects of factors (Temperatura, pH) in PMC.

Interaction of the effects of factors (Temperatura, pH) in SN-PMC.