<Supplementary Information>

Nanodiamond enhanced mechanical and biological properties of extrudable gelatin hydrogel cross-linked with tannic acid and ferrous sulphate

Amitava Bhattacharyya 1, 2, 3, V. N. Karthikai Priya 3, Ji-hyun Kim 1, Mst Rita Khatun 1, R. Nagarajan 3, Insup Noh 1, 2*

a Department of Chemical and Biomolecular Engineering, Seoul National University of Science and Technology, Seoul 01811, Republic of Korea

b Convergence Institute of Biomedical Engineering and Biomaterials, Seoul National University of Science and Technology, Seoul 01811, Republic of Korea

c Functional, Innovative and Smart Textiles, PSG Institute of Advanced Studies, Coimbatore 641004, India *insup@seoultech.ac.kr

Supporting data file

Table 1. Different combination of components used for optimization.

| Gelatin (g) | Tannic acid (g) in 2 ml water | FeSO4 (g) |
| --- | --- | --- |
| 2 in 8 ml water | 0.05 | 0.01 |
|  |  | 0.02 |
|  |  | 0.03 |
|  | 0.1 | 0.01 |
|  |  | 0.02 |
|  |  | 0.03 |
|  | 0.15 | 0.01 |
|  |  | 0.02 |
|  |  | 0.03 |

Table 2. Extrusion images of different gel samples (Gel: gelatin, TA: Tannic acid, FS: Ferrous sulfate; the amount (in g) of TA and FS mentioned in the samples, 2 g gelatin used in each case)

| Sample | Image |
| --- | --- |
| Gel/TA-0.1/FS-0.01 |  |
| Gel/TA-0.1/FS-0.02 |  |
| Gel/TA-0.1/FS-0.03 |  |
| Gel/TA-0.05/FS-0.01 |  |
| Gel/TA-0.05/FS-0.02 |  |
| Gel/TA-0.05/FS-0.03 |  |
| Gel/TA-0.15/FS-0.01 |  |

Figure 1: ND in water using dynamic light scattering (DLS) technique, (a) particle size distribution, (b) zeta protentional

Gel-ND 3 kept for solubility              Gel-ND 3 insoluble after 6 days

Figure 2: Solubility test for nanocomposite gel