Supplementary material

Production and separation of 43Sc for radiopharmaceutical purposes

Katharina A. Domnanich1,2, Robert Eichler1,2, Cristina Müller3,4, Sara Jordi1,2, Vera Yakusheva5, Saverio Braccini6, Martin Behe1,3, Roger Schibli3,4, Andreas Türler2, Nicholas P. van der Meulen1,3*

1Laboratory of Radiochemistry, Paul Scherrer Institute, 5232 Villigen PSI, Switzerland

2Department of Chemistry and Biochemistry University of Bern, 3012 Bern, Switzerland

3Center for Radiopharmaceutical Sciences ETH-PSI-USZ, Paul Scherrer Institute, 5232 Villigen PSI, Switzerland

4Department of Chemistry and Applied Biosciences, ETH Zurich, 8093 Zurich, Switzerland

5GSI Helmholtzzentrum für Schwerionenforschung GmbH, 64291 Darmstadt, Germany

6Albert Einstein Center for Fundamental Physics (AEC), Laboratory for High Energy Physics (LHEP), University of Bern, Sidlerstrasse 5, 3012 Bern, Switzerland

E-mail addresses:

katharina.domnanich@psi.ch; robert.eichler@psi.ch, cristina.mueller@psi.ch; sara.jordi@psi.ch; v.yakusheva@gsi.de; saverio.braccini@lhep.unibe.ch; martin.behe@psi.ch; roger.schibli@psi.ch; andreas.tuerler@dcb.unibe.ch; nick.vandermeulen@psi.ch

* Corresponding author:

Dr. Nicholas P. van der Meulen

Laboratory of Radiochemistry

Paul Scherrer Institute

5232 Villigen-PSI

Switzerland

e-mail: nick.vandermeulen@psi.ch

phone: +41-56-310 50 87

fax:      +41-56-310 28 49

A43Sccalc=σ*ϕ*NT*(1-e-λ*tirr)

Supplementary Fig. S1a Formula for the calculation of the 43Sc activity in Bq (s-1), accessible under the applied irradiation conditions. σ = nuclear cross section of the 46Ti(p,α)43Sc and 43Ca(p,n)43Sc reaction in cm-2, NT = number of 46Ti or 43Ca atoms, Φ = proton flux in protons*s-1, λ = decay constant of 43Sc in s-1, tirr = irradiation time in s

f(43Sc)=A(43Sc)calcA(43Sc)exp

Supplementary Fig. S1b Formula for the discrepancy f between the theoretically achievable and the experimentally obtained 43Sc activity (dimensionless).

Supplementary Fig. S2 XRD Spectra of reduced 46Ti metal of a sample with a determined reduction yield of 99% (a) and 96% (b). The remaining species, insoluble by the HCl dissolution, were identified as TiO in both cases.

Supplementary Fig. S3 XRD Spectrum of precipitated, natural TiO2 after drying at 400 °C for 1 h.

Supplementary Fig. S4 Measured cross section values (squares, triangles and dots, retrieved from the EXFOR database and Carzaniga et al.) (Carzaniga, Auger et al. 2017, International Atomic Energy Agency 2017) as well as the theoretical calculations from the TENDL-2015 library (Koning, Rochman et al. 2015) for the 43Ca(p,n)43Sc (a), 44Ca(p,n)44Sc (b) and the 46Ti(p,α)43Sc (c) nuclear reaction

Supplementary Table S5 Trace metal analysis of the purchased 46TiO2 and reduced 46Ti metal by ICP-OES. Only the elements determined at a concentration higher than the detection limit are listed below

| Element | Ratio of element per mg of Ti |  |
| --- | --- | --- |
|  | purchased 46TiO2 | reduced to 46Ti metal |
| Ca | 3.7*10-5 | 4.9*10-3 |
| Mg | 5.2*10-6 | 1.8*10-4 |
| Sr | 2.4*10-7 | 1.1*10-3 |
| Ti | 1 | 1 |
| Zr | 3.4*10-5 | 6.6*10-4 |

References

Carzaniga, T. S., M. Auger, S. Braccini, M. Bunka, A. Ereditato, K. P. Nesteruk, P. Scampoli, A. Türler and N. Van der Meulen (2017). "Measurement of 43Sc and 44Sc production cross-section with an 18 MeV medical PET cyclotron." Appl Radiat Isot.

International Atomic Energy Agency. (2017). "Experimental Nuclear Reaction Data (EXFOR)."   Retrieved 04.09.2017, from https://www-nds.iaea.org/exfor/exfor.htm.

Koning, A. J., D. Rochman, J. Kopecky, C. Sublet, E. Bauge, S. Hilaire, P. Romain, B. Morillon, H. Duarte, S. van der Marck, S. Pomp, H. Sjostrand, R. Forrest, H. Henriksson, O. Cabellos, S. Goriely, J. Leppanen, H. Leeb, A. Plompen and R. Mills. (2015). "TENDL-2015: TALYS-based evaluated nuclear data library."   Retrieved 05.03.2017, from https://tendl.web.psi.ch/tendl_2015/tendl2015.html.