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Additional File 2. Autodesk Ember PR48 resin formulation. Figure reproduced with permission from Autodesk.
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PR48 Formulation (all percentages are wt/wt):

+ Oligomer: Allnex Ebecryl 8210 39.776%, Sartomer SR 494 39.776%
+ Photoinitiator: Esstech TPO+ (2,4,6-Trimethylbenzoyl-diphenylphosphineoxide) 0.400%
+ Reactive diluent: Rahn Genomer 1122 19.888%

+ UV blocker: Mayzo OB+ (2,2'~(2,5-thiophenediybis(5-tertbutylbenzoxazole)) 0.160 %
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For more information and where to order, visit the Ember Website
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Autodesk Ember PR48 resin formulation. 


Figure reproduced with permission 


from Autodesk.
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