Additional file

Table A1. MENP material properties.

|  | Symbol | CFO | BTO | Reference |
| --- | --- | --- | --- | --- |
| Electrical conductivity |  | 4.2e-5 S/m | 1e-7 S/m | [1], [2] respectively |
| Density | r | 5200 Kg/m3 | 5700 Kg/m3 | COMSOL library |
| Initial magnetic susceptibility | 𝑋! | 70 | Not applicable | [3] |
| Saturation magnetostriction | 𝜆" | -200 ppm | Not applicable | [4] |
| Saturation magnetization | 𝑀" | 2.47e5 A/m | Not applicable | [4] |
| Poisson’s ratio | 𝑣 | 0.48 | Not applicable | COMSOL library |
| Young’s modulus | 𝐸 | 230 GPa | Not applicable | [5] |
| Relative permittivity | 𝜀# | {9.0355, 9.0355, 10.5037} | {1115.1; 1115.1; 1251.3} | COMSOL library |
| Elasticity matrix, voigt notation | {cE11, cE12, cE22, cE13, cE23, cE33, cE14, cE24, cE34, cE44, cE15, cE25, cE35, cE45, cE55, cE16, cE26, cE36, cE46, cE56, cE66}; cEij = cEji | Not applicable | {150.4; 65.6; 150.4; 65.9; 65.9; 145.5; 0; 0; 0; 43.9; 0; 0; 0; 0; 43.9; 0; 0; 0; 0; 0; 42.4} GPa | COMSOL library |
| Coupling matrix, voig notation | {𝑒𝐸𝑆11; 𝑒𝐸𝑆21; 𝑒𝐸𝑆31; 𝑒𝐸𝑆12; 𝑒𝐸𝑆22; 𝑒𝐸𝑆32; 𝑒𝐸𝑆13; 𝑒𝐸𝑆23; 𝑒𝐸𝑆33; 𝑒𝐸𝑆14; 𝑒𝐸𝑆24; 𝑒𝐸𝑆34; 𝑒𝐸𝑆15; 𝑒𝐸𝑆25; 𝑒𝐸𝑆35; 𝑒𝐸𝑆16; 𝑒𝐸𝑆26; 𝑒𝐸𝑆36} | Not applicable | {0; 0; -4.32; 0; 0; -4.32; 0; 0; 17.4; 0; 11.4; 0; 11.4; 0; 0; 0; 0; 0} C/m2 | COMSOL library |
| Domain wall density | a | 1.5e5 A/m | Not applicable | [6] [7] |
| Pinning loss | k | 2e5 A/m | Not applicable | [6] [7] |
| Magnetization reversibility | c | 0.4 | Not applicable | [6] [7] |
| Interdomain coupling | alpha | 1.4 | Not applicable | [6] [7] |

Table A2. Eigenmodes and Q-factor obtained from the Eigenfrequency study for MENP with different core diameters.

| dCORE = 25 nm |  | dCORE = 50 nm |  | dCORE = 100 nm |  |
| --- | --- | --- | --- | --- | --- |
| Eigenfrequency (GHz) | Q-factor | Eigenfrequency (GHz) | Q-factor | Eigenfrequency (GHz) | Q-factor |
| 6.447 | 77115 | 5.2733 | 84306 | 3.6589 | 91135 |
| 49.049+0.001i | 17115 | 36.135+7E-4i | 27140 | 23.462+3E-4i | 46865 |
| 63.827+0.003i | 12394 | 47.341+0.002i | 15478 | 32.247+6E-4i | 25353 |
| 70.652+0.003i | 13902 | 52.258+0.001i | 20803 | 34.630+4E-4i | 40480 |
| 85.626+0.004i | 12023 | 62.099+0.002i | 14075 | 41.286+0.001i | 18311 |
| 89.219+0.003i | 13010 | 64.727+0.002i | 16539 | 43.525+7E-4i | 31739 |

| dCORE = 150 nm |  | dCORE = 200 nm |  | dCORE = 250 nm |  |
| --- | --- | --- | --- | --- | --- |
| Eigenfrequency (GHz) | Q-factor | Eigenfrequency (GHz) | Q-factor | Eigenfrequency (GHz) | Q-factor |
| 2.7137 | 94364 | 2.2940 | 95448 | 1.9274 | 96405 |
| 17.302 | 60393 | 13.687 | 68881 | 11.317 | 74450 |
| 24.441+3E-4i | 36466 | 19.736+2E-4i | 46187 | 16.497 | 54101 |
| 25.739 | 57325 | 20.418 | 68146 | 16.910 | 74916 |
| 31.495+6E-4i | 24356 | 25.517+4E-4i | 31086 | 21.455 | 54265 |
| 32.703+3E-4i | 48567 | 26.051 | 60060 | 21.628 | 70051 |

Fig. A1. Characterization of MENP (dCORE = 50 nm, tSHELL = 15 nm) at HDC = 12 kOe in terms of magnetization, electric field norm, electric potential and strain.

Fig. A2. Electromechanical resonance frequency as a function of static bias magnetic field (HDC) of a MENP with different core diameter values. For each core diameter the maximum shift in resonance frequency and the maximum sensitivity are reported.