Sustainable Metal-Free Leather Manufacture via Synergistic Effects of Triazine Derivative and Vegetable Tannins

Yuanhang Xiao 1, Jiajing Zhou 1,2, Chunhua Wang 1, Jinwei Zhang 1, Vera D. Radnaeva 3,

Wei Lin 1,4*

- Department of Biomass and Leather Engineering, Key Laboratory of Leather Chemistry and Engineering of Ministry of Education, Sichuan University, Chengdu 610065, China

- Department of NanoEngineering, University of California San Diego, 9500 Gilman Drive, La Jolla, CA 92093, United States

- Department of Leather and Fur Technology · Water Resources and Commodity Research, East Siberia State University of Technology and Management, Ulan-Ude, Buryatia 670013, Russia

- National Engineering Research Center of Clean Technology in Leather Industry, Sichuan University, Chengdu 610065, China

* Corresponding Author: Email: wlin@scu.edu.cn (W.L.)

Fig. S1 Schematic diagram of structure and hydrolysis of SACC.

Fig. S2 Structural representation of condensed tannins (a: wattle, b: quebracho, c: bayberry) and hydrolysable tannins (d: chestnut, e: valonea, f: tara).

Fig. S3 The UV spectra of different tanning spent liquors and standard curves of six tannin extracts (a: wattle, b: bayberry, c: quebracho, d: valonea, e: chestnut, f: tara). The insets show the standard curves of six tannin extracts.

Table S1. The combination tanning process of SACC and tannins

| Process | Chemicals | Dosage / % | T / ℃ | Time / min | Remarks |
| --- | --- | --- | --- | --- | --- |
| SACC tanning | Water | 70 | 25 |  | pH ~7.8 |
|  | SACC | 10 |  | 120 |  |
|  | Hot water | 50 | 40 | 120 |  |
|  | Hot water | 50 | 45 | 240 | pH ~5.0 |
|  | Washed, piled overnight; shaved, weighed (baseline of material dosage) |  |  |  |  |
| Rewetting | Water | 150 | 40 |  |  |
|  | oxalic acid | 0.5 |  |  |  |
|  | disodium EDTA | 0.3 |  |  |  |
|  | Degreasing agent | 0.1 |  |  |  |
|  | Wetting agent | 0.2 |  | 60 | pH ~3.5 |
| Neutralization | Water | 150 | 35 |  |  |
|  | Neutralize tannin | 2 |  | 20 |  |
|  | Sodium bicarbonate | 0.5 |  | 60 | pH 4.5−4.7 |
| Vegetable tanning | Water | 80 | 35 |  |  |
|  | tannins | 10−30 |  | 180 |  |
|  | Formic acid | 0.5 |  | 30 | pH ~3.5 |
|  | Washed and piled for 24 h |  |  |  |  |

Table S2. The post-tanning process of tanned leathers

| Process | Chemicals | Dosage / % | T / ℃ | Time / min | Remarks |
| --- | --- | --- | --- | --- | --- |
| Retanning | Water | 80 | 35 |  |  |
|  | DESOATEN NHK | 1 |  |  |  |
|  | DESOPON LQ-5 | 5 |  | 10 |  |
|  | DOWELLTAN RV | 2 |  |  |  |
|  | LEUROTAN 8090 | 2 |  |  |  |
|  | LEUKOTAN 970 | 1 |  | 30 |  |
|  | RETINGAN R6 | 4 |  |  |  |
|  | RETINGAN R7 | 2 |  |  |  |
|  | LEVOTAN X-BIOMER R | 2 |  |  |  |
|  | TANIGAN OS | 1 |  | 30 |  |
|  | TANIGAN AN | 4 |  |  |  |
|  | TANIGAN VR | 3 |  |  |  |
|  | TANIGAN OS | 1 |  | 30 |  |
|  | HCOOH | 0.6 |  | 30 | pH ~4.5 |
| Dyeing | Water | 80 | 50 |  |  |
|  | NH3·H2O | 0.5 |  | 10 |  |
|  | Dye | 3 |  | 60 |  |
| Fatiliquoring | DESOPON DPF | 2 | 50 |  |  |
|  | TRUPON K1 | 2 |  |  |  |
|  | TRUPON LNC | 1 |  |  |  |
|  | TRUPON SWS | 1 |  |  |  |
|  | DESOPON PM-S | 1 |  | 40 |  |
|  | Formic acid | 2 |  | 15*3+30 | pH ~3.5 |
|  | Washed and piled overnight |  |  |  |  |

Note: DESOATEN NHK, DESOPON LQ-5, DESOPON DPF and DESOPON PM-S from Sichuan Decision New Material Technology Co., Ltd. DOWELLTAN RV form Sichuan Dowell. LEUROTAN 8090 and LEUKOTAN 970 from Rohm and Haas. RETINGAN R6, RETINGAN R7, LEVOTAN X-BIOMER R, TANIGAN OS, TANIGAN AN and TANIGAN VR from Lanxess. TRUPON K1, TRUPON LNC and DESOPON PM-S from Trumpler.

Table S3. The solo tanning process of the vegetable tannins

| Process | Chemicals | Dosage / % | T / ℃ | Time / min | Remarks |
| --- | --- | --- | --- | --- | --- |
| Depickling | Water | 100 | 25 |  |  |
|  | NaCl | 8 |  | 30 |  |
|  | Sodium bicarbonate | 1 |  | 60 | pH 4.5−5.0 |
| Vegetable tanning | Tannins | 25 | 25 | 240 | 180 |
|  | Formic acid | 0.5 |  | 30 | pH ~3.5 |
|  | Washed and piled for 24 h |  |  |  |  |