Table S2 x in ZnSnN2-xOx, electron density (ne), and Drude parameters (plasma energy, ωp and broadening factor, ΓD in the Drude function) extracted from the best fit spectra shown in Fig. 2a−d in the main text. The values of Tauc-Lorentz parameters (the oscillator strength S_TL, the broadening parameter γ_TL, the resonance frequency ω0_TL, and ω0_TL is the Tauc gap frequency) listed in this table are the same as the literature value [1]

| Film | x | ne [1020 cm-3] | εD(ω) |  | εTL1(ω) |  |  |  | εTL2(ω) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | ωp [1014 s-1] | ΓD [1014 s-1] | S_TL1 [108 s-1/2] | γ_TL1 [1015 s-1] | ω0_TL1 [1015 s-1] | ωgap_TL1 [1014 s-1] | S_TL2 108 s-1/2] | γ_TL2 [1015 s-1] | ω0_TL2 [1015 s-1] | ωgap_TL2 [1014 s-1] |
| #1 | 0.055 | 2.8 | 2.51 | 0.339 | 0.933 | 0.800 | 0.643 | 3.01 | 1.84 | 3.51 | 2.02 | 6.38 |
| #2 | 0.069 | 3.0 | 2.68 | 0.339 |  |  |  |  |  |  |  |  |
| #3 | 0.071 | 3.3 | 2.78 | 0.314 |  |  |  |  |  |  |  |  |
| #4 | 0.074 | 4.8 | 3.10 | 0.387 |  |  |  |  |  |  |  |  |
| #5 | 0.079 | 5.1 | 3.17 | 0.629 |  |  |  |  |  |  |  |  |

The imaginary part of εTL(ω) is given by [2]

ImεTLω =1ωS2ω0γω-ωgap2ω2-ω022+ω2γ2 for ω>ωgap0                   for ω≦ωgap

where S is the oscillator strength, γ is the damping constant, ω0 is the resonance frequency, and ωgap corresponds to the gap energy (ћωgap). The real part of εTL(ω) is derived via the Kramers-Kronig transformation.

References

1. Deng F, Cao H, Liang L, Li J, Gao J, Zhang H, Qin R, Liu C. Determination of the basic optical parameters of ZnSnN2. Opt Lett. 2015; 40: 1282–5.

2. Jellison Jr GE. and Modine FA. Parameterization of the optical functions of amorphous materials in the interband region. Appl Phys Lett. 1996; 69: 371–3.