Supplementary Information

Photonic memristive devices for in-memory matrix operation

Junying Li1,2*, Weibiao Chen1,3, Yikai Su2, Xuhan Guo2,*

1 Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences; Hangzhou, 310024, China.

2 State Key Laboratory of Micro-Nano Engineering Science, State Key Laboratory of Photonics and Communications, School of Information and Electronic Engineering, Shanghai Jiao Tong University; Shanghai, 200240, China.

3 Aerospace Laser Technology and System Department, Shanghai Institute of Optics and Fine Mechanics, Chinese Academy of Sciences; Shanghai, 201800, China

*Correspondence: junyingli@ucas.ac.cn, guoxuhan@sjtu.edu.cn

Table S1 Key performance of nonvolatile phase tuning approaches

| Nonvolatile phase tuning |  | Δneff | Lπ (mm) | Eπ | Vdrive | tswitching | Bit (bit) | ILp (dB) | Cycles | Fab process |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PCM | Sb2Se3 (E) [1] | 0.053 | 14.6 | Amo: 85.17 nJ Cry: 892.2 nJ | 8-10V; 2.7-3.26V | 100ns; 10µs | 6 | 0.29 | 104 | BEOL |
|  | Sb2Se3 (O) [2] | 0.072 | 25 | Amo: 700 nJ Cry: 47.5 mJ | N/A | 400 ns; 50 ms | >5 | 0.35 | 600 |  |
|  | Sb2Se3 (E)a | 0.02 | 66.7 | Amo: 485.5 nJ Cry: 266.5 μJ | 2.83/4.58 V; 1.95 V | 400 ns; 1.5 ms | 1 | 0.5 | 108 |  |
|  | Sb2S3 (E)[3] | 0.018 | 30.7 | Amo: 171.9 nJ Cry: 5.22 μJ | 7.5V; 1.6V | 150ns; 100µs | 5 | 0.74 | >1600 |  |
| CT | GaAs/HfO2/Al2O3/Si[4] | 2.5×10-4 | 2500 | SET: 1.29 nJ RESET: 0.71 nJ | 9V -5V | 1s | 2 | 3.57 | 100 | Wafer bonding |
| FE | BTO-Si[5] | 2×10-3 | 1000 | SET: 178 pJ RESET: 1.8 mJ | 5-12V; 12.1V | 1 ms; 0.7 s | 3 | 0.48 | 300 | Wafer bonding |
|  | PZT[6] | 4.6×10-3 | 1000 | SET: 196.8 pJ RESET: 1.23 nJ | 8~32 V; 80V | 1 ms | >2 | 0.19 | 105 | Non-Si |
|  | HZO-SiN[7] | 1.5×10-4 | 5167 | 0.69 mJ | 210V | 10-100 s | >3 | ~0 | 0 | FEOL |
|  | HAO-Si[8] | 0.003 | 258 | 18.7 nJ | +5/-5 | 100 μs | 1.5 | 4.67 | 106 | FEOL |
|  | HZO-LN[9] | 1.7×10-4 | 4553 | SET: 3.1 pJ RESET: 358.2 fJ | -6V 3 V | 10 μs | 4b | 3.28 | 107 | Non-Si |
| MO | Ce: YIG-Si[10] | 5.66×10-4 | 1369 | 230 pJ | <±1 V | 1 ns | 3.5 | 11.25 | 109 | Wafer bonding |
| MR | GaAs/Al2O3/Si[11] | 1.88×10-3 | 350 | SET: 0.83 pJ RESET: 2.0 pJ | 5V -4V | 0.3 ns 0.9 ns; | 1.5 | 0.27 | 103 | Wafer bonding |

a From Arka Majumdar's group (manuscript under review).

b 4 bits achieved by cascading three FE field effect transistors in a single MRR with 6 optical states per transistor.

Table S2 Key performance of nonvolatile amplitude tuning approaches

| Non-volatile amplitude tuning |  | Δneff | LdB (mm) | EdB | Vdrive | tswitching | Bit (bit) | ILdB (30 dB) | Cycles | Fab Process |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PCM | GST (O) [12,13] | 0.096+0.063i | 3.51 | Amo: 118.4 pJ; Cry: 596.5 pJ | N/A | 50 ns 250 ns | 5 | 8.3223 | 200 | BEOL |
|  | GST (E) [14,15] | 0.1+0.049i24 | 0.61 | Amo: 2.13nJ; Cry: 1.67 nJ | 5.2-6.8V 3V | 50 ns 200ns | 4 | 624 | 100 |  |
|  | GSST [16,17] | 0.081+0.024i | 0.41 | Amo: 4.2 nJ; Cry: 0.055 mJ | 7.5-8.8 V 1.9-2.25 V | 500 ns 100 ms | >7 | 1.07 | 104 |  |
|  | GSSe [18] | 0.034-0.012i | 5 | Amo: N/A; Cry: 1.5 nJ | 12V 8V | 2 μs >20 μs | 4b | 0.4 | 5105 |  |
| MEMS | vdW MEMS [19] | N/A | 0.84 | SET: 12.6 nJ RESET: 22.5 nJ | 35V | 10 μs 8 μs | 1 | 0.23 | ＞106 | BEOL |
| EC | WO3-LN [20] | 0.59i | 0.5 | SET: 14.56 pJ RESET: 14.56 pJ | 2.5V -2.5V | 8.42 s 3.3 s | >4 | 10.95 | 200 | Non-Si |

Supplementary Note 1.

Tradeoffs in ferroelectric materials-based optical memristors

The low nonvolatile switching energy and ultralow propagation loss are the characteristic advantages of ferroelectric waveguides, including BaTiO₃ (BTO)[5] and lead zirconate titanate (PZT)[6]. The emergence of PZT has addressed the issue in BTO-based devices, which require a constant bias to probe refractive index changes. However, the relatively high-voltage pulses needed (80 V for RESET and 32V for programming, for instance) could pose a challenge for large-scale array control. The Vdrive could be significantly reduced by employing thinner FE films and tuning the effective refractive index (neff) of hybrid waveguides indirectly. Recently, the integration of nonvolatile reconfigurability in Zr-HfO₂ (HZO) ferroelectric thin films with the high-speed Pockels effect in thin-film lithium niobate (TFLN) waveguides[9] marked a milestone, achieving a Vdrive of 6 V, a tswitching of 10 μs, an Eπ of ~3.1 pJ, 4-bit precision, and an endurance of 10⁷ cycles. We are expecting that further performance improvements could be attained by adopting materials with lower coercive fields and robust ferroelectric properties at reduced thicknesses. The deficiency of FE materials lies in their fundamentally-limited low modulation efficiency and commonly seen millimeter-scale modulation lengths. In HZO-TFLN-based devices, the large length required for a π-phase shift (Lπ) of ~4.5 mm also leads to an insertion loss (ILπ) of ~1.2 dB. Since the intrinsic loss of FE materials is very low, the observed loss in these devices may be attributed to the use of the ITO top gate, suggesting a potential avenue for further optimization.

Therefore, although with ultralow switching power down to 3.1 pJ/π, current FE materials offer tailored trade-offs between drive voltage (e.g., 80 V for PZT and 6 V for HZO-TFLN) and insertion loss (e.g., 0.19 dB/π for PZT and 3.28 dB/π for HZO-TFLN)[6,9]. Note that they do not exhibit a significant advantage in programming speed compared to PCM (e.g., 1 ms for PZT, 10 μs for HZO-TFLN, and 10 μs for Sb2Se3-Si[1]).

Supplementary Note 2.

Charge trapping for nonvolatile phase tuning or amplitude modulation?

Charge-trapping optical memristors are inspired by Flash memory technology. Trapping and releasing charges in a capacitor could modulate the waveguide’s refractive index via changes in carrier concentration induced by electrostatic effects. Recent advances make an obvious performance improvement over earlier devices[21,22] by employing a GaAs-Al₂O₃-HfO₂-Al₂O₃-HfO₂-Si waveguide stack[4], and achieve 2-bit phase tuning with a switching time of 1 s, energy consumption of 1.29 nJ/π, and a Vdrive of 9 V. Although further attempts explored a foundry-compatible design using avalanche-induced charge trapping in Si waveguides, they were ultimately hampered by an impractical switching time of 1500 s and a high energy cost of 1.2 J[23]. Due to the free-carrier dispersion in CT-based devices, optical loss is inevitably induced when implementing phase tuning. Meanwhile, the low modulation efficiency of CT also results in a small dynamic range for intensity modulation. As such, we consider it a phase-shifting approach for small phase adjustment with a relatively large footprint (~2.5 mm per π-phase shift) and high insertion loss (~ 3.5 dB per π-phase shift).

Supplementary Note 3.

Electrochromic optical tuning and nonvolatile MEMS

Electrochromic effect (EC) could modulate the amplitude of propagating light in waveguides, but suffers from prohibitively slow switching speeds and poor CMOS compatibility[20,24].

Nonvolatile MEMS operates more digitally, since it relies on latch structure[25], buckling[26], or stiction effect[19] to lock the movable components into a stable position. exhibiting a bistable (on/off) behavior for now at relatively high drive voltages. Nonvolatile MEMS is more suitable for optical switch arrays instead of matrix operation, and is therefore out of scope of this perspective. Consequently, these methods are not discussed in detail.

Supplementary Note 4.

Endurance of PCMs-integrated silicon photonic devices

The challenges of achieving high endurance are similar to the bit precision issue for now, since they both originated from the suboptimal device structures at this stage. Particularly, low-loss PCMs, compared to insulator-metal-transition materials like GST, exhibit more pronounced volume changes during the phase transition process, thus necessitating elaborate device engineering to ensure operational stability throughout the switching cycles. This may involve the optimization of nano-patterned PCM patches, thermal uniformity, capping layers, and other device designs[27]. Substantial progress has been made in this regard—the endurance of Sb2Se3 optical memristors has been improved to a stable 10⁸ cycles (by Arka Majumdar's group, manuscript under review). As the cycling endurance approaches 109, further optimization of PCMs to achieve lower phase segregation and lower mechanical stress has to be addressed.

References

[1]	X. Yang, L. Lu, Y. Li, Y. Wu, Z. Li, J. Chen, and L. Zhou, Non‐Volatile Optical Switch Element Enabled by Low‐Loss Phase Change Material. Advanced Functional Materials 33 (2023). doi:10.1002/adfm.202304601.

[2]	M. Delaney, I. Zeimpekis, H. Du, X. Yan, M. Banakar, D. J. Thomson, D. W. Hewak, and O. L. Muskens, Nonvolatile programmable silicon photonics using an ultralow-loss Sb2Se3 phase change material. Science Advances 7 (2021). doi:10.1126/sciadv.abg3500.

[3]	R. Chen et al., Non-volatile electrically programmable integrated photonics with a 5-bit operation. Nature Communications 14 (2023). doi:10.1038/s41467-023-39180-3.

[4]	S. Cheung et al., Ultra‐Power‐Efficient, Electrically Programmable, Multi‐State Photonic Flash Memory on a Heterogeneous III‐V/Si Platform. Laser & Photonics Reviews 18 (2024). doi:10.1002/lpor.202400001.

[5]	J. Geler-Kremer, F. Eltes, P. Stark, D. Stark, D. Caimi, H. Siegwart, B. Jan Offrein, J. Fompeyrine, and S. Abel, A ferroelectric multilevel non-volatile photonic phase shifter. Nature Photonics 16, 491 (2022). doi:10.1038/s41566-022-01003-0.

[6]	C. Li et al., PZT optical memristors. Nat Commun 16, 6340 (2025). doi:10.1038/s41467-025-61536-0.

[7]	K. Taki, N. Sekine, K. Watanabe, Y. Miyatake, T. Akazawa, H. Sakumoto, K. Toprasertpong, S. Takagi, and M. Takenaka, Nonvolatile optical phase shift in ferroelectric hafnium zirconium oxide. Nat Commun 15, 3549 (2024). doi:10.1038/s41467-024-47893-2.

[8]	G. Zhang et al., Thin film ferroelectric photonic-electronic memory. Light Sci Appl 13, 206 (2024). doi:10.1038/s41377-024-01555-6.

[9]	Z. Xu, C. K. Chen, H. L. Lin, M. Sivan, E. Zamburg, J. Y. Lee, S. Venkatesan, A. Danner, and A. V. Thean, Ferroelectric-based Pockels photonic memory. Nat Commun 16, 8329 (2025). doi:10.1038/s41467-025-63850-z.

[10]	P. Pintus, M. Dumont, V. Shah, T. Murai, Y. Shoji, D. Huang, G. Moody, J. E. Bowers, and N. Youngblood, Integrated non-reciprocal magneto-optics with ultra-high endurance for photonic in-memory computing. Nature Photonics 19, 54 (2024). doi:10.1038/s41566-024-01549-1.

[11]	B. Tossoun, D. Liang, S. Cheung, Z. Fang, X. Sheng, J. P. Strachan, and R. G. Beausoleil, High-speed and energy-efficient non-volatile silicon photonic memory based on heterogeneously integrated memresonator. Nature Communications 15 (2024). doi:10.1038/s41467-024-44773-7.

[12]	X. Li, N. Youngblood, C. Ríos, Z. Cheng, C. D. Wright, W. H. P. Pernice, and H. Bhaskaran, Fast and reliable storage using a 5  bit, nonvolatile photonic memory cell. Optica 6 (2018). doi:10.1364/optica.6.000001.

[13]	X. Li, N. Youngblood, Z. Cheng, S. G.-C. Carrillo, E. Gemo, W. H. P. Pernice, C. D. Wright, and H. Bhaskaran, Experimental investigation of silicon and silicon nitride platforms for phase-change photonic in-memory computing. Optica 7 (2020). doi:10.1364/optica.379228.

[14]	W. Zhou et al., In-memory photonic dot-product engine with electrically programmable weight banks. Nature Communications 14 (2023). doi:10.1038/s41467-023-38473-x.

[15]	J. Zheng et al., Nonvolatile Electrically Reconfigurable Integrated Photonic Switch Enabled by a Silicon PIN Diode Heater. Advanced Materials 32 (2020). doi:10.1002/adma.202001218.

[16]	M. Wei et al., Monolithic back-end-of-line integration of phase change materials into foundry-manufactured silicon photonics. Nat Commun 15, 2786 (2024). doi:10.1038/s41467-024-47206-7.

[17]	K. Xu et al., Back‐End‐Of‐Line Integrated Non‐Volatile Reconfigurable Devices for Programmable Photonic Integrated Circuits. Laser & Photonics Reviews (2025). doi:10.1002/lpor.202501846.

[18]	J. Meng et al., Electrical programmable multilevel nonvolatile photonic random-access memory. Light: Science & Applications 12 (2023). doi:10.1038/s41377-023-01213-3.

[19]	Y. Hu et al., Nonvolatile silicon photonic MEMS switches enabled by van der Waals force. Science Advances 11, eadv7099 (2025). doi:doi:10.1126/sciadv.adv7099.

[20]	E. Hopmann, B. N. Carnio, C. J. Firby, B. Y. Shahriar, and A. Y. Elezzabi, Nanoscale All-Solid-State Plasmochromic Waveguide Nonresonant Modulator. Nano Lett 21, 1955 (2021). doi:10.1021/acs.nanolett.0c04315.

[21]	J. F. Song et al., Integrated photonics with programmable non-volatile memory. Sci Rep 6, 22616 (2016). doi:10.1038/srep22616.

[22]	M. Grajower, N. Mazurski, J. Shappir, and U. Levy, Non‐Volatile Silicon Photonics Using Nanoscale Flash Memory Technology. Laser & Photonics Reviews 12 (2018). doi:10.1002/lpor.201700190.

[23]	Y. Yuan et al., All-silicon non-volatile optical memory based on photon avalanche-induced trapping. Communications Physics 8 (2025). doi:10.1038/s42005-025-01934-4.

[24]	J. T. Kim, J. Song, and C. S. Ah, Optically Readable Waveguide-Integrated Electrochromic Artificial Synaptic Device for Photonic Neuromorphic Systems. ACS Applied Electronic Materials 2, 2057 (2020). doi:10.1021/acsaelm.0c00314.

[25]	S. Abe and K. Hane, Variable-Gap Silicon Photonic Waveguide Coupler Switch With a Nanolatch Mechanism. IEEE Photonics Technology Letters 25, 675 (2013). doi:10.1109/lpt.2013.2248354.

[26]	M. Bagheri, M. Poot, M. Li, W. P. Pernice, and H. X. Tang, Dynamic manipulation of nanomechanical resonators in the high-amplitude regime and non-volatile mechanical memory operation. Nat Nanotechnol 6, 726 (2011). doi:10.1038/nnano.2011.180.

[27]	C. C. Popescu et al., Understanding and Circumventing Failure Mechanisms in Chalcogenide Optical Phase Change Material Ge2Sb2Se4Te. Advanced Optical Materials (2024). doi:10.1002/adom.202402751.