Engineered Vildagliptin-loaded Polymeric Nanoparticles via Microfluidic and Spray Drying for enhanced Antidiabetic activity

Eknath Kolea, Krishna Jadhavb, Zia Khana, Rahul K. Vermab, Jitendra Naika*

aDepartment of Pharmaceutical Technology, University Institute of Chemical Technology, KBC North Maharashtra University, Jalgaon M.S. 425001, India.

bPharmaceutical Nanotechnology Lab, Institute of Nano Science and Technology, Sahibzada Ajit Singh Nagar (Mohali), Punjab 140306, India.

Correspondence author*

Prof. Jitendra B. Naik

Director

University Institute of Chemical Technology,

KBC North Maharashtra University, Jalgaon M.S.425001, India

Email- jbnaik@nmu.ac.in

Phone- +91 9422205671

ORCID: 0000-0001-8906-7903

S1. Setup of Microreactor

The microreactor setup included two inlets for introducing Solutions A and B. Solution A, comprising chitosan and vildagliptin, and Solution B, containing dextran sulfate, were infused into the microreactor using Uni Labs syringe pumps to ensure constant and precise flow rates, typically varied between 0.1 to 1.0 mL/min. The narrow channels within the microreactor facilitated rapid and homogeneous mixing of the solutions.

Flow rates for both solutions were systematically adjusted between 0.2 mL/min to 0.8 mL/min to study their impact on nanoparticle size. The chitosan concentration in Solution A was maintained at 50 mg in a 0.5% acetic acid solution, while the dextran sulfate concentration in Solution B was 0.1% w/v in double-distilled water. Both solutions were stirred at a constant speed of 800 rpm using a LabQuest Motorless Magnetic Stirrer during preparation and collection. Prior to infusion, the solutions were sonicated for 15 minutes to ensure complete dispersion and removal of any agglomerates, and then filtered using a 0.45 µm filter.

The synthesis process was carried out at room temperature, approximately 25°C, to maintain the stability of the solutions and nanoparticles. The resulting nanosuspension was collected from the microreactor outlet under continuous magnetic stirring at 800 rpm to prevent aggregation and ensure uniform particle distribution.

Figure S1. (A) Schematic for microreactor setup for production of VLG nanoparticles. (B) Image for microreactor (AmAR 2 metal) assembly, a microfluidic device supplied by Amar Equipment Pvt. Ltd, India

Table S1. Summary of ANOVA for Y1, Y2, Y3, and Y4 the response CDNPs prepared by BBD

| Particle size (Y1) | Source | df | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- |
|  | Model | 9 | 12.72 | 0.0015 | significant |
|  | X1-Chitosan | 1 | 5.84 | 0.0463 |  |
|  | X2-Dextran Sulphate | 1 | 1.81 | 0.2204 |  |
|  | X3-Tween 80 | 1 | 0.3135 | 0.5930 |  |
|  | X1X2 | 1 | 10.81 | 0.0133 |  |
|  | X1X3 | 1 | 0.1701 | 0.6923 |  |
|  | X2X3 | 1 | 6.58 | 0.0373 |  |
|  | X1² | 1 | 12.58 | 0.0094 |  |
|  | X2² | 1 | 57.62 | 0.0001 |  |
|  | X3² | 1 | 20.89 | 0.0026 |  |
|  | Lack of Fit | 3 | 1.71 | 0.3020 | not significant |
| PDI (Y2) | Model | 9 | 4.76 | 0.0258 | significant |
|  | X1-Chitosan | 1 | 10.73 | 0.0136 |  |
|  | X2-Dextran Sulphate | 1 | 9.75 | 0.0168 |  |
|  | X3-Tween 80 | 1 | 1.56 | 0.2524 |  |
|  | X1X2 | 1 | 6.44 | 0.0388 |  |
|  | X1X3 | 1 | 0.0047 | 0.9475 |  |
|  | X2X3 | 1 | 5.55 | 0.0507 |  |
|  | X1² | 1 | 0.7546 | 0.4138 |  |
|  | X2² | 1 | 0.1449 | 0.7148 |  |
|  | X3² | 1 | 8.09 | 0.0249 |  |
|  | Lack of Fit | 3 | 3.05 | 0.1548 | not significant |
| EE% (Y4) | Model | 9 | 25.91 | 0.0001 | significant |
|  | X1-Chitosan | 1 | 5.19 | 0.0569 |  |
|  | X2-Dextran Sulphate | 1 | 49.57 | 0.0002 |  |
|  | X3-Tween 80 | 1 | 52.39 | 0.0002 |  |
|  | X1X2 | 1 | 55.70 | 0.0001 |  |
|  | X1X3 | 1 | 0.2871 | 0.6087 |  |
|  | X2X3 | 1 | 1.01 | 0.3479 |  |
|  | X1² | 1 | 52.10 | 0.0002 |  |
|  | X2² | 1 | 10.54 | 0.0141 |  |
|  | X3² | 1 | 6.27 | 0.0408 |  |
|  | Lack of Fit | 3 | 1.50 | 0.3426 | not significant |

Figure S2. Morphology of L6 cell line (rat skeletal muscle cell line) (10X)

S2. Drug release kinetics

To investigate the drug release mechanism and evaluate the fit of various kinetic models, the release data were analyzed using several approaches, including the Higuchi, first-order, zero-order, Hixson-Crowell, and Korsmeyer-Peppas models (Table S2). At pH 1.2, the Higuchi model (R² = 0.9007) provided the best correlation, indicating that the drug release was primarily diffusion-controlled. The first-order model (R² = 0.7395) suggested that the release rate was somewhat dependent on the drug concentration, while the zero-order model (R² = 0.6809) showed a less consistent fit, pointing to a more varied release rate. The Hixson-Crowell model (R² = 0.7203) highlighted the potential role of particle size reduction or erosion in the release process. The Korsmeyer-Peppas model (R² = 0.3159) showed poor alignment, suggesting that it is not a suitable model for describing the release mechanism at pH 1.2.

At pH 6.8, the Higuchi model (R² = 0.8648) continued to describe the release mechanism well, though diffusion appeared to be slightly less dominant than at pH 1.2. The first-order model (R² = 0.7203) showed that the release rate remained somewhat concentration-dependent, while the zero-order model (R² = 0.5156) indicated greater variability in the release rate. The Hixson-Crowell model (R² = 0.6941) again suggested a role for erosion, while the Korsmeyer-Peppas model (R² = 0.2317) provided a poor fit, reinforcing its unsuitability for this release profile. Overall, diffusion remained the primary release mechanism across both pH levels, with contributions from other processes varying depending on the pH.

Table S2. Drug release kinetics of VLG from nanoformulation

| Release kinetic Model | Formulation |  |
| --- | --- | --- |
|  | pH-1.2 | pH-6.8 |
|  | R2 | R2 |
| Zero-order kinetics | 0.6809 | 0.6401 |
| First-order kinetics | 0.7395 | 0.7203 |
| Higuchi model | 0.9007 | 0.8648 |
| Hixson-Crowell model | 0.7203 | 0.6941 |
| Korsmeyer-Peppas model | 0.3159 | 0.2317 |