Table S1 List of phthalates compounds analyzed

| Abbreviation | Name | CAS |
| --- | --- | --- |
| DMP | Dimethyl phthalate | 131-11-3 |
| DEP | Diethyl phthalate | 84-66-2 |
| DAP | Di-2-propenyl Phthalate | 131-17-9 |
| DMEP | Bis(2-methoxyethyl) phthalate | 117-82-8 |
| BMPP | Bis(4-methyl-2-pentyl) phthalate | 84-63-9 |
| DEEP | Bis(2-ethoxyethyl) phthalate | 605-54-9 |
| DPP | Di-n-propyl Phthalate | 131-16-8 |
| DNHP | Di-n-hexyl Phthalate | 84-75-3 |
| BBP | benzyl butyl phthalate | 85-68-7 |
| DBEP | Dibutoxy ethyl phthalate | 117-83-9 |
| DCHP | Dicyclohexyl phthalate | 84-61-7 |
| DEHP | bis(2-ethylhexyl)phthalate | 117-81-7 |
| DPhP | Di(2-propylheptyl) phthalate | 53306-54-0 |
| DNOP | Di-n-octyl phthalate | 117-84-0 |
| DINP | Di-iso-nonyl Phthalate | 28553-12-0 |
| DNP | Di-n-nonyl phthalate | 84-76-4 |

Table S2 Characteristics and indicator compounds related to MRM settings

| Polymer | Characteristic pyrolyzate | Precursor Ion | Product Ion | Collision Energy (eV) | RT (min) |
| --- | --- | --- | --- | --- | --- |
| PVC Polyvinyl Chloride | Napthalene | 128 | 102.1* 78.1 | 30 30 | 8.1 |
|  | Indene | 116 | 115.1 89.1 | 20 30 | 6.8 |
|  | 1-Methylindene | 130 | 129.1 115.1 | 20 30 | 7.9 |
| PET Polyethylene Terphthalates | Biphenyl | 154 | 152.1* 153.1 | 30 10 | 9.6 |
|  | Vinyl benzoate | 105 | 77.0 51.0 | 10 30 | 7.6 |
|  | Divinyl terephthalate | 175 | 147.1 104.1 | 10 10 | 10.8 |
| PE Polyethylene | 1-Heneicosene | 82 | 67.0* 41.2 | 10 20 | 13.8 |
|  | 1-Tetradecene | 82 | 67.0 41.2 | 10 20 | 9.6 |
|  | 1-Pentadecene | 82 | 67.0 41.2 | 10 20 | 10.3 |
| PS Polystyrene | 5-Hexene-1,3,5-triyltribenzene | 91 | 65.0* 51.0 | 20 40 | 15.9 |
|  | 3-Butene-1,3-diyldibenzene | 91 | 65.0 51.1 | 20 30 | 11.9 |
|  | Bibenzyl | 91 | 65.0 51.0 | 20 40 | 10.6 |
| PP Polypropylene | 2,4,6,8-tetramethyl-1-undecene | 126 | 83.1 55.1 | 10 20 | 4.6 |
|  | 2,4-Dimethyl-1-heptene | 111 | 69 41.1 | 10 20 | 8.7 |
| PMMA poly (methyl methacrylate) | Methyl methacrylate | 100 | 41.2* 69.0 | 20 10 | 2.7 |
|  | Methyl acrylate | 85 | 57.0 45.0 | 10 40 | 1.9 |

Table S3 Calibration related data for microplastics detection

| Polymer | Calibration Range |  |  |  |  | Formula | R2≧0.9801 | QDL (μg) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | CS1 | CS2 | CS3 | CS4 | CS5 |  |  |  |
| PVC | 2.808 | 6.048 | 10.8 | 21.924 | 42.552 | y = 1306.934050 * x + 6534.383221 | 0.993826872 | 2.808 |
| PET | 1.177 | 2.534 | 4.525 | 9.186 | 17.829 | y = 6426.990960 * x + 22760.911893 | 0.990029934 | 1.177 |
| PS | 0.559 | 1.204 | 2.15 | 4.365 | 8.471 | y = 478220.759722 * x - 120858.629972 | 0.99009056 | 0.559 |
| PMMA | 0.566 | 1.218 | 2.175 | 4.415 | 8.57 | y = 45320.235874 * x - 47056.436318 | 0.99009056 | 0.566 |
| PE | 10.92 | 23.52 | 42 | 85.26 | 165.48 | y = 8181.468650 * x - 46630.173361 | 0.99009056 | 10.92 |
| PP | 2.607 | 5.614 | 10.025 | 20.351 | 39.499 | y = 4007.362820 * x - 4022.786561 | 0.99009056 | 2.607 |

Table S4 Calibration related data for plastics additives analysis

| Compound | CS1 | CS2 | CS3 | CS4 | CS5 | QDL (ng) | Blank | QC (100) |  | ICV (100) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 10 | 20 | 50 | 100 | 200 | 40 | Concentration | Concentration | Recovery | Concentration | Recovery |
|  | Formula |  |  |  |  | R2 | (ppb) | (ppb) | (%) | (ppb) | (%) |
| DMP | y = 10.053250 * x + 0.151075 |  |  |  |  | 0.998714 | 0 | 98.0966 | 98.097 | 101.610 | 101.610 |
| DEP | y = 15.252431 * x - 0.079927 |  |  |  |  | 0.997806 | < QDL (5.93) | 120.4223 | 114.492 | 90.715 | 90.715 |
| DAP | y = 7.138815 * x - 0.087214 |  |  |  |  | 0.998806 | 0 | 111.7401 | 111.740 | 92.690 | 92.690 |
| DIBP&DBP | y = 10848.583796 * x + 14308.119159 |  |  |  |  | 0.999135 | < QDL (3.04) | 103.7394 | 100.699 | 102.295 | 102.295 |
| DMEP | y = 14.200067 * x + 0.084414 |  |  |  |  | 0.998717 | 0 | 96.9192 | 96.919 | 93.788 | 93.788 |
| BMPP | y = 26.515036 * x - 0.33583 |  |  |  |  | 0.988387 | 0 | 98.7464 | 98.746 | 81.462 | 81.462 |
| DEEP | y = 6.780674 * x + 0.022109 |  |  |  |  | 0.998237 | 0 | 109.6041 | 109.604 | 97.891 | 97.891 |
| DPP | y = 4.242378 * x + 0.054932 |  |  |  |  | 0.988231 | 0 | 109.1862 | 109.186 | 112.441 | 112.441 |
| DNHP | y = 74.751849 * x + 1.573208 |  |  |  |  | 0.995481 | 0 | 100.2298 | 100.230 | 99.378 | 99.378 |
| BBP | y = 16.141482 * x + 0.327213 |  |  |  |  | 0.993213 | 0 | 102.5276 | 102.528 | 83.583 | 83.583 |
| DBEP | y = 1.42029 * x + 0.011149 |  |  |  |  | 0.999836 | 0 | 106.0332 | 106.033 | 84.260 | 84.260 |
| DCHP | y = 43.528465 * x + 0.477588 |  |  |  |  | 0.997418 | 0 | 100.0790 | 100.079 | 92.717 | 92.717 |
| DEHP | y = 22.390544 * x + 0.267169 |  |  |  |  | 0.999568 | 80.1081 | 180.5370 | 100.429 | 92.749 | 92.749 |
| DPhP | y = 0.570767 * x + 0.011523 |  |  |  |  | 0.994221 | 0 | 117.4043 | 117.404 | 91.571 | 91.571 |
| DNOP | y = 70.782816 * x - 0.479188 |  |  |  |  | 0.995396 | 0 | 103.6129 | 103.613 | 96.003 | 96.003 |
| DINP | y = 29.563508 * x - 0.194967 |  |  |  |  | 0.998694 | < QDL (7.48) | 110.1038 | 102.624 | 92.649 | 92.649 |
| DNP | y = 81.757614 * x - 0.932898 |  |  |  |  | 0.998735 | 0 | 96.4889 | 96.489 | 96.067 | 96.067 |
| BPA | y = 5.088864 * x + 0.18736 |  |  |  |  | 0.995448 | 0 | 96.8918 | 96.892 | 102.307 | 102.307 |

*QDL values are expressed as instrumental detection amounts measured in the final extract. Reported environmental concentrations were calculated from the measured amount in the extract and normalized to the original water-sample volume; therefore, sample results are presented as ng/L. Method blank values were processed using the same calculation procedure and subtracted from sample concentrations for blank correction.