Additional file for

Lead halide perovskite sensitized WSe2 photodiodes with ultrahigh open circuit voltages

Sung-Joon Lee1,2,4†, Hung-Chieh Cheng1†, Yiliu Wang3, Boxuan Zhou1, Dehui Li3, Gongming Wang3, Yuan Liu1, Jian Guo1, Hao Wu1, Dae Joon Kang2*, Yu Huang1*, Xiangfeng Duan3*

1Department of Materials Science and Engineering, University of California, Los Angeles, CA, USA.

2Department of Physics, Sungkyunkwan University, Suwon, Republic of Korea.

3Department of Chemistry and Biochemistry, University of California, Los Angeles, CA, USA.

4Current affiliation: Materials Science and Technology Division, U.S. Naval Research Laboratory, Washington, DC, USA.

†Sung-Joon Lee and Hung-Chieh Cheng authors contributed equally to this work.

*Correspondence: xduan@chem.ucla.edu, yhuang@seas.ucla.edu, djkang@skku.edu

Fig. S1. Material characterization of our as-exfoliated monolayer WSe2 for device fabrication. a Photoluminescence spectrum of monolayer WSe2 under 633-nm laser showed the bright single-peak emission at 751 nm as the indirect to direct bandgap transition from few-layer to monolayer WSe2. b Raman spectrum of monolayer WSe2 under 633-nm laser showed the softening of E2g1&A1g modes and the change of spectral weight in monolayer WSe2 as compared to the few-layer WSe2 [55].

Fig. S2. Schematic illustrations of van der Waals integration of MAPbI3 perovskite with WSe2 field-effect transistors (FETs). Prefabricated WSe2 FET (1), PbI2 lamination (2), vapor-phase conversion of MAPbI3 perovskite in CVD furnace (3) and MAPbI3/WSe2 FET (4).

Fig. S3. Single-layer WSe2 FET before MAPbI3 integration. a Optical image of a single-layer WSe2 FET before integration of MAPbI3 perovskite. The white scale bar is 10 μm. b Output characteristics (IDS-VDS) of the device under white light illumination and in dark. c Transfer characteristics (IDS-VBG) of the device under white light illumination and in dark.

Fig. S4. a The time-domain photoresponse of the MAPbI3/WSe2 photodiode after negative lateral poling process measured under 532-nm laser illumination with 7 Hz of chopping frequency. b The photocurrent (Iph) and response time () estimated from the mean values of the current steps during on and off states. The Iph and  were extracted from part a (red dashed frame): Iph ~ 83.3 pA and  ~ 450 µsec at VDS = 0 V.

Fig. S5.  Negatively-poled MAPbI3/WSe2 photodiodes. a, b Output characteristics (IDS-VDS) of MAPbI3/WSe2 FET and MAPbI3 FET measured after negative lateral poling process in dark (a) and under 532-nm laser illumination (b), showing that the diode behaviors were prominent in the device integrated with WSe2. All the measurements were conducted at 79 K.

Fig. S6. Gate-tunable properties of MAPbI3/WSe2 FETs. a Gate-dependent output curves (IDS-VDS) of MAPbI3/WSe2 FET with Au contact electrodes under 532-nm laser illumination. b The comparison of gate-dependent open circuit voltage (VOC) of MAPbI3/WSe2 FET either with graphene (red) or Au (blue) contact after negative lateral poling process.

Table S1. Summary of the photodiode parameters in different studies. Data are from this work and references.

| Device structure | Layer number | Contact | Wavelength (nm) | VOC (V) | EQE (%) [effective area] | Source |
| --- | --- | --- | --- | --- | --- | --- |
| MAPbI3/WSe2 | 1 | graphene | 532 | 1.08 | 91.3 [device area] | This work |
| MAPbI3/WSe2 | 1 | Au | 532 | 0.78 | 84.3 [device area] | This work |
| Split-gated WSe2 | 1 | Cr/Au | 532 | 0.70 | 0.1 [device area] | [56] |
| Split-gated WSe2 | 1 | Pd/Au and Ti/Au | 500-800 | 0.83 | 1.9 [split gate area] | [16] |
| Split-gated WSe2 | 1 | Pd/Au and Ti/Au | 500-800 | 0.75 | 1.9 [split gate area] | [16] |
| Split-gated WSe2 | 4 | Au | 405 | 0.73 | 30 [laser spot] | [46] |
| Split-gated WSe2 | 1 | Au | 473 | 1.05 | 2.2 [laser spot] | [46] |
| Split-gated WSe2 | 1 | graphite | 750 | N/A | 0.75 [laser spot] | [57] |
| Split-gated WSe2 | 1 | Au | 522 | 0.6 | 0.2 [laser spot] | [15] |
| Split-gated WSe2 | 1 | V/Au | 660 | N/A | 0.1 [laser spot] | [14] |
| AuCl3/MoS2 | ~75 | Pd and Cr/Au | 500 | ~0.5 | 15 at VDS = 0.1 V [device area] | [58] |
| Vertical diode structure WSe2 | N/A | Pt and graphite | 365 | N/A | 94 [device area] | [59] |
| Vertical diode structure n-MoS2/p-MoS2 | ~50 | graphene/Au | 300 | 0.169 | 80.7 [device area] | [60] |
| Vertical diode structure MoS2/AsP | ~82/~73 | Cr/Au | 520 | 0.61 | 71 [device area] | [61] |
| Vertical diode structure n-MoS2/p-MoS2 | ~50 | graphene/Au | 532 | 0.169 | 47.3 [device area] | [60] |
| Vertical diode structure (PEA)2SnI4/MoS2 | ~25 | graphite | 451 | N/A | 38.2 [device area] | [62] |
| Vertical diode structure FA0.85Cs0.15PbI3/PtSe2 | ~18 | Au | 808 | 0.23 | 14.9 [device area] | [63] |
| Vertical diode structure MoTe2/MoS2 | ~4/~10 | Pd/Au and Cr/Au | 637 | 0.51 | N/A | [64] |