Supplement

Procedure

The procedure for calculating the Gr, as referenced in Table 1, is described herein. Table 1 comprises several columns: the first column lists the serial number of the initial trial; the second column presents the initial diameter of the specimen (ΔD1) prior to grinding; the third column indicates the final diameter of the specimen (ΔD2) after grinding; the fourth column records the length of the specimen (L). The fifth column details the volume of the workpiece material removed, with the formula for this calculation provided in the sample calculation. The sixth column specifies the initial diameter of the grinding wheel (Δd1) before the grinding. The seventh column reports the graphite coupon wear observed under a microscope. The eighth column shows the final diameter of the grinding wheel (Δd2) after the grinding operation, which was calculated as the initial diameter of the wheel minus the graphite coupon wear. The ninth column quantifies the volume of wheel wear, and the final column presents the grinding ratio for the respective run, with the formulas available in Table 1.

The wear of the grinding wheel was measured in microns, and the calculations of the grinding ratio are presented with three decimal places, with figures rounded accordingly. A confirmation test for the Taguchi method was conducted, yielding satisfactory results.

Table 1 for the first trail (GR I)

| Sl. No. | ΔD1 (mm) | ΔD2 (mm) | L (mm) | The volume of workpiece removal (mm3) | Δd1 (mm) | Graphite Coupon wear (mm) | Δd2 (mm) | The volume of wheel wear (mm3) | Gr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 30.506 | 30.209 | 35.5 | 502.771 | 489.52 | 0.00169 | 489.518 | 46.132 | 10.89 |
| 2 | 30.45 | 30.164 | 35.5 | 483.344 | 489.21 | 0.00185 | 489.208 | 50.467 | 9.57 |
| 3 | 30.451 | 30.172 | 35.5 | 471.584 | 489.17 | 0.00187 | 489.168 | 51.009 | 9.24 |
| 4 | 30.52 | 30.22 | 35.5 | 508.0591 | 489.09 | 0.0017 | 489.0883 | 46.3644 | 10.95 |
| 5 | 30.447 | 30.159 | 35.5 | 486.66 | 489.05 | 0.0018 | 489.048 | 49.087 | 9.91 |
| 6 | 30.503 | 30.20 | 35.5 | 512.827 | 488.97 | 0.00221 | 488.967 | 60.258 | 8.51 |
| 7 | 30.450 | 30.171 | 35.5 | 471.569 | 488.93 | 0.00179 | 488.928 | 48.803 | 9.66 |
| 8 | 30.456 | 30.152 | 35.5 | 513.714 | 488.85 | 0.00217 | 488.847 | 59.153 | 8.68 |
| 9 | 30.459 | 30.166 | 35.5 | 495.264 | 488.81 | 0.00224 | 488.807 | 61.056 | 8.11 |

Table 2 for the second trail (GR-II)

| Sl. No. | ΔD1 (mm) | ΔD2 (mm) | L (mm) | The volume of workpiece removal (mm3) | Δd1 (mm) | Graphite Coupon wear (mm) | Δd2 (mm) | The volume of wheel wear (mm3) | Gr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 30.542 | 30.123 | 35.5 | 708.713 | 488.188 | 0.0022 | 488.1858 | 59.890 | 11.39 |
| 2 | 30.516 | 30.116 | 35.5 | 676.207 | 488.180 | 0.0023 | 488.1777 | 62.616 | 10.43 |
| 3 | 30.457 | 30.118 | 35.5 | 572.547 | 488.162 | 0.0022 | 488.1598 | 59.887 | 9.46 |
| 4 | 30.453 | 30.141 | 35.5 | 527.111 | 488.168 | 0.0017 | 488.1663 | 46.277 | 11.19 |
| 5 | 30.51 | 30.214 | 35.5 | 501.152 | 488.156 | 0.0017 | 488.1543 | 46.275 | 10.30 |
| 6 | 30.547 | 30.194 | 35.5 | 597.826 | 488.150 | 0.0022 | 488.1478 | 59.885 | 9.63 |
| 7 | 30.448 | 30.154 | 35.5 | 496.766 | 488.148 | 0.0017 | 488.1463 | 47.173 | 10.53 |
| 8 | 30.446 | 30.116 | 35.5 | 557.227 | 488.142 | 0.0019 | 488.1401 | 51.718 | 10.42 |
| 9 | 30.452 | 30.134 | 35.5 | 537.177 | 488.120 | 0.0024 | 488.1176 | 65.325 | 8.21 |