Supplementary Material Figure 1. Chemical structure of Metformin HCl (ChemDraw™ Ultra Ver. 15.0.; CambridgeSoft, Cambridge, MA, USA)

Supplementary Material Figure 2. ATR-FTIR spectra of : a) Raw Metformin HCl; b) SD Met (25% PR); c) SD Metformin (50% PR); d) SD Metformin (75% PR); e) SD Metformin (100% PR); and f) all.

Supplementary Material Figure 3. Raman spectra of:  a) Raw Metform HCl and b) SD Metformin (25% PR).

| Spray Drying Conditions |  |
| --- | --- |
| Parameter |  |
| Inlet Temperature | 150 ˚C |
| Aspirator Rate | 100% 40 m3/hour |
| Pump rate % (Feed Rate) | 25% (7.5 mL/min) 50% (15 mL/min) 75% (22.5 mL/min) 100% (30 mL/min) |
| Gas Flow | 670 L/hour 55 mm Hg |
| Feed Solution Concentration | 0.1% w/v |
| Solvent | Methanol |
| Atomizer and Drying gas | UHP Nitrogen |
| Nozzle type and diameter | Stainless steel 0.7mm |

Supplementary Material Table I. Advanced spray drying parameters for metformin spray dried (SD) powders from methanol (MeOH) solution using advanced organic solution closed-mode spray drying particle engineering design.

Supplementary Material Table II. Spraying drying pump rates with corresponding outlet temperatures.

| System Composition | Outlet Temperature (C) |
| --- | --- |
| SD Metformin (25% PR) | 80-83 |
| SD Metformin (50% PR) | 64-65 |
| SD Metformin (75% PR) | 62 |
| SD Metformin (100% PR) | 53 |

Supplementary Material Table III. Particle size volumetric diameter (Dv) by laser sizer diffraction for SD metformin particles (mean ± SD, n=3).

| System Compositon | Dv10 (µm) | Dv50 (µm) | Dv90 (µm) | Mean ± std dev (µm) | Span |
| --- | --- | --- | --- | --- | --- |
| SD Metformin (25% PR) | 0.266±0.05 | 0.348±0.05 | 0.522±0.080 | 0.363±0.059 | 0.735 |
| SD Metformin (50% PR) | 0.652±0.09 | 0.897±0.14 | 1.366±0.22 | 0.959±0.16 | 0.795 |
| SD Metformin (75% PR) | 0.357±0.05 | 0.46±0.08 | 0.685±0.12 | 0.482±0.08 | 0.712 |
| SD Metformin (100% PR) | 0.469±0.12 | 0.621±0.18 | 0.937±0.28 | 0.653±0.19 | 0.752 |

Supplementary Material Table IV. Particle size diameters by image analysis. (n=100, Mean ± SD).

| System Composition | Mean Size (µm) ± Std Dev | Range (µm) |
| --- | --- | --- |
| Raw Metformin HCl | 281.49±135.35 | 797.85-94.32 |
| SD Metformin (25% PR) | 5.622±2.397 | 0.859-17.547 |
| SD Metformin (50% PR) | 1.1±0.295 | 0.552-1.805 |
| SD Metformin (75% PR) | 3.134±1.503 | 0.888-8.465 |
| SD Metformin (100% PR) | 3.147±2.279 | 0.721-12.285 |

Supplementary Material Table V. DSC phase transition values for raw and SD metformin powders. (n = 3, Mean ± SD).

| System Composition | Tpeak (⁰C) | Enthalpy (J/g) |
| --- | --- | --- |
| Raw Metformin HCl | 226.81±0.16 | 312.2±5.20 |
| SD Metformin (25% PR) | 225.29±0.01 | 306.9±7.45 |
| SD Metformin (50% PR) | 225.54±0.35 | 300.43±11.94 |
| SD Metformin (75% PR) | 225.64±0.42 | 301.6±6.58 |
| SD Metformin (100% PR) | 225.58±0.42 | 302.6±6.58 |

Supplementary Material Table VI.  KFT residual water content values (n=3, mean ± SD) for SD metformin powders.

| System Composition | Residual Water content (% w/w) |
| --- | --- |
| Raw Metformin HCl | 0.33±0.13 |
| SD Metformin (25% PR) | 3.41±2.39 |
| SD Metformin (50% PR) | 1.31±1.28 |
| SD Metformin (75% PR) | 1.74±0.03 |
| SD Metformin (100% PR) | 1.45±0.34 |

Supplementary Material Table VII. In vitro aerosol dispersion parameters including mass median aerodynamic diameter (MMAD), geometric standard deviation (GSD), fine particle fraction (FPF), respirable fraction (RF), and emitted dose (ED). (n=3, mean ± SD).

| System Composition | ED (%) | FPF (%) | RF (%) | MMAD (m) | GSD (m) |
| --- | --- | --- | --- | --- | --- |
| Aerolizer® |  |  |  |  |  |
| SD Metformin (25% PR) | 99.1119 | 25.422.11 | 79.381.31 | 5.570.17 | 1.900.05 |
| SD Metformin (50% PR) | 99.560.31 | 26.581.19 | 77.182.17 | 5.820.12 | 1.810.07 |
| SD Metformin (75% PR) | 98.881.04 | 28.662.08 | 80.290.89 | 5.40.19 | 1.840.04 |
| SD Metformin (100% PR) | 99.470.23 | 52.063.89 | 92.090.27 | 3.610.51 | 1.790.07 |
| NeoHaler™ |  |  |  |  |  |
| SD Metformin (25% PR) | 99.720.49 | 27.391.44 | 65.575.5 | 6.90.36 | 1.780.08 |
| SD Metformin (50% PR) | 99.870.22 | 32.052.46 | 53.561.36 | 5.120.29 | 2.250.04 |
| SD Metformin (75% PR) | 97.911.80 | 35.084.73 | 77.486.23 | 4.621.24 | 1.870.1 |
| SD Metformin (100% PR) | 99.870.22 | 26.640.97 | 612.17 | 5.600.57 | 1.790.07 |
| HandiHaler® |  |  |  |  |  |
| SD Metformin (25% PR) | 99.870.22 | 26.640.67 | 612.17 | 70.32 | 1.910.8 |
| SD Metformin (50% PR) | 99.310.63 | 31.683.5 | 66.874.05 | 7.070.58 | 2.400.70 |
| SD Metformin (75% PR) | 917.97 | 24.038.1 | 43.5313.16 | 8.951.30 | 2.470.22 |
| SD Metformin (100% PR) | 94.749.10 | 27.366.05 | 55.954.12 | 7.530.16 | 1.860.11 |