# Supplementary Data

# Injectable PLGA-based in situ forming subconjunctival implant for sustained ocular delivery of ketotifen fumarate: Formulation, drug release, and biocompatibility studies

Nur Mita 1,2, Xuejia Kang 1,3, Pengyu Chen3, Oladiran Fasina4, Shenise Howard5, Anna-Catherine Bowden5, Richard J. McMullen Jr.5,6, Amol Suryawanshi7, R. Jayachandra Babu 1,*

1Department of Drug Discovery and Development, Harrison College of Pharmacy, Auburn University, AL 36849, USA

2Faculty of Pharmacy, Mulawarman University, Samarinda, Kalimantan Timur, 75119, Indonesia

3Materials Research and Education Center, Materials Engineering, Department of Mechanical Engineering, Auburn University, Auburn, AL 36849, USA

4Department of Biosystems Engineering, Samuel Ginn College of Engineering, Auburn University, Auburn, AL 36849, USA

5Department of Clinical Sciences, College of Veterinary Medicine, Auburn University, AL 36849, USA

6Equine Department, Vetsuisse Faculty, University of Zurich, 8057 Zurich, Switzerland

7Department of Population Health and Pathobiology, College of Veterinary Medicine, North Carolina State University, Raleigh, NC, USA

*Corresponding author

R. Jayachandra Babu: ramapjb@auburn.edu
List of Supplementary Table and Figures

Table S1. The needle dimensions used in the injectability parameters prediction

Figure S1. Comparison of initial burst release at 24 hours for different PLGA concentrations and various release-modifying agents

Figure S2. HPLC chromatogram of ketotifen fumarate (100 μg/mL) compared to the diluent (blank) for baseline assessment

Figure S3. Calibration curve of ketotifen fumarate: Plot of peak area versus concentration (μg/mL) obtained from HPLC analysis

Table S1. The needle dimensions used in the injectability parameters prediction

| Needle Dimension | 𝑅n (mm) |
| --- | --- |
| 19 Gauge | 0.69 |
| 20 Gauge | 0.60 |
| 21 Gauge | 0.51 |
| 25 Gauge | 0.26 |
| 27 Gauge | 0.21 |

Figure S1. Comparison of initial burst release at 24 hours for different PLGA concentrations and various release-modifying agents

Figure S2. HPLC chromatogram of ketotifen fumarate (100 μg/mL) compared to the diluent (blank) for baseline assessment

Figure S3. Calibration curve of ketotifen fumarate: Plot of peak area versus concentration (μg/mL) obtained from HPLC analysis