PLGA–Phospholipid Hybrid Oleogel In Situ Forming Implant for Sustained 30-Day Co-Delivery of Donepezil and Memantine

Baljinder Singh1, Weranga Rajapaksha1, Haripriya Koppisetti1, Deepa Nakmode1, Yunmei Song1, Sanjay Garg1*

1Centre for Pharmaceutical Innovation (CPI), School of Pharmacy and Biomedical Science, College of Health, Adelaide University, Adelaide, SA, Australia

Corresponding Author- Sanjay.garg@adelaide.edu.au

Supplementary Table 1: Formulation screening matrix summarizing the effects of lipid type, PLGA composition, oils, solvents, and additives on implant formation, in vitro release behaviour, and physical stability. The table outlines the systematic optimization process used to identify the final DM00PG‑M13 formulation.

| Component Category | Ingredient | Conc (%w/w) | Implant Formation | In vitro Release | Stability |
| --- | --- | --- | --- | --- | --- |
| Lipoid Type | Lipoid- S100 | 10–80% | Yes | BR → CR (conc-dependent) | Stable |
|  | Lipoid- E80 |  | Weak gel | BR | Unstable (colour change after 1 month) |
| PLGA Type | PLGA 50:50 | 2.5–30% | Yes | CR | Stable |
|  | PLGA 75:25 |  | Yes | Very slow CR | Stable |
|  | PLGA 85:15 |  | Yes | Very slow CR | Stable |
|  | 50:50 + 75:25 |  | Yes | Very slow CR | Stable |
|  | 50:50 + 85:15 |  | No | – | Phase separation |
|  | 50:50 + 75:25 + 85:15 |  | No | – | Phase separation |
| Oils | Captex 300 | 10–70% | Yes | BR | Stable |
|  | Captex 355 |  | Yes | BR → CR | Stable |
|  | Sesame oil |  | Yes | CR | Stable |
|  | Castor oil |  | Yes | Very slow CR | Stable |
|  | Captex 300 + Sesame |  | Yes | Very slow CR | Stable |
|  | Captex 355 + Sesame |  | Yes | Very slow CR | Stable |
|  | Captex 300 + Castor |  | Yes (became viscous after 1 week) | – | Unstable |
|  | Captex 355 + Castor |  | Yes (became viscous after 1 week) | – | Unstable |
|  | Captex 355 + Sesame + Castor |  | No | – | Unstable |
| Polymers | Poloxamer 407 | 2–10% | Yes | BR | Phase separation (2 weeks) |
|  | Ethyl cellulose |  | Yes | BR | Stable |
|  | Poloxamer 407 + EC |  | No | – | – |
| Solvents | Ethanol | 6–30% | Yes | Initial BR | Stable |
|  | PEG 400 | 5–10% | Yes | Initial BR | Stable |
|  | DMSO | 5–10% | Yes | Very slow CR | Stable |
|  | NMP | 10–30% | Yes | CR | Stable |
|  | Benzyl alcohol (BA) | 10–20% | Yes | BR | Stable |
|  | DMSO + BA | 30–60% | Yes | BR | Stable |
|  | DMSO + Ethanol |  | Yes | BR | Stable |
|  | DMSO + BB |  | Yes | BR (memantine) | Stable |
|  | PEG 400 + Triacetin + BA |  | No | – | Phase separation (24 h) |
|  | BB + BA + Ethanol |  | No | – | Phase separation (24 h) |
|  | PEG 400 + BA + BB |  | No | – | Phase separation (24 h) |
|  | NMP + BB |  | Yes | BR | Stable |
|  | GF + Triacetin + Ethanol |  | Yes | BR | Stable |
|  | BB + Ethanol |  | No | – | Phase separation (24 h) |
|  | Triacetin + Ethanol + PEG 400 |  | No | – | Phase separation (24 h) |
|  | Triacetin + Ethanol |  | Yes | – | Too viscous |
|  | NMP + GF |  | No | – | Phase separation (24 h) |
|  | GF + Ethanol |  | No | – | Phase separation (24 h) |
|  | NMP + GF + Ethanol |  | No | – | Phase separation (24 h) |
| Other Additives | Tween (varied) | 0.3–1% | Yes | BR | – |
|  | IPM | 5% | No | – | Phase separation (24 h) |
|  | Stearic acid | 3–5% | No | – | Phase separation |
|  | Cholesterol | 3% | No | – | Phase separation |

BR- Burst release; CR-controlled release.

Supplementary Fig 2: Visual confirmation of cohesive in situ depot formation (highlighted with blue dye) within the porcine muscle tissue immediately following intramuscular delivery.