Supporting Information

Deep Learning-based Multimodal Analysis for Transition Metal Dichalcogenides

Shivani Bhawsar1, Mengqi Fang1, Abdus Salam Sarkar1, Siwei Chen1, and Eui-Hyeok Yang1,2

1Department of Mechanical Engineering, Stevens Institute of Technology

2Center for Quantum Science and Engineering, Stevens Institute of Technology

eyang@stevens.edu *Corresponding author

Table S1 Comparison of exemplary ML-based studies for TMD characterization.

| S.No | Model | TMDs | No. of images | Number of layers | Input dimension | Training duration | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | Convolutional neural network | WSe2, MoS2 and hBN | 580 | monolayer | 2592 × 1944 | 23 min | 8 |
| 2. | Support vector machine | Graphene | 18 | monolayer, bilayer, >=3 layers | 2592 × 1944 |  | 37 |
| 3. | Convolutional neural network | MoS2 | 800 | monolayer, bilayer, trilayer, multilayer | 96 × 96 | 3h for 100 epochs | 14 |
| 4. | Convolutional neural network | graphene, hBN, 2H-phase semiconducting and metallic TMDs, 1T-HfSe2, black phosphorous, CrI3, RuCl3, and ZrTe5 | 917 | monolayer, 2–6L for bilayer to 6-layer, and >6 for greater than 6 layers) | 1636 × 1088 | 30 h 56 min 23 s | 15 |
| 5. | Convolutional neural network | MoS2, Graphene | 960 | monolayer, bilayer | 512 × 512 |  | 38 |
| 6. | cGAN (Our method) | MoS2, WS2, WSe2, heterostructures | 100 | Monolayer, bilayer, trilayer, four layers, bulk(>4) | 780 × 588 | 3h for 200 epochs | 23 |