Table S1. The timeline table for the efficiency and stability evolution of Pb-free Halide perovskites for metals (Sn, Bi, Sb and AgBi-based Rudoffite perovskites).

| Tin-based Perovskite Solar Cells |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Year | Structure | Initial PCE | Inst. | Life time | Test condition | Ref |
| 2014.3.18 | FTO/TiO2/CH3NH3SnI3-XBrX/Spiro-OMeTAD/Au | 5.73 | Northwestern U | T80=12 h | dark storing in N2, JV test regularly | 1 |
| 2014.5.1 | FTO/TiO2/CH3NH3SnI3/Spiro-OMeTAD/ | 6.4 | U Oxford | none | none | 2 |
| 2016.8.29 | ITO/PEDOT:PSS/FASnI3/PCBM/BCP/Ag | 6.22 | U Toledo | T85=30 d | dark storing in N2, JV test regularly | 3 |
| 2017.4.21 | FTO/TiO2/FASnI3/PTAA/Au | 7.14 | Northwestern U | T80=40 min | AM 1.5G, ambient air (ISOS-L-1) | 4 |
|  |  |  |  | T96=1000 h | dark storing in N2 |  |
| 2017.7.14 | ITO/PEDOT:PSS/ FA0.75MA0.25SnI3/PCBM/BCP/Ag | 8.12 | Peking U | T80=400 h | storing in N2, JV test regularly | 5 |
| 2017.9.22 | ITO/PEDOT:PSS/FASnI3/PCBM/BCP/Al | 9.0 | U.Groningen | T96≈2 h | continuous 1 sun light in N2 | 6 |
|  |  |  |  | T59=76 h | continuous 1 sun light in 20% humidity |  |
| 2018.10.9 | ITO/PEDOT:PSS/ FA0.75MA0.25SnI3/PCBM/BCP/Al | 9.06 | NJUPT | T75=30 d | dark storing in N2, JV test regularly | 7 |
| 2018.10.9 | ITO/PEDOT:PSS/GAxFA(0.98−x)SnI3–1%EDAI2/PCBM/BCP/Ag | 9.6 | NCTU, Taiwan | T80=96 h, T30=150 h | Dark storing in RH 60%, JV test regularly | 8 |
|  |  |  |  | T100=170 h | Dark storing in RH 20%, JV test regularly |  |
|  |  |  |  | T100=2000 h | Dark storing in N2, JV test regularly PCE increased from 7.3% to 9.6%. |  |
| 2019.8.18 | FTO/PEDOT:PSS/FA0.98EDA0.01SnI3/ PCBM/BCP/Au Ag | 10.18 | UEC, Japan | none | none | 9 |
| 2020.3.6 | ITO/PEDOT/PEA0.15FA0.85SnI3-SCN/ICBA/BCP/Ag | 12.4 | ShanghaiTech U | T90=3800 h | dark storing in N2, JV test regularly | 10 |
|  |  |  |  | T50=5 h | AM 1.5G, OC in N2 ISOS-L |  |
| 2020.4.16 | FTO/PEDOT:PSS/ GeI2-(FA0.9EA0.1)0.98EDA0.01SnI3/PCBM/BCP/Ag/Au | 13.24 | UEC, Japan | none | none | 11 |
| 2021.2.3 | ITO/PEDOT:PSS/FASnI3/PCBM/BCP/Ag | 13.4 | Peking U | T91=4800 h | dark storing in N2, JV test regularly | 12 |
|  |  |  |  | T82=300 h | AM 1.5G, OC in N2, ISOS-L |  |
| 2021.7.23 | ITO/PEDOT:PSS/FASnI3/FPEABr(2D/3D)/PCBM/BCP/Al | 14.81 | SUST, China | T80=432 h | dark storing in N2, JV test regularly | 13 |
|  |  |  |  | T30≈0.5 h | dark storing in Air RH 75%, JV test regularly |  |
|  |  |  |  | T65≈ 1h | Heating press, 85 °C, JV test regularly |  |
|  |  |  |  | T70≈ 2.5 h | AM 1.5G, JV test regularly |  |
| 2024.1.29 | ITO/PEDOT:PSS/FASnI3(TPPF)/PCBM/BCP/Ag | 15.38 | Huaqiao U, China | T99=3000 h | dark storing in N2, JV test regularly | 14 |
|  |  |  |  | T93=500 h | AM 1.5G in N2?, MPP? |  |
|  |  |  |  | T98= 33.3 h | dark storing in Air RH 30%, JV test regularly |  |
|  |  |  |  | T100=11 h | dark storing in N2, heating 85 °C, JV test regularly |  |
| 2024.4.2 | ITO/PEDOT:PSS/FASnI3/FPEABr/ICBA/Ag | 15.7 |  | None | None | 15 |
| Bismuth-based Perovskite Solar Cells |  |  |  |  |  |  |
| Year | Structure | Initial PCE | Inst. | Life time | Test condition | Ref |
| 2015.9.29 | FTO/TiO2/Cs3Bi2I9/HTL/Au | 1.09 | Uppsala U | none | dark storing in air RH 10%, JV test regularly, PCE from 0.17 to 0.29. | 16 |
| 2017.8.25 | FTO/TiO2/ MA3Bi2I9/ Spiro-OMeTAD/Au | 1.64 | Hubei U | T100=2550 h | dark storing in N2, JV test regularly | 17 |
| 2018.4.16 | FTO/TiO2/MA3Bi2I9/P3HT/Au | 3.17 | Swansea U | T97=1440 h | ?dark storing in air, JV test regularly? | 18 |
|  |  |  |  | T87=375 h | AM 1.5G in air, MPPT, ISOS-L-1 |  |
| 2018.4.21 | FTO/TiO2/Cs3Bi2I9/CuI | 3.20 | NUST, China | T57=912 h | dark storing in air RH 45%, JV test regularly | 19 |
| 2019.12.2 | FTO/TiO2/0.5Cs3Bi2I9-Ag3Bi2I9/PDBD-T/Au | 3.59 | USTC, China | T80=1680 h | dark storing in air RH 35%, JV test regularly | 20 |
|  |  |  |  | T90=450 h | dark storing in N2, and heating at 85 degrees |  |
| 2021.9.1 | FTO/TiO2/Cs2AgBiBr6/Spiro-OMeTAD/Ag | 4.23 | Jilin U | T85=1080 h | dark storing in air, JV test regularly | 21 |
|  |  |  |  | T98=6 h | AM 1.5G in air, MPPT |  |
| 2022.6.13 | ITO/SnO2/Cs2AgBiBr6/Spiro-OMeTAD/Au | 6.37 | BUT, China | T95=1400 h | Light illumination in N2 at 20 degrees | 22 |
|  |  |  |  | T91=1400 h | Dark storing in N2 at 85 degrees, JV test regularly |  |
|  |  |  |  | T84=1400 h | Light illumination in N2 at 85 degrees |  |
|  |  |  |  | T42=1400 h | Light illumination in air RH 85% at 85 degrees |  |
| 2024.3.19 | FTO/TiO2/CsBiSCl2/Spiro-OMeTAD/Au | 10.38 | SJTU, China | T97=4500 h | Dark storing in air, JV test regularly | 23 |
|  |  |  |  | T93=200 h | AM 1.5G, light illumination |  |
| Sb-based Perovskite Solar Cells |  |  |  |  |  |  |
| Year | Structure | Initial PCE | Inst. | Life time | Test condition | Ref |
| 2017.9.13 | ITO/PEDOT:PSS/MA3Sb2I9/PCBM/BCP/Al | 2.04 | Academia Sinica, Taiwan | T10=720 h | Dark storing in N2, JV test regularly | 24 |
| 2018.9.25 | ITO/Cu:NiO/MA3Sb2I9/ZnO/Al | 2.69 | IACS, India | T80=360 h | Dark storing in air, JV test regularly | 25 |
| 2020.3.16 | FTO/TiO2/MA3Sb2I9–xClx/Spiro-OMeTAD/Au | 3.34 | NCEPU, China | T90=4000 h | Room light illumination in N2, OC | 26 |
|  |  |  |  | T92=1400 h | Dark storing in air RH 30%, JV test regularly |  |
| 2022.1.15 | ITO/PEDOT:PSS/Cs3Sb2ClxI9−x/PCBM/Al | 3.42 | IACS, India | none | none | 27 |
| Rudorffite AgBiX solar cells |  |  |  |  |  |  |
| Year | Structure | Initial PCE | Inst. | Life time | Test condition | Ref |
| 2016.6.29 | FTO/TiO2/AgBi2I7/P3HT/Au | 1.22 | U Toronto | T100=240 h | Dark storing in air, JV test regularly | 28 |
| 2017.5.8 | FTO/TiO2/Ag2BiI5/P3HT/Au | 2.10 | Uppsala U | T99.8=960 h | Dark storing in N2, JV test regularly | 29 |
| 2017.6.28 | FTO/TiO2/Ag3BiI6/PTAA/Au | 4.30 | CEREBA, Japan | none | none | 30 |

Table S2. Single cell modules and Tandem modules from industry. The table encompasses certified and no-certified data.

| Company | Module Eff (%) (c=certified) | Aperture/Active area (cm2) | Ref |
| --- | --- | --- | --- |
| Single cell modules |  |  |  |
| Microquanta Semiconductor | 21.8 | 19.35 | 31, 32 |
| Wuxi Utmolight Technology | 19.5 | 810.1 | 33 |
|  | 18.2 | 7200 | 34 |
|  | 20.7 | 810 | 35 |
| Kunshan GCL Optoelectronic Material | 15.31 | 1246.16 | 36 |
|  | 18.04 | 20000 |  |
|  | 19.04 | 20000 |  |
| WonderSolar | 12.5 | 100 | 37 |
| Toshiba | 11.6 | 802 | 38-40 |
|  | 16.6 | 703 |  |
| Panasonic | 17.9 | 804 | 41 |
| Saule Technologies | 17 10 | 100 | 42, 43 |
| Solaronix SA | 14.9 12 | 1 100 | 42, 44 |
| Renshine Solar | 18 | 20000 | 45 |
|  | 18.4 | 72 |  |
|  | 20.86 | 927.5 |  |
| DaZheng | 13-15 | 6000 |  |
| SolaEon Technology | 19.2 c | 1027.1 | 46 |
|  | 21.63 | 1200 |  |
| Mellow Energy | 21.5 | 800.9 | 47 |
|  | 20.79 | 900 |  |
| Singfilm Solar | 22.6 | 30.25 | 48 |
| Solertix | 20.7 | 2.6 | 49 |
| Sunflex | 16.8 | 1225 | 50 |
| Rollshine | 19.71 | 100 | 51 |
| Solliance | 12.6 | 0.1 | 52 |
| PSC/Si Tandem |  |  |  |
| LONGI | 33.9 | 1 | 53 |
|  | 33.5 | 1 | 54 |
|  | 31.8 | 1 | 55 |
|  | 30.1 | 275.56 | 56 |
| Auner | 25.45 30.83 | 275.6 25 | 45 |
| Tongwei | 23.84 | 220.5 |  |
| KANEKA | 29.20 | 64 | 45 |
| OXFORD PV | 28.60 | 258.1 | 57 |
|  | 25.0 | 16800 (1.68 m2) | 58 |
|  | 26.9 | 17000 (1.6 m2, 1m x 1.7m) | 59 |
| Trina Solar | 28.53 | 16 | 60 |
| GCL | 27.34 | 2,050 | 45 |
|  | 26.36 | 17,100 |  |
|  | 26.34 | 2,048 |  |
|  | 26.17 | 1028.6 |  |
| Tandem PV | 26 | 100 | 61 |
| PeroNova | 28 | 900 | 62 |
| Microquanta Semiconductor | 26.63 | 20 | 63 |
| Solertix | 28.4 | 4.4 | 64 |
| 3Sun | 28.7 | 9 | 65 |
| PSC/PSC Tandem |  |  |  |
| Renshine Solar | 24.50 | 20.25 | 66 |
|  | 21.7 | 20.25 |  |
| SolaEon Technology | 21.95 | 1200 | 46 |

References

1.	F. Hao, C.C. Stoumpos, D.H. Cao, R.P.H. Chang and M.G. Kanatzidis, Nat. Photonics. 8, 489-494 (2014).https://doi.org/10.1038/nphoton.2014.82

2.	N.K. Noel, S.D. Stranks, A. Abate, C. Wehrenfennig, S. Guarnera, A.-A. Haghighirad, A. Sadhanala, G.E. Eperon, S.K. Pathak, M.B. Johnston, A. Petrozza, L.M. Herz and H.J. Snaith, Energy Environ. Sci. 7, 3061-3068 (2014).https://doi.org/10.1039/C4EE01076K

3.	W. Liao, D. Zhao, Y. Yu, C.R. Grice, C. Wang, A.J. Cimaroli, P. Schulz, W. Meng, K. Zhu, R.G. Xiong and Y. Yan, Adv. Mater. 28, 9333-9340 (2016).https://doi.org/10.1002/adma.201602992

4.	W. Ke, C.C. Stoumpos, M. Zhu, L. Mao, I. Spanopoulos, J. Liu, O.Y. Kontsevoi, M. Chen, D. Sarma and Y. Zhang, Science advances. 3, e1701293 (2017).https://doi.org/10.1126/sciadv.1701293

5.	Z. Zhao, F. Gu, Y. Li, W. Sun, S. Ye, H. Rao, Z. Liu, Z. Bian and C. Huang, Advanced Science. 4, 1700204 (2017).https://doi.org/10.1002/advs.201700204s

6.	S. Shao, J. Liu, G. Portale, H.-H. Fang, G.R. Blake, G.H. ten Brink, L.J.A. Koster and M.A. Loi, Advanced Energy Materials. 8, 1702019 (2018).https://doi.org/10.1002/aenm.201702019

7.	X. Liu, K. Yan, D. Tan, X. Liang, H. Zhang and W. Huang, ACS Energy Lett. 3, 2701-2707 (2018).https://doi.org/10.1021/acsenergylett.8b01588

8.	E. Jokar, C.H. Chien, C.M. Tsai, A. Fathi and E.W.G. Diau, Adv. Mater. 31, 1804835 (2019).https://doi.org/10.1002/adma.201804835

9.	M.A. Kamarudin, D. Hirotani, Z. Wang, K. Hamada, K. Nishimura, Q. Shen, T. Toyoda, S. Iikubo, T. Minemoto, K. Yoshino and S. Hayase, The Journal of Physical Chemistry Letters. 10, 5277-5283 (2019).https://doi.org/10.1021/acs.jpclett.9b02024

10.	X. Jiang, F. Wang, Q. Wei, H. Li, Y. Shang, W. Zhou, C. Wang, P. Cheng, Q. Chen, L. Chen and Z. Ning, Nat. Commun. 11, 1245 (2020).https://doi.org/10.1038/s41467-020-15078-2

11.	K. Nishimura, M.A. Kamarudin, D. Hirotani, K. Hamada, Q. Shen, S. Iikubo, T. Minemoto, K. Yoshino and S. Hayase, Nano Energy. 74, 104858 (2020).https://doi.org/10.1016/j.nanoen.2020.104858

12.	C. Wang, Y. Zhang, F. Gu, Z. Zhao, H. Li, H. Jiang, Z. Bian and Z. Liu, Matter. 4, 709-721 (2021).https://doi.org/10.1016/j.matt.2020.11.012

13.	B.-B. Yu, Z. Chen, Y. Zhu, Y. Wang, B. Han, G. Chen, X. Zhang, Z. Du and Z. He, Adv. Mater. 33, 2102055 (2021).https://doi.org/10.1002/adma.202102055

14.	J. Chen, J. Luo, E. Hou, P. Song, Y. Li, C. Sun, W. Feng, S. Cheng, H. Zhang, L. Xie, C. Tian and Z. Wei, Nat. Photonics. 18, 464-470 (2024).https://doi.org/10.1038/s41566-024-01381-7

15.	Y. Shi, Z. Zhu, D. Miao, Y. Ding and Q. Mi, ACS Energy Lett. 9, 1895-1897 (2024).https://doi.org/10.1021/acsenergylett.4c00529

16.	B.-W. Park, B. Philippe, X. Zhang, H. Rensmo, G. Boschloo and E.M.J. Johansson, Adv. Mater. 27, 6806-6813 (2015).https://doi.org/10.1002/adma.201501978

17.	Z. Zhang, X. Li, X. Xia, Z. Wang, Z. Huang, B. Lei and Y. Gao, The Journal of Physical Chemistry Letters. 8, 4300-4307 (2017).https://doi.org/10.1016/j.matt.2020.11.012

18.	S.M. Jain, D. Phuyal, M.L. Davies, M. Li, B. Philippe, C. De Castro, Z. Qiu, J. Kim, T. Watson, W.C. Tsoi, O. Karis, H. Rensmo, G. Boschloo, T. Edvinsson and J.R. Durrant, Nano Energy. 49, 614-624 (2018).https://doi.org/10.1016/j.nanoen.2018.05.003

19.	F. Bai, Y. Hu, Y. Hu, T. Qiu, X. Miao and S. Zhang, Sol. Energy Mater. Sol. Cells. 184, 15-21 (2018).https://doi.org/10.1016/j.solmat.2018.04.032

20.	W. Hu, X. He, Z. Fang, W. Lian, Y. Shang, X. Li, W. Zhou, M. Zhang, T. Chen, Y. Lu, L. Zhang, L. Ding and S. Yang, Nano Energy. 68, 104362 (2020).https://doi.org/10.1016/j.nanoen.2019.104362

21.	B. Wang, N. Li, L. Yang, C. Dall’Agnese, A.K. Jena, T. Miyasaka and X.-F. Wang, Journal of the American Chemical Society. 143, 14877-14883 (2021).https://doi.org/10.1021/jacs.1c07200

22.	Z. Zhang, Q. Sun, Y. Lu, F. Lu, X. Mu, S.-H. Wei and M. Sui, Nat. Commun. 13, 3397 (2022).https://doi.org/10.1038/s41467-022-31016-w

23.	J. Huang, H. Wang, C. Jia, H. Yang, Y. Tang, K. Gou, Y. Zhou and D. Zhang, The Journal of Physical Chemistry Letters. 15, 3383-3389 (2024).https://doi.org/10.1021/acs.jpclett.4c00310

24.	K.M. Boopathi, P. Karuppuswamy, A. Singh, C. Hanmandlu, L. Lin, S.A. Abbas, C.C. Chang, P.C. Wang, G. Li and C.W. Chu, Journal of Materials Chemistry A. 5, 20843-20850 (2017).http://dx.doi.org/10.1039/C7TA06679A

25.	S. Chatterjee and A.J. Pal, ACS Appl. Mater. Interfaces. 10, 35194-35205 (2018).https://doi.org/10.1021/acsami.8b12018

26.	Y. Yang, C. Liu, M. Cai, Y. Liao, Y. Ding, S. Ma, X. Liu, M. Guli, S. Dai and M.K. Nazeeruddin, ACS Appl. Mater. Interfaces. 12, 17062-17069 (2020).https://doi.org/10.1021/acsami.0c00681

27.	G. Paul and A.J. Pal, Solar Energy. 232, 196-203 (2022).https://doi.org/10.1016/j.solener.2021.12.056

28.	Y. Kim, Z. Yang, A. Jain, O. Voznyy, G.-H. Kim, M. Liu, L.N. Quan, F.P. García de Arquer, R. Comin, J.Z. Fan and E.H. Sargent, Angew. Chem. Int. Ed. 55, 9586-9590 (2016).https://doi.org/10.1002/anie.201603608

29.	H. Zhu, M. Pan, M.B. Johansson and E.M.J. Johansson, ChemSusChem. 10, 2592-2596 (2017).https://doi.org/10.1002/cssc.201700634

30.	I. Turkevych, S. Kazaoui, E. Ito, T. Urano, K. Yamada, H. Tomiyasu, H. Yamagishi, M. Kondo and S. Aramaki, ChemSusChem. 10, 3754-3759 (2017).https://doi.org/10.1002/cssc.201700980

31.	Microquanta, 21.8%, Microquanta won the champion in the perovskite field of CPVS Best Research-Cell Efficiencies, 2023, https://www.microquanta.com/#/pc/new/125.

32.	P. Zhu, C. Chen, J. Dai, Y. Zhang, R. Mao, S. Chen, J. Huang and J. Zhu, Adv. Mater. 36, 2307357 (2024).https://doi.org/10.1002/adma.202307357

33.	M.A. Green, E.D. Dunlop, M. Yoshita, N. Kopidakis, K. Bothe, G. Siefer and X. Hao, Progress in Photovoltaics: Research and Applications. 32, 3-13 (2024).https://doi.org/10.1002/pip.3750

34.	R. Peleg, Wuxi UtmoLight Technology announces 18.2% efficiency for large area perovskite solar module, 2020, https://www.perovskite-info.com/wuxi-utmolight-technology-announces-182-efficiency-large-area-perovskite-solar.

35.	R. Peleg, Wuxi UtmoLight reports 20.7% steady-state efficiency for its perovskite solar modules, 2024, https://www.perovskite-info.com/wuxi-utmolight-reports-207-steady-state-efficiency-its-perovskite-solar-modules.

36.	PVTIME, 19.04%! GCL Perovskite Hits High Conversion Efficiency on Single-junction Perovskite Modules (1,000mmx2,000mm), 2024, https://www.pvtime.org/19-04-gcl-perovskite-hits-high-conversion-efficiency-on-single-junction-perovskite-modules-1000mmx2000mm/.

37.	A. Mei, Y. Sheng, Y. Ming, Y. Hu, Y. Rong, W. Zhang, S. Luo, G. Na, C. Tian and X. Hou, Joule. 4, 2646-2660 (2020).https://doi.org/10.1016/j.joule.2020.09.010

38.	V. Thompson, Toshiba claims 16.6% efficiency for polymer film-based large-area perovskite solar module, 2023, https://www.pv-magazine.com/2023/08/25/toshiba-claims-16-6-efficiency-for-polymer-film-based-large-area-perovskite-solar-module/.

39.	Toshiba, Toshiba’s Polymer Film-Based Perovskite Large-Area Photovoltaic Module Reaches Record Power Conversion Efficiency of 15.1%, 2021, https://news.toshiba.com/press-releases/press-release-details/2021/Toshibas-Polymer-Film-Based-Perovskite-Large-Area-Photovoltaic-Module-Reaches-Record-Power-Conversion-Efficiency-of-15.1/default.aspx.

40.	Toshiba, Toshiba’s Perovskite Photovoltaic Modules have the World’s Highest Solar Cell Power Conversion Efficiency, 2018, https://www.global.toshiba/ww/news/corporate/2018/08/tp0901.html.

41.	E. Bellini, Panasonic testing BIPV glass based on perovskites, 2023, https://www.pv-magazine.com/2023/09/05/panasonic-testing-bipv-glass-based-on-perovskites/.

42.	A. Extance, Nature. 570, 429-432 (2019).https://doi.org/10.1038/d41586-019-01985-y

43.	G. Overton, Saule prints flexible perovskite solar modules with consistent 10% efficiency, 2019, https://www.laserfocusworld.com/detectors-imaging/article/14035450/saule-prints-flexible-perovskite-solar-modules-with-consistent-10-efficiency.

44.	SOLARONIX, Solaronix Achieves Major Breakthrough Toward Perovskite Solar Cell Industrialization, 2016, https://www.solaronix.com/news/solaronix-achieves-major-breakthrough-toward-perovskite-solar-cell-industrialization/.

45.	J. Zhao, CHINA ADVANCES TO GW-SCALE MASS PRODUCTION OF PEROVSKITE SOLAR CELLS, 2024, https://www.mitsui.com/mgssi/en/report/detail/__icsFiles/afieldfile/2024/08/13/2407_t_zhao_e.pdf.

46.	R. Peleg, SolaEon claims 21.95% efficiency of monolithic perovskite tandem solar cells, 2024, https://www.perovskite-info.com/solaeon-claims-2195-efficiency-monolithic-perovskite-tandem-solar-cells.

47.	PVTIME, 21.5%! Mellow Energy Sets Efficiency Record for Flexible Perovskite Module, 2023, https://www.pvtime.org/21-5-mellow-energy-sets-efficiency-record-for-flexible-perovskite-module/.

48.	E. Bellini, Singaporean startup achieves 22.6% efficiency for perovskite solar module, 2024, https://www.pv-magazine.com/2024/07/17/singaporean-startup-achieves-22-6-efficiency-for-perovskite-solar-module/.

49.	E. Bellini, Italian startup develops 20.7%-efficient mini perovskite solar modules with 99.6% geometrical fill factor, 2024, https://www.pv-magazine.com/2024/06/03/italian-startup-develops-20-7-efficient-mini-perovskite-solar-modules-with-99-6-geometrical-fill-factor/.

50.	SunFLex, 17.4%SunFLex´s large-area flexible perovskite efficiency breaks the record again!, 2024, https://www.sflex.cn/newsinfo/7294656.html.

51.	Rollshine, Efficiency breakthrough丨Rollshine's flexible perovskite module obtains SCM authoritative certification, 2024, https://mp.weixin.qq.com/s/d6cQFncy4UysShLbR7cWFg.

52.	Solliance, Solliance sets world record for roll-to-roll produced perovskite-based solar cells with a stabilized efficiency of 12,6%, 2024, https://www.solliance.eu/2017/solliance-sets-world-record-for-roll-to-roll-produced-perovskite-based-solar-cells-with-a-stabilized-efficiency-of-126/.

53.	NREL, Best Research-Cell Efficiency Chart, https://www.nrel.gov/pv/interactive-cell-efficiency.html.

54.	LONGi, LONGi announces new conversion efficiency of 33.5% for its silicon-perovskite tandem solar cells at Intersolar Europe 2023, 2023, https://www.longi.com/en/news/new-conversion-efficiency/.

55.	LONGi, LONGi announces the new efficiency of 31.8% for perovskite/crystalline silicon tandem solar cells based on commercial CZ silicon wafers, 2023, https://www.longi.com/en/news/new-efficiency-of-solar-cells/.

56.	R. Peleg, LONGi announces new world record efficiency of 30.1% for commercial M6 size wafer-level silicon-perovskite tandem solar cells, 2024, https://www.perovskite-info.com/longi-announces-new-world-record-efficiency-301-commercial-m6-size-wafer-level.

57.	V. Thompson, Oxford PV sets 28.6% efficiency record for full-size tandem cell, 2023, https://www.pv-magazine.com/2023/05/24/oxford-pv-sets-28-6-efficiency-record-for-full-size-tandem-cell.

58.	V. Thompson, Fraunhofer ISE, Oxford PV produce 25%-efficient perovskite-silicon tandem PV module, 2024, https://www.pv-magazine.com/2024/01/31/fraunhofer-ise-announces-25-efficient-perovskite-silicon-tandem-photovoltaic-module/.

59.	J. Gifford, Oxford PV unveils 26.9% perovskite tandem module efficiency record, 2024, https://www.pv-magazine.com/2024/06/19/oxford-pv-presents-26-9-cell-efficiency-record-at-intersolar-europe-2024/.

60.	PVTIME, Trina Solar Cancels Fundraising for 20GW Solar Cell and 10GW Module Projects, 2024, https://www.pvtime.org/trina-solar-cancels-fundraising-for-20gw-solar-cell-and-10gw-module-projects/.

61.	V. Thompson, US startup developing perovskite-silicon tandem panels with 26% efficiency, 2024, https://www.pv-magazine.com/2024/01/19/tandem-pv-raises-6-million/.

62.	V. Thompson, U.S. startup develops 28%-efficient perovskite-silicon tandem solar module, 2024, https://www.pv-magazine.com/2024/08/05/u-s-startup-develops-28-efficient-perovskite-silicon-tandem-solar-module/.

63.	S. Global, Microquanta claims record 26.63% efficiency on 4-terminal perovskite-Si tandem module, 2024, https://www.solarbeglobal.com/Microquanta-claims-record-26-63-efficiency-on-4-terminal-perovskite-Si-tandem-module/.

64.	The 4th tandemPV Workshop will be held from June 26-28, 2024, in Amsterdam, the Netherlands., https://tandempv.conexio-pse.de/.

65.	3Sun, Tandem 3SUN technology, a new efficiency record at 28.7%, 2024, https://www.3sun.com/en/search-news/news/2024/06/Tandem-3SUN-technology-a-new-efficiency-record.

66.	R. Peleg, RenShine Solar announces 24.5% efficiency for all-perovskite tandem cell module, 2022, https://www.perovskite-info.com/renshine-solar-announces-245-efficiency-all-perovskite-tandem-cell-module.