Supplementary Information

Self-assembled green composites of silk fibroin and microfibrillated cellulose

Melissa Puerta1, Diego Gomez-Maldonado2,3, Adriana Restrepo-Osorio1,2,4*, & Maria Soledad Peresin2*

1	New Materials Research Group, Universidad Pontificia Bolivariana, Medellín, Colombia

2	Sustainable Bio-Based Material Laboratory, College of Forestry, Wildlife and Environment, Auburn University, Auburn, AL, USA.

3	Fiber and Biopolymer Research Institute, Department of Plant & Soil Science, Texas Tech University, Lubbock, TX, USA.

4	Engineering School, Universidad Pontificia Bolivariana, Medellín, Colombia.

*Corresponding authors: soledad.peresin@auburn.edu, adriana.restrepo@upb.edu.co, adriana.restrepo@auburn.edu

Table SI. Summary of the TGA and MDSC data obtained from cryogels.

| Sample | Tonset [°C] | Tmax [°C] |  | Tg [°C] |
| --- | --- | --- | --- | --- |
| SFW | 261.73 | 287.35 |  | 179.29 |
| SFWI | 270.77 | 287 |  | 205.29 |
| MFC | 252.5 | 311.05 |  | 229.51 |
| MFCI | 266.85 | 326.87 |  | 242.72 |
| SFWMFC | 264.62 | 289.47 | 177.20 | 336.48 |
| SFWMFCI | 273.49 | 293.75 | 198.15 | 347.84 |

Figure S1. UV-Vis data for weight loss test.

Figure S2. UV-Vis data for weight loss test.

Figure S3. Statistically significant differences (p-values <0.05) for weight loss data.