[bookmark: _Ref56258078]Table I Summary of nanoindentation Surface Free Energy results on all analyzed samples.
	Sample
	Pull-off force 
(µN)
	SFE - JKR 
(mJ/m2)
	SFE - DMT (mJ/m2)

	Mica
	29 ± 3
	77 ± 15
	62 ± 7

	Bare germanium
	21 ± 2
	42 ± 8
	24 ± 5

	Silanized germanium
	3.5 ± 0.6
	1.55 ± 0.34
	0.9 ± 0.2

	Patterned germanium
	0.47 ± 0.2
	0.023 ± 0.016
	0.013 ± 0.009

	Patterned and silanized germanium
	0.2 ± 0.1
	0.0039 ± 0.0025
	0.0022 ± 0.0014
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Figure I Environmentally controlled glove-box system for the Nanoindenter.
2

image1.png
NanoindenteriNano





