Table I Summary of nanoindentation Surface Free Energy results on all analyzed samples.

| Sample | Pull-off force (µN) | SFE - JKR (mJ/m2) | SFE - DMT (mJ/m2) |
| --- | --- | --- | --- |
| Mica | 29 ± 3 | 77 ± 15 | 62 ± 7 |
| Bare germanium | 21 ± 2 | 42 ± 8 | 24 ± 5 |
| Silanized germanium | 3.5 ± 0.6 | 1.55 ± 0.34 | 0.9 ± 0.2 |
| Patterned germanium | 0.47 ± 0.2 | 0.023 ± 0.016 | 0.013 ± 0.009 |
| Patterned and silanized germanium | 0.2 ± 0.1 | 0.0039 ± 0.0025 | 0.0022 ± 0.0014 |

Figure I Environmentally controlled glove-box system for the Nanoindenter.