# SUPPLEMENTARY INFORMATION

Corresponding Author Email: robin.demeyere@seh.ox.ac.uk

# A MODIFIED TRENCH FIBRE PUSH-OUT METHOD TO EVALUATE INTERFACIAL FAILURE IN LONG FIBRE COMPOSITES

Robin M. G. De Meyere1 *, Kay Song2, Louise Gale3, Stephen Harris3, Ian Edmonds3, Thomas J. Marrow1, Eduardo Saiz4, Finn Giuliani4, David E. J. Armstrong1, Oriol Gavaldà-Diaz4

1Department of Materials, University of Oxford, Oxford, OX1 3PH, UK

2Department of Engineering Science, University of Oxford, Oxford, OX1 3PJ, UK

3Rolls-Royce plc, Derby, DE24 8BJ, UK

4Centre for Advanced Structural Ceramics, Department of Materials, Imperial College London, London, SW72AZ, UK

Keywords: Aerospace, Micromechanical Testing, Micromechanics Composites, CMC, Processing, SiC/SiC, SiCf/SiC, Nano-indentation, Interfaces, Interfacial Shear Strength, Fibre Push-out, Roughness

Ex-situ tests were performed on a Keysight Nanosuite G200 instrument as a control experiment to test whether the techniques produced similar results. There was a clear load plateau during fibre sliding inside the trench (FIG. 1) which enabled calculation of the ISS with minimal error. The ex-situ trench push-out also showed no fibre cracking.

FIG. 1: Load-displacement curve from the ex-situ trench push-out performed on a SiC/SiC composite with Tyranno type SA3 fibres and a thick BN interphase.

TABLE S1: Comparing the interfacial frictional stresses obtained from a half fibre and a full fibre trench push-out experiment in the SiC/BN/SiC composite with Hi-Nicalon fibres. The error on the load stems from standard deviation along the plateau whereas the fibre radius error quoted stems from uncertainties in measuring the fibre radius. Both errors propagate to the ISS.

|  | Units | Half Fibre | Full Fibre |
| --- | --- | --- | --- |
| Plateau Load | mN | 7.5 ± 0.3 | 13.5 ± 0.2 |
| Fibre Radius | μm | 4.0 ± 0.1 | 3.5 ± 0.1 |
| Interfacial (Frictional) Shear Stress | MPa | 23.8 ± 0.3 | 24.6 ± 0.3 |

TABLE S2: Mean values for loads, computed stresses and energies for all successful half fibres trench push-outs (6 Hi-Nicalon and 3 Tyranno SA3 tests). All sliding distances on the displacement controlled instrument were set to be the same. RMS roughness of the fibre surface were obtained from the nanoindenter surface topography analysis; all errors stem from standard deviations in the populations and express a minimum as artefacts such as crack formation in the CVI were not included.

| Fibre Type | Units | Hi-Nicalon | Tyranno Type SA3 |
| --- | --- | --- | --- |
| Plateau Load | mN | 5 ± 4 | 7 ± 1 |
| Maximum Load | mN | 22 ± 12 | 35 ± 20 |
| Plateau Shear Stress | MPa | 14 ± 7 | 20 ± 2 |
| Maximum Shear Stress | MPa | 200 ± 80 | 70 ± 25 |
| RRMS Fibre Roughness | nm | 35 ± 5 | 100 ± 5 |