# Supporting Information

Single- or Double A-Site Cations in A3Bi2I9 Bismuth Perovskites – What is the suitable choice?

Feray Ünlü1, Ashish Kulkarni2, Khan Lê1, Christoph Bohr1, Andrea Bliesener3, Seren Dilara Öz1, Ajay Kumar Jena4, Yoichi Ando3, Tsutomu Miyasaka4, Thomas Kirchartz2,5, and Sanjay Mathur1*

1 Department for Chemistry, Institute for Inorganic Chemistry, University of Cologne, Greinstr. 6, 50939 Cologne, Germany.

2IEK5-Photovoltaics, Forschungszentrum Jülich, 52425 Jülich, Germany

3 Physics Institute II, University of Cologne, Zülpicher Str. 77, 50937 Cologne, Germany

4Graduate School of Engineering, Toin University of Yokohama, Aoba, Yokohama 225-8503, Japan

5Faculty of Engineering and CENIDE, University of Duisburg-Essen, Carl-Benz-Str. 199, 47057 Duisburg, Germany

Corresponding author: sanjay.mathur@uni-koeln.de

Figure S 1: Taken photographs of the various organic-inorganic and all-inorganic bismuth iodide thin films, spin-coated on FTO/TiO2 substrates.

Figure S 2: XRD pattern of MA3Bi2I9 thin film on mesoporous TiO2, coated on FTO substrate (peaks labeled as # belong to FTO/TiO2), compared to the simulated pattern from cif data of Eckhardt et al.1

Figure S 3: XRD pattern of GA3Bi2I9 on FTO/TiO2 substrate (peaks labeled as # belong to FTO/TiO2), compared with simulated pattern from cif data of Szklarz et al. 2

Figure S 4: XRD pattern of Cs3Bi2I9 thin film on mesoporous TiO2, coated on FTO substrate (peaks labeled as # belong to FTO/TiO2), compared to the simulated pattern from cif data of Chabot and Parthé.3

Figure S 5: XRD pattern of Rb3Bi2I9 thin film on mesoporous TiO2, coated on FTO substrate (peaks labeled as # belong to FTO/TiO2), compared to the simulated pattern from cif data of Lehner et al.4

Figure S6: Tauc plots for indirect band gap determination of organic-inorganic bismuth iodide thin films (a-b) and Tauc plots for direct band gap determination of organic-inorganic bismuth iodide thin films (c-d). The first absorption edge belongs to the excitonic absorption and the second edge was taken as optical band gap.

Table S1: Extrapolated band gaps for organic-inorganic bismuth iodide thin films from the Tauc plots in Figure S5.

|  | Direct band gap (eV) |  | Indirect band gap (eV) |  |
| --- | --- | --- | --- | --- |
|  | excitonic | optical | excitonic | optical |
| MA3Bi2I9 | 2.5 | 2.9 | 2.4 | 2.8 |
| FA3Bi2I9 | -- | 2.6 | -- | 1.7 |
| GA3Bi2I9 | 2.3 | 2.7 | 2.2 | 2.5 |
| DMA3Bi2I9 | 2.2 | 2.4 | 2.0 | 2.1 |

Figure S7: a) Tauc plots for indirect band gap determination of all-inorganic bismuth iodide thin films. b) Tauc plots for direct band gap determination of all-inorganic bismuth iodide thin films.

Table S2: Extrapolated band gaps for all-inorganic bismuth iodide thin films from the Tauc plots in Figure S6.

|  | Direct band gap (eV) |  | Indirect band gap (eV) |  |
| --- | --- | --- | --- | --- |
|  | excitonic | optical | excitonic | optical |
| Cs3Bi2I9 | 1.9 | 2.3 | 1.5 | 1.8 |
| Rb3Bi2I9 | 2.2 | 2.5 | 2.0 | 2.1 |
| K3Bi2I9 | 2.0 | 2.3 | 1.9 | 1.7 |
| Na3Bi2I9 | 2.3 | 2.5 | 2.2 | 2.2 |
| Li3Bi2I9 | 2.3 | 2.5 | 2.2 | 2.3 |

Figure S 8: J-V curves of a) organic-inorganic and b) all-inorganic bismuth iodide based champion solar cells in forward (solid curves) and reverse (dashed curves) scans.

Table S 3: Open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF) and power conversion efficiency (PCE) from the champion solar cell IV curves, with organic-inorganic bismuth iodide thin films in forward and reverse scan.

|  | Scan direction | VOC (V) | JSC (mA∙cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| MA3Bi2I9 | forward | 0.65 | 0.54 | 63.0 | 0.22 |
|  | reverse | 0.65 | 0.56 | 56.8 | 0.21 |
| FA3Bi2I9 | forward | 0.51 | 0.090 | 48.2 | 0.02 |
|  | reverse | 0.50 | 0.050 | 90.3 | 0.02 |
| GA3Bi2I9 | forward | 0.52 | 0.036 | 59.4 | 0.011 |
|  | reverse | 0.31 | 0.036 | 51.5 | 0.006 |
| DMA3Bi2I9 | forward | 0.54 | 0.073 | 43.4 | 0.017 |
|  | reverse | 0.53 | 0.065 | 49.2 | 0.017 |

Table S 4: Open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF) and power conversion efficiency (PCE) from the champion solar cell IV curves with all-inorganic bismuth iodide thin films in forward and reverse scan.

|  | Scan direction | VOC (V) | JSC (mA∙cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| Cs3Bi2I9 | forward | 0.62 | 0.59 | 48.7 | 0.18 |
|  | reverse | 0.65 | 0.42 | 86.1 | 0.24 |
| K3Bi2I9 | forward | 0.55 | 0.21 | 86.0 | 0.10 |
|  | reverse | 0.52 | 0.32 | 50.2 | 0.08 |
| Rb3Bi2I9 | forward | 0.60 | 0.32 | 51.7 | 0.10 |
|  | reverse | 0.61 | 0.29 | 61.8 | 0.11 |
| Na3Bi2I9 | forward | 0.45 | 0.41 | 80.5 | 0.15 |
|  | reverse | 0.36 | 0.40 | 41.9 | 0.06 |

Figure S9: Solar cell parameters for perovskite solar cells (n = 8) using monovalent organic cations MA+ (black), DMA+ (cyan), FA+ (blue) and GA+ (magenta) displayed as a) power conversion efficiency (PCE), b) short-circuit current density (JSC) c) open-circuit voltage (VOC) d) fill factor (FF). The parameters were extracted from forward and reverse (dashed) J-V scans and displayed together.

Figure S10: Solar cell parameters for perovskite solar cells (n = 8) using alkali metal cations Cs+ (black), K+ (cyan), Rb+ (blue), Na+ (magenta) displayed as a) PCE, b) JSC c) VOC d) FF. The parameters were extracted from forward and reverse (dashed) J-V scans and displayed together.

Figure S11: a) Optical and scanning electron microscope image of hexagonal shape perovskite grains on glass, and grain sizes of the 10 mol% Cs doped MA3Bi2I9 perovskites on FTO. b) Tauc plot for indirect band gap determination of the mixed cation bismuth iodide thin film with 10 mol% Cs amount and extrapolated band gap values for each excitonic and optical absorptions. c) Tauc plot for direct band gap determination of Cs/MA bismuth iodide thin film.

Figure S 12: Cross-section and Top-view SEM (inset scale bar 1 µm) images of double-cation bismuth iodide thin film from 45 wt% precursor solution leading to a capping layer on top of the mesoporous TiO2. The scale bar is 500 nm.

Figure S 13:Best performing J-V curves of the devices based on MA3Bi2I9 (blue curve) and (Cs10MA90)3Bi2I9 (black curve) sensitized solar cells.

Figure S14: Solar cell parameters for perovskite solar cells (n = 18) using double-cation Cs/MA displayed as a) PCE, b) JSC c) VOC d) FF. The parameters were extracted from forward (black boxes) and reverse (blue boxes) J-V scans and displayed together.