Supplementary information

High strain rate in situ micropillar compression of a Zr-based metallic glass

Rajaprakash Ramachandramoorthy,1,2,** Fan Yang,3 Daniele Casari,2 Moritz Stolpe,4 Manish Jain,2 Jakob Schwiedrzik,2 Johann Michler,2 Jamie J. Kruzic5 and James P. Best1,5,6,**

1 Max-Planck-Institut für Eisenforschung GmbH, Max-Planck-Straße 1, 40237 Düsseldorf, Germany

2 Laboratory for Mechanics of Materials and Nanostructures, Empa – Swiss Federal Institute for Materials Science and Technology, 3603 Thun, Switzerland

3 Institut für Materialphysik im Weltraum, Deutsches Zentrum für Luft- und Raumfahrt (DLR), 51170 Köln, Germany

4 Heraeus Amloy Technologies GmbH, Heraeusstraße 12-14, 63405 Hanau, Germany

5 School of Mechanical and Manufacturing Engineering, UNSW Sydney, Sydney NSW 2052, Australia

6 Institut für Metallkunde und Materialphysik, RWTH Aachen University, 52056 Aachen, Germany

** Corresponding authors: Dr. Rajaprakash Ramachandramoorthy (r.ram@mpie.de) & Dr. James P. Best (j.best@mpie.de)

Table T1. Overview of micropillar testing geometries.

| Sample | Top diameter | Corrected height | Aspect ratio | Taper angle | # pillars |
| --- | --- | --- | --- | --- | --- |
|  | µm | µm | - | ° | - |
| (AMZ4)L | 2.95 ± 0.02 | 7.14 ± 0.10 | 2.32 ± 0.04 | 3.50 ± 0.19 | 21 |
| (AMZ4)H | 2.93 ± 0.02 | 6.74 ± 0.11 | 2.21 ± 0.03 | 3.25 ± 0.30 | 20 |

Table T2. Summary of sampling rates and load noise at tests conducted at different strain rates.

|  | Strain rate (s-1) |  |  |  |
| --- | --- | --- | --- | --- |
|  | 5.0 × 10-4 | 0.05 | 5.82 | 520 |
| Sampling rate (Hz) | 5 | 200 | 50000 | 1.0 × 106 |
| Noise level S.D. (mN) | 0.0016 | 0.0107 | 0.34 | 0.7 |

Figure S1. High fidelity raw data captured at a sampling rate of 1 MHz during high-speed BMG micropillar compression that results in a strain rate of ~520 s-1. Raw load versus time data with a noise floor standard deviation of 0.7 mN (a). Raw displacement versus time data with a noise floor standard deviation of 13 nm (b). Both insets show a magnified view of the elastic loading region of ~47.5 µs, highlighting a time interval of 1 µs between sampling points in both load and displacement.