Synthesis and Behavior of Bulk Iron Nitride Soft Magnets via High Pressure Spark Plasma Sintering – Supplemental Information

Fig. S1.  Backscattered electron (BSE) SEM image of the surface of a sintered iron nitride toroid.

Table S1.  WDS results collected from the surface of a sintered iron nitride toroid.

| Location | Fe (Atomic %) | N (Atomic %) |
| --- | --- | --- |
| Grain center | 81.3 | 18.7 |
| Grain boundary | 84.2 | 15.8 |

Fig. S2.  Schematic of graphite die assembly for the fabrication of iron nitride based toroids using SPS.